## Slide 1
Superconducting Quantum computers
Technical University of Munich, TUM school of Natural Sciences
Walther-Meißner-Institute, Germany
Leon.Koch@wmi.badw.de
2nd Workshop on Silicon Sensors, Berg

## Slide 2
- ein Übersichtstalk zu “euren” qubits allgemein und einen etwas fokussierteren in Richtung Technologie
First introduce super conducting qubits
Then go into how to fabricate them and what are future challenges
Talk should be 45 min long

## Slide 3: Overview
Superconducting qubit
Quality
Scaling
Part I
Part II
Part III

## Slide 4: Quantum harmonic oscillators and transmon qubits
LC circuit with quadratic potential
Equal energy spacing unwanted
Introduce non linear inductivity
Josephson junction is key ingredient to form two level system
Qubit is a quantum mechanical two level system
Notes: Lets have a look at the bulding block that we use for computation the (qubits) and what these qubits are
Qubit = quantum mechanical TLS: quantum dots, trapped ions, photons, neutral atoms and superconducting circuits (artificial atoms) which is what I’m working with
One of the most promising approaches
In principle similar to something that we all know LC circuit
Can not address states individually => need anharmonicity => like a non linear inductor instead of the coil => Josephson junction
Transmon at the moment most widely used qubit

## Slide 5: Microscope image of qubit chip
1 mm
200 nm
Notes: Make a picture of only a single transmon

## Slide 6: The Josephson junction
Superconductor-Insulator- Superconductor trilayer (SIS)
Substrate
Aluminum
Aluminum
Aluminum
Oxide
200 nm
Notes: Lets talk a bit more about what a josephson junction is
Nothing magic in fact quite simple
Trilayer of metal insulator metal
Insulator acts as thin tunnel barrier the superconducting charge carriers can tunnel thorugh
If one calculates properties precisely on finds non linear inductance term (4th order
now we know that a qubit is almost like an LC circuitbut with a josephson junction instead of a coil
Lets compare its properties to a classical bit

## Slide 7: The Josephson junction
Superconductor-Insulator- Superconductor trilayer (SIS)
For qubits typically Al-AlO-Al
AlO builds tunnelbarrier (1.8 nm)
non-linear inductance
Substrate
Aluminum
Aluminum
Aluminum
Oxide
Notes: Lets talk a bit more about what a josephson junction is
Nothing magic in fact quite simple
Trilayer of metal insulator metal
Insulator acts as thin tunnel barrier the superconducting charge carriers can tunnel thorugh
If one calculates properties precisely on finds non linear inductance term (4th order
now we know that a qubit is almost like an LC circuitbut with a josephson junction instead of a coil
Lets compare its properties to a classical bit

## Slide 8: Bit vs. Qubit - Superposition
Quantum Bit (Qubit)
0 or 1
Combinations of 0 and 1 imagine a point on a (Bloch-)Sphere
Classical Bit
Notes: now we know that a qubit is almost like an LC circuit but with a josephson junction instead of a coil as inductive element
Lets compare its properties to a classical bit
Classical bit like a switch can be either in on or off 0 or 1
Qubit imagine like a sphere state represented by a point on this sphere / vector
Has some probability to be in 0 or 1 and a phase deoted by phi in the picture
If its not exatly at the poles then its in superposition which is what we mean if we say it can be in 0 and 1 at the same time
One bit bit or qubit is a bit boring and useless lets add another one

## Slide 9: Bit vs. Qubit - Entanglement
2 Classical Bits
2 Quantum Bits (Qubits)
qubits are no longer independent, measurement of one qubit has influence on all qubits
Each switch position can be described independently
“Spooky action at a distance” – Albert Einstein
Notes: One bit bit or qubit is a bit boring and useless lets add another one
So far so good what happens if we add another bit or qubit
Can also bring them into an combined state which is mathematically not just the sum of the individual states of the single qubits
Do something that we call entanglement
N-qubit state is not just sum of individual states of qubits
4 basis states with 4 probabilities (exponential scaling of states we can be in with our qubits) what people call state space or hilbertspace of the system

## Slide 10: Superconducting Qubits as sensors
Qubits are sensitive to single quasi particles
  exploit as meV phonon sensor
Can be used to detect single THz photons
Easy signal readout
Low thermal noise (mK environment)
Low noise amplifiers (quantum limited)
Qubit can be coupled to other systems and used for sensitive readout
Fink et al. PRA 22.5 (2024)

## Slide 11: Supraleitende Quantencomputer
Features
Artificial atoms
Individual control
Typical frequencies: GHz (microwave range)
Fast gates on 10 ns timescales
Semiconductor tools used for fabrication

## Slide 12: Challenges ahead (hardware centric)
Quality: identification of loss channels and noise sources (two-level fluctuators, quasi-particles and ionizing radiation, B-field fluctuations), mitigation (by design, by choice of materials, by fabrication), high fidelity
Number of qubits: cross-coupling and cross-talk, uniformity & reproducibility, scalable control, I/O, qubit size, thermal budget, connectivity, cryogenic electronics
Speed and control: fast coherence limited gates, pulse optimization, benchmarking sequences, multi-qubit operations & extended gate sets
System stability and connectivity: automated calibration & bring-up, run-time environment, characterization & verification, quantum/classical integration, (cryogenic) electronics
Lisenfeld, Jürgen, et al. "Electric field spectroscopy of material defects in transmon qubits." npj Quantum Information 5.1 (2019); Eagle quantum processor, IBM
Eagle quantum processor, IBM

## Slide 13: Part II
Superconducting qubit
Quality
Scaling
Part I
Part II
Part III

## Slide 14: Fermi`s golden rule
Decay rate can be influenced by the coupling strength (design)
and by the noise spectral density (fabrication)
J. M. Martinis et al., Phys. Rev. Lett. 95, 21 (2005); J. Gao et al., Appl. Phys. Lett. 92,15 (2008); J. Lisenfeld et al., Nat. comm. 6.1 (2015); G. Calusine et al., Appl. Phys. Lett. 112, 06 (2018); C. Müller et al., Rep. Prog. Phys. 82, 12 (2019); J. Biznárová arXiv: 2310.06797; M. Bal arXiv: 2304.13257
Notes: Lets start with Fermis golden rule which describes the decay rate between two quantum states that are coupled to a noise source. In order to lower this decay rate we can eigther decrease the coupling stregth by design
Second knob noise spectral density. That can be influenced by fabrication
In order to improve the noise spectral density one needs to eliminate loss channels. For sc qubits this means that one need to minimize the amount of TLS by cleaning procedures. Since TLSs are mainly hosted at the interfaces these are the areas of interest
Especially at interfaces (MA, SA) host many TLS. They couple to electric fiels qubit and exchange energy with it=> which in turn leads to decay of qubit from exited to ground state
Talk about bulk being crystal
Statements a few word on the main message of this slide

## Slide 15: Fabrication steps
Cleaned Si (100) substrate (10to 20)
DC magnetron sputtering 150 nm niobium
Spin coating, resist exposure (DLW)
Pattern transfer via RIE (chemistry)
Coplanar waveguide resonator fabrication steps
Ground plane fabrication
Notes: Participation ratios of our resonators (compared to other resonators?
Then we transferred our learnings from the fabrication of high quality resonators to qubit fabrication
Next I will shortly introduce the procedure we use to fabricate qubits
First of all we have to clean our silicon substrate to remove the native surface oxides
Sputter niobium thin film
Before continuing with an optical lithography step to define all structures that are larger than 1 µm
Finally we remove the resist and continue with the fabrication of the josephson junctions
Piranha
Solution consisting of H2SO4 and H2O2 (3:1 v/v)
Dissolves organic contaminations due to the formation of atomic oxygen
Immersion for 10 minutes in a 80 °C water bath
BOE
Buffered oxide etch (BOE) solution consisting of HF (7%), NH4F (35%) and H2O (58%)
Removes lossy oxide layer of Si substrate → strongly improves the substrate-metal interface
Last step prior to metal deposition, as substrate re-oxidizes (~5 minutes)
Immersion for 30 seconds at roomtemperature

## Slide 16: Fabrication steps
Bilayer resist system CSAR and PMMA
Josephson junction fabrication
Qubit fabrication steps
Ground plane fabrication
Cleaned Si (100) substrate (10to 20)
DC magnetron sputtering 150 nm niobium
Spin coating, resist exposure (DLW)
Pattern transfer via RIE (chemistry)
Resist removal
Post process cleaning

## Slide 17: Qubit fabrication steps
Al Evaporation and dynamic oxidation
90° rotation and evaporation of second layer
Resist stripping and metal liftoff
Bilayer resist system
Bilayer resist system CSAR and PMMA
Josephson junction fabrication
Repetition of electron beam process for bandaging using Ar-ion milling
Ground plane fabrication
Cleaned Si (100) substrate (10to 20)
DC magnetron sputtering 150 nm niobium
Spin coating, resist exposure (DLW)
Pattern transfer via RIE (chemistry)
Resist removal
Post process cleaning
Notes: Add details resitst thickness
Add ebeam and DLW

## Slide 18: Microscope image of qubit chip
1 mm
10 µm
200 nm
Notes: Moderately sized transmon
qubit

## Slide 19: Part III
Superconducting qubit
Quality
Scaling
Part I
Part II
Part III

## Slide 20: The Goal
Fault tolerant quantum computing
  Quantum error correction
  1000 logical qubits needed for real applications
  At the state of the art this means a million physical qubits
  is the error of the logical qubit is the code distance, is the error threshold (around 1%), is the error of the physical qubit,
Dennis, Eric, et al. "Topological quantum memory." Journal of Mathematical Physics 43.9 (2002)
Google Quantum AI. " Suppressing quantum errors by scaling a surface code logical qubit ". Nature 614 (2023)

## Slide 21: Chip architecture

## Slide 22: Chip architecture
Qubit
Tunable coupler
Flux line
Drive line
Readout line

## Slide 23: Chip architecture
17 qubits
48 lines needed
On average 2.8 lines per physical qubit

## Slide 24: Quality – Status quo
times
times
Dedicated QPU
17-Q QPU
60.4 µs
7.5 µs
420 µs
Google Willow
68 µs
89 µs
540 µs
> 5000
50
> 2100
17-qubit QPU
T1,med = 420 µs
T1,max 800 µs
Single qubits
Among world‘s best
  Qubit coherence
  time: median and quartiles on 17-qubit QPU, on single qubits
  time: median and quartiles on 17-qubit QPU, on single qubits
  : 50 on 17-qubit QPU
https://quantumai.google/static/site-assets/downloads/willow-spec-sheet.pdf

## Slide 25: Quality – Status quo
times
times
Dedicated QPU
17-Q QPU
60.4 µs
7.5 µs
420 µs
Google Willow
68 µs
89 µs
540 µs
> 5000
50
> 2100
1|2-Qu. Gate fid.
99.95 | 99.9 %
99.5 | 97.8 %
99.96|99.86 %
Glaser, Niklas J, "Controlled-controlled-phase gates for superconducting qubits mediated by a shared tunable coupler." Physical Review Applied 19.4 (2023)
  Internationally leading two-qubit gate fidelities of will be implemented on next-gen 17-Qubit
Adiabatic gate with closed-loop optimization
  Gate set: SU(2) and controlled-Z gate on 17-qubit QPU; CZ and iSWAP on 6-qubit QPU
  Gate fidelities: 99.48 % / 97.7 % median single-/two- qubit gate (RB); 99.95 % / 99.9 % on dedicated devices
  2-qubit gates
https://quantumai.google/static/site-assets/downloads/willow-spec-sheet.pdf

## Slide 26: Quality – Status quo
times
times
Dedicated QPU
17-Q QPU
60.4 µs
7.5 µs
420 µs
Google Willow
68 µs
89 µs
540 µs
> 5000
50
> 2100
1|2-Qu. Gate fid.
99.95 | 99.9 %
99.5 | 97.8 %
99.96|99.86 %
> 98 %
> 90 %
> 99.33 %
Readout fid.
  Multiplexed readout for 5 qubits demonstrated (limited by individual fidelities)
  Parametric amplifiers and Purcell-filters in development
  Transfer to large chips in progress
  Fidelity: Above 90 % on 17-qubit QPU (multiplexed); up to 98 %, improvements ongoing
  Readout
4-way
1-2
17
4-way
105
2-way
Readout
https://quantumai.google/static/site-assets/downloads/willow-spec-sheet.pdf

## Slide 27: Scaling up to 100 qubits
Scaling up the number of qubits requires additional technology and precision
Air bridges allow crossing of lines

## Slide 28: Scaling up to 100 qubits
Scaling up the number of qubits requires additional technology and precision
Air bridges allow crossing of lines

## Slide 29: Scaling up to 100 qubits
Scaling up the number of qubits requires additional technology and precision
Air bridges allow crossing of lines
Reproducibility in freq. targeting and coherence (outliers matter), yield

## Slide 30: Scaling up to 100 qubits
Scaling up the number of qubits requires additional technology and precision
Air bridges allow crossing of lines
Reproducibility in freq. targeting and coherence (outliers matter), yield
Flip chip bonding for routing and against crosstalk
Low aspect ratio TSVs to break modes

## Slide 31: Scaling up to 100 qubits
Scaling up the number of qubits requires additional technology and precision
Air bridges allow crossing of lines
Reproducibility in freq. targeting and coherence (outliers matter), yield
Flip chip bonding for routing and against crosstalk

## Slide 32: Scaling up to 1.000 qubits
High aspect ratio superconducting through substrate vias (TSVs)
Signal redistribution layers (RDLs)
High density coaxial lines (flex cables)
Advanced packaging depending on yield several qubit chips bonded to one interposer
Yost, Donna-Ruth W., et al. "Solid-state qubits integrated with superconducting through-silicon vias." npj Quantum Information 6.1 (2020)

## Slide 33: Scaling up to over 10.000 qubits
Cross talk might become a leading error source (due to line density)
Thermal and space budget is limited
  Cryogenic CMOS control electronics on different stages
Microwave inter chip couplers above 10.000 qubits
(Optical) inter fridge couplers above 100.000 qubits
Additional tuning knobs like TLS tuning
Circuit level scaling challenges (verification, testing, debugging)
Fault tolerant QC generated by Dall-E 3
Mohseni, Masoud, et al. "How to Build a Quantum Supercomputer: Scaling from Hundreds to Millions of Qubits." arXiv preprint arXiv:2411.10406 (2024)

## Slide 34: The Goal – from a different angle
Fault tolerant quantum computing
  Instead of increasing code distance reduce physical error rate
  Alternative qubits with high coherence and fidelity fluxonium, 0-pi qubit
  is the code distance, is the error threshold (around 1%), is the error of the physical qubit, is the error of the logical qubit

## Slide 35
Thank you for your attention
Stefan Filipp
Nicolas Arlt
Vera Bader
Daniil Bazulin
Niklas Bruckmoser
David Bunch
Julian Englhardt
Julius Feigl
Noelia Fernandez
Niklas Glaser
Christian Gnandt
Longxiang Huang
Gerhard Huber
Fabian Jochum
Kevin Kiener
Martin Knudsen
Leon Koch
Vincent Koch
Gleb Krylov
Benedikt Lezius
Klaus Liegener
Florian Maier
Frederik Pfeiffer
Léa Richard
Joao Romeiro
Federico Roy
Lasse Södergren
Saya Schöbe
Johannes Schirk
Christian Schneider
Malay Singh
Agata Skoczylas
Ivan Tsitsilin
Lucia Valor
Lukas Vetter
Florian Wallner
Rui Wang
Max Werninghaus
Jan Wozniak
Emily Wright