## Slide 1: Next Generation Depfet - PXD13
Alexander Bähr

## Slide 2: The DePFET
  MOSFET on n-substrate
  deep-n implant below gate
    potential minimum for electrons
    „internal gate“ (IG)
    conductivity modulated by electrons
      Source Follower
      Drain Current Readout
  reset via clear and clear gate
  good signal to noise
  unobstructed backside contact
  typical charge gain values ~420 pA/e-
  Applications:
    Belle II, BepiColombo, Athena, EDET, etc.
drain
source
Q(t)
signal(t)
clear gate
gate

## Slide 3: can we improve the depfet?
increase signal to noise minimize impact ionization reduce voltage variations reduce clear voltages

## Slide 4: Device Simulations
3D device simulation - study complex geometries
charge collection, clear, etc
source
gate
drain
clear gate
clear
internal gate
source
gate
drain
2D device simulation – DePFET transistor properties
charge gain, noise, impact ionization, etc

## Slide 5: Simulation – 2D scaling

## Slide 6: Simulation – 2D scaling
impact ionization
Electric Field
source
gate
drain
charge gain (@-70°C)

## Slide 7: Standard DePFET
implants of DEPFET (without clear):
p+ source/drain
deep-n (internal gate)
channel implant (threshold adjustment)
W/L=20 µm / 5 µm
charge gain ~420 pA/e- @20°C

## Slide 8: 1) DePfet with halo implant
tested in context of the ATHENA WFI (W. Treberspurg et al 2018 JINST 13 P09014)
reduces impact ionization (allows for example for up to 0.5 V more negative Vd)
increases charge gain by ~10% (460 pA/e- @20°C)
Reference technology

## Slide 9: 2) optimized “standard” technology
vary all standard implants (dose and energy)
keep halo as is
charge gain increasy by ~10% (500 pA/e- @20°C)

## Slide 10: 2 b ) vary halo implant
higher dose
further reduction of impact ionization
further increase of charge gain by ~10% (540 pA/e-)
higher possibility for parasitic channel below clear-gate

## Slide 11: 3) Super gq
source
gate
drain
internal gate
source
gate
drain
additional n-implant
gq~1 nA/e- @ 20°C

## Slide 12: 3) Super gq
super gq and scaling
charge gain (@-70°C)
impact ionization

## Slide 13: 3) Super gq
trade off
L=5 µm
W=20 µm

## Slide 14: 4) Focussing (HE) implant using a masked HE-implant
For selected test structures
high energy implant aligned to pixel structure
Quadropix: reduce intrinsic asymmetry
DePFET: sharpen pixel borders reduce susceptibility to bulk doping variations
Quadropix
4 DePFETs in one Superpixel
collection controllable by voltages
pixel border depends on collection state
Notes: 5 MeV implant @ ~3 µm depth; n-type

## Slide 15: Technology
Standard: reference
Super gq:
additional implant
drastic increase in S/N
(Masked) HE implant
For example for Quadropix
Minimize asymmetry of
charge collection
Optimized:
optimized implants
improved S/N

## Slide 16: DePFET Layout
prototype-/test-production
small test devices
no backside thinning
limit number of different „frames“
Athena-frame
64x64 pixels
75µm < pixel size < 130 µm
XS-frame
64x64 pixels
pixel size < 75 µm
Belle-frame
32x64 pixels
belle-type

## Slide 17: DePFET layouts - Standard
Belle Type
55 x 50 µm²
fast readout
Athena Type
130 x 130 µm²
imaging spectroscopy
Small Pixels
15 x 15 µm² to 30 x 30 µm²
“limit” test
drift 2
S
D
G
S
D
G
CG
CG
CL
CL
CL
D
D
S
G
G
CL
D
S
G
S
drift
drift
drift 1

## Slide 18: DePFET layouts – Multigate DePFETs
Multiple storages
Infinipix
2 storage nodes
selectable charge collection
suppress rolling shutter effects
Quadropix
4 storage nodes
selectable charge collection
suited for high precision polarimetry
RNDR DePFETs
repetitive non destructive readout (RNDR)
additional implant for transfer channel
subelectron noise
single electron resolution
S
D
G1
G2
TG
CG
S
S
G1
G2
G1
G2
D1
D2
D1
D2
D4
D3
CG
CL
CG
CL
CL
->see talk by W. Trebersburg

## Slide 19: Summary
DePFET Layouts | 
Belle DePFET | fast readout
Athena DePFET | spectroscopy
Small DePFET | 15 – 30 µm test devices
Infinipix | 2 storage nodes per pixel
Quadropix | 4 storage nodes per pixel
RNDR DePFET | low noise (subelectron)
12 wafers in production
test production; minimum of inspection
same layout on all wafers
production started October 2022 -> finished end of Juli 2023; diced August 2023
move of the HLL
technology (#Wafers)
reference (2)
reference + HE (2)
optimized (4)
optimized version b (2)
super gq (2)

## Slide 20: First results
die level measurements – IV characteristics, yield measurements, noise measurements
- yield: 31 standard Athena devices tested for shorts + 2 assembled chips
1 defective chip found so far
test setup – operation of prototype matrices, detailed performance qualification
- see talk by Sebastian

## Slide 21: Thanks for your attention
Alexander Bähr

## Slide 22: 3) Technology option super gq
Add deep-n implant on source side
localize internal gate to part of the channel
potential distribution – DePFET internal gate
expected gq of ~1.3 nA/e-
@W/L =20/5 (design)
@20°C

## Slide 23: 3) Super Gq 3d simulation of clear
Belle like geometry
super gq implant
simulation of clear process for different clear high voltages
drift
clear
gate
drain
source
lower IG potential
further optimization possible

## Slide 24: Derivation of standard Transistor Equations
drift
diffusion
consider in 1D
Vc
Vb
Vg
in strong inversion:
surface potential and surface charge
solve Poissons equ.
get as function of Q’ and Vext
charge sheet appr.
graded channel appr.
etc. ...