## Slide 1
Results of an aging study for the graphite coating of thin-gap RPCs for the ATLAS phase 2 upgrade
Davide Costa
on behalf of the MPP ATLAS Muon Group
DPG-Frühjahrstagung 2025
Göttingen – 31st March - 4th April 2025

## Slide 2
The role of graphite in RPCs
1
triple graphite layer edge
lower resistivity (<20 kΩ/◻) on edge to improve the high voltage distribution.
graphite coating
(ρs = 350 kΩ/◻)
graphite coating of the HPL electrodes
The graphite layer plays an important role in the performance of RPCs:
Ohmic contact uniformly distributes the field.
Transparent to prompt avalanche signal.
Limits rate capability
  An increase in total electrode resistance displaces the working point of the detector, worsening performance.
  The graphite layer must maintain a constant resistance over the whole operation of ATLAS at the rates expected for HL – LHC.
schematic drawing of RPC singlet
Voltage drop in RPC electrode
Charge per event
Event
rate
Electrode
resistance

## Slide 3
Introduction to aging
2
10 yrs HL
S.F. x 1
S.F. x 3
The principal aging phenomenon in RPCs is a decrease in rate capability
  Increase in total electrode resistance [i] leading to:
                Reduced applied to the gas
                Potential loss of field uniformity
Expectations for HL – LHC
  Charge per count →
  Max interaction rate in BIS →
  Effective exposure time (50%) →
Tests performed at different voltages to study what
impact acceleration rate has on aging.

## Slide 4
Aging studies at MPP
3
Investigating different contributions to aging under different conditions
The Graphite test
  10x10 cm2 Bakelite (HPL) plates
  Graphite coating on both sides
  Most similar to standard RPC configuration
  and to tests performed in the literature
The HPL test
  10x10 cm2 Bakelite (HPL) plates
  Uncoated
  Isolate effects of aging on bulk resistivity
ONGOING
ONGOING
The Irradiation test
  10x10 cm2 Bakelite (HPL) plates
  Graphite coating on both sides
  Behaviour of coating under heavy irradiation at the CHARM facility at CERN
PLANNED
The Graphite and HPL tests are currently being carried out in the clean room at MPP in Garching

## Slide 5
HPL test
4
No graphite coating. Electrical contact is ensured by squeezing the samples between brass foil electrodes, backed by insulating foam and PMMA plates.
Resistance of the sample is measured through the voltage drop across a read-out resistor.
Setup has been under test since 20/12/2024.

## Slide 6
HPL test
5
The test serves to isolate the contribution to aging from the HPL itself.
Carried out in the MPP clean room.

## Slide 7
HPL test – Results*
Results are consistent across samples.
For the moment, no significant aging effect has been observed.
Strong polarisation effect
* - As of 30/03/2025
increased from 200 to 500 V
Polarization of the sample
6

## Slide 8
Graphite test
7
Current is forced through the sample by applying a voltage across opposing electrodes.
Resistance of the sample is measured through the voltage drop across a read-out resistor.
Setup has been under test since 28/11/2024.

## Slide 9
Graphite test
8
Readout circuit
The test is being carried out in the MPP clean room to ensure stable environmental conditions, and to allow for continuous monitoring of environmental parameters.

## Slide 10
Graphite test
9
Additional terminals for surface resistance monitoring.
The test is being carried out in the MPP clean room to ensure stable environmental conditions, and to allow for continuous monitoring of environmental parameters.

## Slide 11
Graphite test – Results*
10
Results are consistent across samples.
For the moment, no significant aging effect has been observed.
Outside of an initial polarisation period and environmental effects, the current in the sample is constant.
* - As of 30/03/2025

## Slide 12
Graphite test – Results*
11
* - As of 30/03/2025
Results are consistent across samples.
For the moment, no significant aging effect has been observed.
Outside of an initial polarisation period and environmental effects, the current in the sample is constant.

## Slide 13
Graphite test – Results
12
“Spikes” are due to variations in environmental parameters ( mainly RH ).
Correction is non-trivial.
@ 800 V
@ 400 V
Current
Current
% RH
% RH

## Slide 14
Graphite test - Surface
13
Manually monitor surface resistance of the
graphite electrodes at regular intervals.
Small variations observed, but within acceptable limits ( for anode, for cathode @ 800 V).
Acceptance limit is 30%.

## Slide 15
Graphite test - Surface
14
Manually monitor surface resistance of the
graphite electrodes at regular intervals.
Small variations observed, but within acceptable limits ( for anode, for cathode @ 400 V).
Acceptance limit is 30%.

## Slide 16
Irradiation test
15
Radiation exposure could damage the graphite, further increasing electrode resistance.
Tests on legacy RPCs have been carried out using ( source at GIF++ ), but neutrons have greater potential to cause damage, and are a significant component of the spectrum present where the new RPCs will be installed.
Test will take place at the CHARM facility
(details incoming).
Spectrum in the hottest region of ATLAS. Y axis should be multiplied by 4000 to match expected integrated luminosity expected for HL - LHC

## Slide 17
Irradiation test
16
High radiation environment imposes technical challenges and regulatory restrictions.
Monitoring of bulk resistivity AND surface resistance must be carried out remotely, automatically, and reliably, for the whole duration of the test.
5 samples, prepared in the same way as the “Main” test, operated at 800 V.
1 week “dry run” planned at MPP.

## Slide 18
Future prospects
18
Test under irradiation at CHARM (planned for May).
Continue ongoing test until a safety factor 3 is reached.
Compositional analysis to better elucidate the mechanisms behind aging of RPC graphite paint.

## Slide 19
Conclusions
19
A SF of 1 has already been reached, satisfying certification requirements for production.
Ongoing tests have given us an improved understanding of the influence of environmental parameters on the behaviour of materials used in the construction of RPCs.
Graphite test
HPL test

## Slide 20
Thank you for your attention

## Slide 21
Extras

## Slide 22
Sample preparation
10 cm x 10 cm HPL plates, 1.3 mm thick, bulk resistivity ~Ωcm.
Graphite paint provided by KODEL. Already used for the CMS i-RPC system.
Higher surface resistivity square .
Lower surface resistivity strips ensure uniform distribution of the electric field.
2 brass foil contacts per side, secured with conductive glue.
Samples used both for “Graphite” and “Irradiation” tests.

## Slide 23
Sample preparation
1h @ 105 °C
1
2
3
4
x 2

## Slide 24
Sample preparation
1h @ 105 °C
1
2
3
4
x 2

## Slide 25
Graphite test – Results*
800 V
400 V

## Slide 26
HPL test
The test serves to isolate the contribution to aging from the HPL itself.
Carried out in the MPP clean room.

## Slide 27
HPL test
The test serves to isolate the contribution to aging from the HPL itself.
Carried out in the MPP clean room.

## Slide 28
HPL test
The test serves to isolate the contribution to aging from the HPL itself.
Carried out in the MPP clean room.

## Slide 29
HPL test – Results*

## Slide 30
Environmental parameters
Conductivity in the HPL is mainly due to internal water ions () [iii]
HPL is hygroscopic.
5 samples, baked for 3 h at 105 °C.
Kept at stable* T, RH and tested
at regular intervals.
Mass recovers to the initial value faster
than bulk resistivity.

## Slide 31
Temperature and current

## Slide 32
Environmental effects in “HPL”
200 [V]

## Slide 33
Correlation plots “Graphite”

## Slide 34
Correlation plots “HPL”
Test voltage raised 200 V → 500 V

## Slide 35
Correlation plots “HPL”
Before raising voltage to 500 V

## Slide 36
Irradiation test
protons from the PS, impinging on a copper target, provide a high intensity mixed field.
X 4 for HL - LHC

## Slide 37
Read-out resistors

## Slide 38
An HV PS provides power to the samples and a reference ground for measurement
Read-out resistors

## Slide 39
Read-out resistors
Relays, controlled by an Arduino, allow us to power the faces independently and switch between readout channels

## Slide 40
Read-out resistors
The PicoLog 1216 ADC is used for data taking.

## Slide 41
Location of BIS RPCs
Image Credit: ATLAS Collaboration [ii]

## Slide 42
Sources
Aielli, G., et. al (2003), Further advances in aging studies for RPCs, Nuclear Instrumentation and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment, 515(1-2), 335-341
ATLAS collaboration (2022), Technical Design Report for the Phase-II Upgrade of the ATLAS Muon Spectrometer.
G. Aielli (2024), Design and construction of RPC detectors, DRD1 gaseous detectors school, https://indico.cern.ch/event/1384298/contributions/6070891/attachments/2978847/5244587/RPC%20construction_DRD1%20school.pdf