## Slide 1: Data Handling Processor Chip Development
Second version of Data Handling Processor DHP 0.2 currently being implemented
  Scheduled for MPW production end of May  chip available approx. end of August
  IBM 90nm technology (still risk of MPW non-availability but change of technology would delay DHP 0.2 considerably)
Chip features
  64 channels (full size chip)
  C4 bump bonds
  Chip size 3.2 mm x 4.3 mm
  Static pedestal memory (JTAG update)
  Full implementation of data processing (some limits in max. occupancy and error detection & prevention due to limited implementation time)
  Improved data format (up to 26% bandwidth reduction)
  Fully implemented Switcher sequencer
  On-chip bias DACs and temperature sensor (U Barcelona)
  Gbit link with programmable pre-emphasis

## Slide 2: Data Handling Processor Chip Development
Preparation of second batch of PXD6 matrix production to support direct flip chip mounting of DHP 0.2
DHP 0.1 tests
  Electrical DHP test ongoing
    Gbit link
    JTAG communication
    Communication with DCD (tbd – see comment on flip-chip mounting below)
  Irradiation test (planned)
    TID (10-20 MeV electron beam at ELSA accelerator in Bonn): Gbit link performance, analog blocks, digital clock speed
    SEU (to be organized): memory and register data safety
Problems with flip chip mounting of DCD – DHP assemblies
  low bump connection yield
  Reflow process currently being optimized (use of flux, plasma oven)