## Slide 1: Testing PXD6 - summary and plans
Jelena Ninkovic for the HLL team

## Slide 2: PXD6 Batch 1 wafers
  L1 - lithography dummy but has some of the implantations
S1, W02 – hot wafers with ZMI=600nm
W21 – hot wafer with ZMI=1000nm and Plasma etching of Polysilicon
W11 – Reference wafer (not SOI material)
  Some parts of the wafer have 100nm thinner Oxide then the rest of the wafer
  Non of the copies of ILC matrices passed pretests
  Significant number of small Belle designed matrices passed pretests

## Slide 3: Back side diodes on SOI material
Handle wafer
n+
p+
Al
200nm Oxide
50mm
Direct bonding on 50mm silicon without mechanical support works and no increase in the leakage current was observed

## Slide 4: ILC vs. Belle in the testing differences
128 Drain connections 128
Gate connections 16
Physical columns 32
256 Physical rows 64
Clear SW
Gate SW
SW
ILC (2 fold read out)
Belle (4 fold read out)

## Slide 5: Hybrid 4.1
Statistics on the yield on
Hybrid 4.1 assembly
2.5 out of 14 adapters DCDB/DCDRO
SWB
All chips were taken into assembly without any precharacterisation !!!
Matrices are preselected

## Slide 6: Yield of the chips on the adapters
DCDRO
DCDRO
DCDB
DCDB

## Slide 7: Hybrid 4.1 plans
DCDB - characterization on chip level before flip chipping (Planned)
characterization after flip chipping (not yet planned)
optimization of ACDs parameters for functional chips before assembly
SWB - characterization on chip level before flip chipping (Planned)
characterization after flip chipping (not yet planned)
We will need this procedure also for the final Belle PXD assembly
Preparation of this will take additional time ….( 3-4 months ?)

## Slide 8: MiMa
Will soon become nice tool ….
low noise
flexible system
But can be used only as multiple (48) single depfet setup for the 4-fold read out
3 setups exist : Prags, MPI-HLL, LMU

## Slide 9
Hybrid 3.1 - S3B system (CURO + SW3)
PXD6 ILC Design can be used with Hybrid 3.1 (electrical identical with Hybrid 3.0 cut-out 4.3 x 9mm² instead of 5.3 x 10 mm²).
PXD6 Wafer:
  3 x ILC type (24 x 24 µm² - type used as DUT in TB2009)
  3 x ILC type VS (20 x 20 µm² - type as the best DUT TB2009)

## Slide 10: S3B system with Belle matrix
Prepared last Thursday
Matrix can be swithed ON/OFF
Reacts on light
DEPFET currents look ok
DAQ/Monitor was not ready for 4 fold read out
Hybrid is 2 times more noisy then usual
Further investigation is needed
One more hybrid of this kind will be prepared within the coming week.

## Slide 11: Dynamic measurements – Initial proposal
Decision made in Prague - to risky to use SAMTEC connectors better to prepare more hybrids each assembled with ASICs and Matrix