## Slide 1
SVD Ribs and SLM
M.Friedl, F.Buchsteiner, R.Thalmeier (HEPHY Vienna)
27 May 2014

## Slide 2
Introduction
Thermal Cycling
Sliding FW Endmount
Summary & Outlook

## Slide 3: SLM = Slide Lock Mechanism
Ladder mount concept:
  Fixed on backward side (Origin)
  Sliding on forward side to allow thermal movement

## Slide 4: Alternative Meanings
Second Life Magazine
Swiss vitamin drink
Selective Laser Melting

## Slide 5: How It Began
Informal discussion after February BPAC
  Does SLM really work?
  How smooth is the motion?
  Decided to perform tests with climate chamber to verify thermal motion due to CTE mismatch
Idea
  Mount ribs (with a priori unknown, but presumably low CTE) onto a support with high and known CTE
  Thermal cycling between 0 and 40°C
  Observe relative motion with gauge and camera

## Slide 6
Introduction
Thermal Cycling
Sliding FW Endmount
Summary & Outlook

## Slide 7: First Measurements with Straight Ribs
Support
Ribs
Thermometer
SLM
Camera

## Slide 8: Results
CTE quantification of CF ribs (time-lapse movie)
  www.youtube.com/watch?v=71rupQkHZV0
  180µm relative motion (negative direction)
    240µm is absolute motion of iron support
    Remainder (60µm) is CF sandwich ribs: 3 ppm/°C (same as silicon)
Real-time video
  www.youtube.com/watch?v=1oRLbkiR7i8
    20 min = very boring because nothing happens
    No abrupt motion is visible (µm scale)
    Perfectly smooth sliding with latest SLM (strong springs)

## Slide 9: Mission Accomplished?
Done!
Done?
We were asked to also perform these measurements with slanted ribs
That is where the real problems started…

## Slide 10: Micrometer Gauge with Slanted Ribs
Vertical displacement
Horizontal displacement

## Slide 11: Results
Made several measurements with changing parameters
Always the same problem: more vertical displacement than horizontal motion
Problem: rib is not stiff enough (at the knee)
Need to stiffen rib

## Slide 12: First Attempts
Improved stiffness, but also increase in material budget
Next: truss (skeleton) structure

## Slide 13: L6 Optimization Study
Rib | Displacement | Volume [cm3] | Dmax [mm]
Original |  | 13.80 | 7.44
V0 |  | 31.54 | 1.15
V2 |  | 16.74 | 1.66
V4 |  | 16.17 | 1.79
Same displacement scale (10:1) and color range for all ribs
V0: filling up all available volume
V2, V4: with cutouts

## Slide 14: Optimized L6 Prototype Measurement

## Slide 15: Results
www.youtube.com/watch?v=qfRq4qdJKP0
Maximum observed displacement: Hmax=260 µm, Lmax=383 µm
For the first time: L > H as it should be 
Use this design and make similar optimization for L5 and L4

## Slide 16: Optimized Ribs
Significant Dmax improvement in all cases
Minimal increase of material budget
L5: very limited space towards L4
  <1mm clearance to PA1/PA2 in some cases
New ribs ordered, expected back in early July
Rib | Displacement | Volume [cm3] | Dmax [mm]
L6 |  | 16.17 | 1.79
L5 |  | 12.37 | 1.89
L4 |  | 8.21 | 0.63

## Slide 17
Introduction
Thermal Cycling
Sliding FW Endmount
Summary & Outlook

## Slide 18: Latest Sliding Forward Endmount
Components
  End mount with swallow tail
  Prism rail (brass)
  2 x coil springs (weak and strong variants)
  2 x 1.5mm stainless steel balls

## Slide 19: Thermal Conduction Test Setup (1/2)
Dummy end ring with big metal block in water bath
Latest SLM with weak or strong springs
Heater wires simulating APV25 power (4W total)

## Slide 20: Thermal Conduction Test Setup (2/2)
SLM must also work in upside-down position loaded with the weight of a ladder
Adding 100 g to simulate this condition

## Slide 21: Result With Weak Spring
Larger T with 100 g load  spring too weak
Chart: Sliding SLM Thermal Mockup Test (weak spring)
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 105 | 110 | 115 | 120 | 125 | 130 | 135 | 140 | 145 | 150 | 155 | 160 | 165 | 170 | 175 | 180 | 185 | 190 | 195 | 200 | 205 | 210 | 215 | 220 | 225 | 230 | 235 | 240 | 245 | 250 | 255 | 260 | 265 | 270 | 275 | 280 | 285 | 290 | 295 | 300 | 305 | 310 | 315 | 320 | 325 | 330 | 335 | 340 | 345 | 350 | 355 | 360 | 365 | 370 | 375 | 380 | 385 | 390 | 395 | 400 | 405 | 410 | 415 | 420 | 425 | 430 | 435 | 440 | 445 | 450 | 455 | 460 | 465 | 470 | 475 | 480 | 485 | 490 | 495 | 500 | 505 | 510 | 515 | 520 | 525 | 530 | 535 | 540 | 545 | 550 | 555 | 560 | 565 | 570 | 575 | 580 | 585 | 590 | 595 | 600 | 606 | 611 | 616 | 621 | 626 | 631 | 636 | 641 | 646 | 651 | 656 | 661 | 666 | 671 | 676 | 681 | 686 | 691 | 696 | 701 | 706 | 711 | 716 | 721 | 726 | 731 | 736 | 741 | 746 | 751 | 756 | 761 | 766 | 771 | 776 | 781 | 786 | 791 | 796 | 801 | 806 | 811 | 816 | 821 | 826 | 831 | 836 | 841 | 846 | 851 | 856 | 861 | 866 | 871 | 876 | 881 | 886 | 891 | 896 | 901 | 906 | 911 | 916 | 921 | 926 | 931 | 936 | 941 | 946 | 951 | 956 | 961 | 966 | 971 | 976 | 981 | 986 | 991 | 996 | 1001 | 1006 | 1011 | 1016 | 1021 | 1026 | 1031 | 1036 | 1041 | 1046 | 1051 | 1056 | 1061 | 1066 | 1071 | 1076 | 1081 | 1086 | 1091 | 1096 | 1101 | 1106 | 1111 | 1116 | 1121 | 1126 | 1131 | 1136 | 1141 | 1146 | 1151 | 1156 | 1161 | 1166 | 1171 | 1176 | 1181 | 1186 | 1191 | 1196 | 1201 | 1206 | 1211 | 1216 | 1221 | 1226 | 1231 | 1236 | 1241 | 1246 | 1251 | 1256 | 1261 | 1266 | 1271 | 1276 | 1281 | 1286 | 1291 | 1296 | 1301 | 1306 | 1311 | 1316 | 1321 | 1326 | 1331 | 1336 | 1341 | 1346 | 1351 | 1356 | 1361 | 1366 | 1371 | 1376 | 1381 | 1386 | 1391 | 1396 | 1401 | 1406 | 1411 | 1416 | 1421 | 1426 | 1431 | 1436 | 1441 | 1446 | 1451 | 1456 | 1461 | 1466 | 1471 | 1476 | 1481 | 1486 | 1491 | 1496 | 1501 | 1506 | 1511 | 1516 | 1521 | 1526 | 1531 | 1536 | 1541 | 1546 | 1551 | 1556 | 1561 | 1566 | 1571 | 1576 | 1581 | 1586 | 1591 | 1596 | 1601 | 1606 | 1611 | 1616 | 1621 | 1626 | 1631 | 1636 | 1641 | 1646 | 1651 | 1656 | 1661 | 1666 | 1671 | 1676 | 1681 | 1686 | 1691 | 1696 | 1701 | 1706 | 1711 | 1716 | 1721 | 1726 | 1731 | 1736 | 1741 | 1746 | 1751 | 1756 | 1761 | 1766 | 1772 | 1777 | 1782 | 1787 | 1792 | 1797 | 1802 | 1807 | 1812 | 1817 | 1822 | 1827 | 1832 | 1837 | 1842 | 1847 | 1852 | 1857 | 1862 | 1867 | 1872 | 1877
#REF! | 1
#REF! | 1
No weight
With 100 g

## Slide 22: Result With Strong Spring
Chart: Sliding SLM Thermal Mockup Test (strong spring)
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 105 | 110 | 115 | 120 | 125 | 130 | 135 | 140 | 145 | 150 | 155 | 160 | 165 | 170 | 175 | 180 | 185 | 190 | 195 | 200 | 205 | 210 | 215 | 220 | 225 | 230 | 235 | 240 | 245 | 250 | 255 | 260 | 265 | 270 | 275 | 280 | 285 | 290 | 295 | 300 | 305 | 310 | 315 | 320 | 325 | 330 | 335 | 340 | 345 | 350 | 355 | 360 | 365 | 370 | 375 | 380 | 385 | 390 | 395 | 400 | 405 | 410 | 415 | 420 | 425 | 430 | 435 | 440 | 445 | 450 | 455 | 460 | 465 | 470 | 475 | 480 | 485 | 490 | 495 | 500 | 505 | 510 | 515 | 520 | 525 | 530 | 535 | 540 | 545 | 550 | 555 | 560 | 565 | 570 | 575 | 580 | 585 | 590 | 595 | 600 | 605 | 610 | 615 | 620 | 625 | 630 | 635 | 640 | 645 | 650 | 655 | 660 | 665 | 670 | 675 | 680 | 685 | 690 | 695 | 700 | 705 | 710 | 715 | 720 | 725 | 730 | 735 | 740 | 745 | 750 | 755 | 760 | 765 | 770 | 775 | 780 | 785 | 790 | 795 | 800 | 805 | 810 | 815 | 820 | 825 | 830 | 835 | 840 | 845 | 850 | 855 | 860 | 865 | 870 | 875 | 880 | 885 | 890 | 895 | 900 | 905 | 910 | 915 | 920 | 925 | 930 | 935 | 940 | 945 | 950 | 955 | 960 | 965 | 970 | 975 | 981 | 986 | 991 | 996 | 1001 | 1006 | 1011 | 1016 | 1021 | 1026 | 1031 | 1036 | 1041 | 1046 | 1051 | 1056 | 1061 | 1066 | 1071 | 1076 | 1081 | 1086 | 1091 | 1096 | 1101 | 1106 | 1111 | 1116 | 1121 | 1126 | 1131 | 1136 | 1141 | 1146 | 1151 | 1156 | 1161 | 1166 | 1171 | 1176 | 1181 | 1186 | 1191 | 1196 | 1201 | 1206 | 1211 | 1216 | 1221 | 1226 | 1231 | 1236 | 1241 | 1246 | 1251 | 1256 | 1261 | 1266 | 1271 | 1276 | 1281 | 1286 | 1291 | 1296 | 1301 | 1306 | 1311 | 1316 | 1321 | 1326 | 1331 | 1336 | 1341 | 1346 | 1351 | 1356 | 1361 | 1366 | 1371 | 1376 | 1381 | 1386 | 1391 | 1396 | 1401 | 1406 | 1411 | 1416 | 1421 | 1426 | 1431 | 1436 | 1441 | 1446 | 1451 | 1456 | 1461 | 1466 | 1471 | 1476 | 1481 | 1486 | 1491 | 1496 | 1501 | 1506 | 1511 | 1516 | 1521 | 1526 | 1531 | 1536 | 1541 | 1546 | 1551 | 1556 | 1561 | 1566 | 1571 | 1576 | 1581 | 1586 | 1591 | 1596 | 1601 | 1606 | 1611 | 1616 | 1621 | 1626 | 1631 | 1636 | 1641 | 1646 | 1651 | 1656 | 1661 | 1666 | 1671 | 1676 | 1681 | 1686 | 1691 | 1696 | 1701 | 1706 | 1711 | 1716 | 1721 | 1726 | 1731 | 1736 | 1741 | 1746 | 1751 | 1756 | 1761 | 1766 | 1771 | 1776 | 1781 | 1786 | 1791 | 1796 | 1801 | 1806 | 1811 | 1816 | 1821 | 1826 | 1831 | 1836 | 1841 | 1846 | 1851 | 1856 | 1861 | 1866 | 1871 | 1876
#REF! | 1
#REF! | 1
T always around 15°C  spring is strong enough
No weight
With 100 g

## Slide 23
Introduction
Thermal Cycling
Sliding FW Endmount
Summary & Outlook

## Slide 24: Summary
Thermal cycling tests of ribs & SLM showed that
  Sliding works well (with strong spring)
  Original ribs too weak (knee)
Optimized ribs with truss structure
  Minimal increase of material budget
  Large improvement of stiffness
Heat transfer measurement with latest SLM design (upside down position without and with 100g weight)
  Strong spring: always sufficient heat transfer (T~15°C)
  Weak spring: worse with 100g weight

## Slide 25: Outlook
Ribs
  Base material (CF/Airex sandwich panels) ordered
    Bad quality delivered  sent back, waiting for reproduction
  Water jet cutting for ribs ordered
  Expected in early July
Forward SLM
  Design and tolerance specifications ready (in SVN)
  Production until end of July