## Slide 1
Electrical Tests
of Modules and Ladders
Markus Friedl (HEPHY Vienna)
2 October 2014

## Slide 2: Introduction
We already know how to test bare
  Hybrids
  Origamis
See http://kds.kek.jp/getFile.py/access?contribId=3&resId=0&materialId=slides&confId=16355
Now we should think about testing modules (=hybrids with sensor with or without bias)
Purposes:
  Verification of (partial) wire bonding during ladder assembly
  Final tests of completed module

## Slide 3: Possible Defects
Affecting full sensor
  No bias connection > no depletion > large noise
  Large common mode noise > could indicate problem with bias
Affecting single strips
  No connection > low noise
  Hot strip > high noise
  Shorted neighbors > half calibration signal (for 2 strips; lower to zero with more to many more)
  Pinhole > low/no calibration signal
Defect may lie with PA and/or sensor
Common mode correction (CMC) can invert low <> high noise
Calibration run (includes noise) needed to find all those defects

## Slide 4: Origami Assembly Flow: n-Side
Excerpt from L5 ladder assembly process flow (Twiki)
Electrical test after each step
n-side bias bonds are made initially
n-side APV25
DSSD
Origami +PA0

## Slide 5: Electrical Tests: n-Side
No bias possible yet
Noise on n-side
  Inner row: higher for even strips (0,2,…)
    Never tried – not clear if really visible
  Full PA0: slightly higher and uniform
  Full DSSD: much higher (no bias)
Screenshots by Sasaki-san
  Upper picture: ½ connections made on both APV and DSSD sides
    Even/odd structure clearly visible
    Con: no way to distinguish PA and DSSD problems
  Lower picture: n-side completed
    Average noise level ~10 ADC

## Slide 6: What to Learn Here?
Deviations from ideal pattern indicate problems
Here: most likely bad wire bond to PA > attempt to repair

## Slide 7: What We Can and Can’t Do On n-Side
Remember: we have no bias yet
  Would require p-side wire bonds which cannot be placed yet
Without bias, we can find
  No connections
  Shorted strips
We cannot (reliably) find
  Pinholes
  Hot strips
Luckily, pinholes on n-side are harmless
  Only p-side is affected

## Slide 8: Origami Assembly Flow: p-Side
Similar to n-side case
Sensor side is already bonded to PA1/PA2
p-side bias bonds are made initially
p-side APV25
DSSD
PA1/PA2

## Slide 9: Electrical Tests: p-Side
Bias bonded first
  Start with simple IV measurement
Noise on p-side (no bias)
  Inner row: higher for even strips (0,2,4,…)
  Middle row: higher for all except 3,7,11,…
  Outer row: higher and uniform (no bias), somewhat lower (with bias)
Screenshots by Sasaki-san
  Upper picture: inner row bonded
    Even/odd structure clearly visible
  Lower picture: inner+middle rows bonded
    High noise for every 4th strip (CMC inverts low <> high noise)
CMC effect

## Slide 10: Semi-Final Measurement
Electrical test (with bias) after finishing all bonding reveals
  If biasing works (noise must decrease for both p- and n-sides)
  Pinholes and hot strips
Wires of p-side pinholes & hot strips should be removed (with pull tester)
Reliable pinhole detection using separation voltage between p-bias and local APV ground
  Calibration curve amplitude changes vs. separation voltage
  DAC add-on circuit to be supplied to all ladder assembly sites
  Allows separation voltage to be set by software (automated measurement procedure)

## Slide 11: Remedy For Too Many Pinholes
Only current flow INTO APV is problem = p-side only
Remedy: offset voltage between HV bias and APV_GND

## Slide 12: DAC Add-On for APVDAQ Test System
DAC circuit which can create -5…+5V offset to HV
  Tested OK, PCBs (25x33mm2) received but not yet assembled
Connection points to repeater board

## Slide 13: Final Measurement
Source or laser scan
Real measurements of sensor signals
Requires
  90Sr source with trigger scintillator+logic
    or
  Pulsed laser with trigger input or output (APVDAQ needs NIM input signal for external trigger)
  Movable stage to change position of ladder relative to source or laser
  Software control for movable stage to scan one sensor of the ladder at a time

## Slide 14: Vienna Solution
Light-proof box with xy control for ladder motion
Source + PM are mounted in the center
So far used in beam tests (without source)
Allows CO2 cooling & dry gas flushing

## Slide 15: Additional Information
Twiki: Origami Wire Bonding Order (step-by-step table) https://belle2.cc.kek.jp/~twiki/bin/view/Detector/SVD/OrigamiWireBondingOrder
Sasaki-san: Origami measurement data http://hep.phys.s.u-tokyo.ac.jp/~sasaki/sasaki_eqa_document.zip http://hep.phys.s.u-tokyo.ac.jp/~sasaki/add_eqa_docu.zip (this is also the source of the wire-bonding sketches)
  Also includes suggestions for good/bad thresholds
  Probably a bit too early to decide about grading