## Slide 1
Switcher bumping at PacTech

## Slide 2: The Motivation
:- SWB bumping so far on chip level in a (semi) manual procedure
:- place gold stud on SWB last metal, jetting of solder on gold stud
:- possible issues and concerns:
:- reproducibility
:- long-term stability of the interconnect (Au-Sn joint)
:- two process steps for each individual bump (on 340 SWBs + spares)
:- Quality control ….
DCDRO – same bumping techno

## Slide 3: Possible solutions
SWB engineering run and bumping on wafer level at IZM
:- standard UBM and e-p SAC solder
2. MPW run for SWB and bumping on chip level
:- more tricky, needs to be qualified …
:- PacTech, Germany, close to Berlin, is offering such a service

## Slide 4: Bumping at PacTech - UBM

## Slide 5: Bumping at PacTech - balling
100 µm

## Slide 6
6 June 2014: 20 hot SWB18 1.0 + 10 setup dummies sent to PacTech
:- received warnings because of scratches and probe marks on the pads
:- confirmed that we take the risk
10 July 2014: received 20 bumped hot chips + 6 from setup
 ~9000 Euro, mostly for setup cost, does not scale with #chips

## Slide 7: Bump height  very homogeneous

## Slide 8: Bump height  very homogeneous
One row of a sample: ~67 µm (-2/+8)

## Slide 9: X-ray  some blisters, <20%, acceptable
PacTech
SAC on Au Stud

## Slide 10: X-ray  some blisters, <20%, acceptable

## Slide 11: Shear tests

## Slide 12: Shear tests

## Slide 13: Shear tests
All ball shear, 54g/bump  pass

## Slide 14: Cross section

## Slide 15: Detail

## Slide 16: summary
:- first bumping test of SWB at PacTech so far successful
Next steps:
:- test ASICs on probe station after bumping (have the ASICs here ..)
:- flip chip tests on recently finished bump adapters
:- smaller ball diameter??
:- go for this? Or bumping on wafer level??