## Slide 1: Laser studies on PXD-5 (Kristof Schmieden)

## Slide 2: Outline
System setup & DUTs
Parameter scans
Clear performance
Internal amplification (241 Am γ-source)
Capacity of the internal gate
Charge collection homogeneity
Summary

## Slide 3: Specs
Laser:
  λ = 680 nm
  Spot diameter Ø = 2.6 µm (FWHM)
  Backside illumination
  Correction of temperature effects by reference detector
DUTs:
  Rec Tesla Small (old layout, but ME, 33 x 23.75 µm²)
  CoCG L B (32 x 24 µm²)
Robert Kohrs – Bonn University 2

## Slide 4: Rec Tesla Small (PXD-5)
Best Signal / Noise : Cl low = 9.7 V
CCG = 10.2 V
(V Source = 7V, Cl hi = 21.8 V)

## Slide 5: CoCG L B
Best Signal / Noise : Cl low = 10.8 V
CCG = 7.2 V
(V Source = 7V, Cl hi = 21.8 V)

## Slide 6: Clear performance
ΔVmin = 9.9 V
ΔVmin = 10.4 V

## Slide 7: Clear timing
Clear duration [ns]
Clear duration [ns]
Minimal regular step size of current system 20 ns
Required for complete clear

## Slide 8: Internal amplification PXD5 CoCG L B
gQ = (361 ± 7) pA/e-

## Slide 9: Capacity of the internal gate
Integration interval [ms]
Accumulated Charge [fC]
Leakage current:
PXD5 CoCG L B

## Slide 10: Homogeneity

## Slide 11: Inaccurate Common Mode Correction

## Slide 12: Summary
Clear performance
  Still ΔUclear = 10.4V needed for optimal S/N
  Clear duration with existing setup (Switcher 2, 64 x 128 pixels matrix) around 20 ns.
Internal amplification
  Up to 20% higher than with Rec Tesla Small design.
  Large differences in gQ observed for matrices with identical design
Capacity of internal gate
  58000 e- should be more than sufficient.
Homogeneity
  No systematic structures (in-pixel, large area) observed.
  Method is susceptible to intensity changes (temperature, detector surface , …)  x-check with testbeam data!

## Slide 13: Temperature correction