## Slide 1: SiMPl for particle detection
Jelena Ninkovic for the MPG HLL team
Outline:
  Material status
  Sensor production plan
  Contacting & Testing

## Slide 2: SOI material status
We found out that the old material could not be used so we had to get new SOI (edge chipping)
Initial difficulties to get raw wafer material of specified resistance - solved end 2013
Thinning down with re-polishing test
  to estimate homogeneity of the top wafer thickness when additional thinning procedure is applied to adjust the Quench resistor value
SOI material production done (30mm thickness)
Final thickness
  Measurement of the implantation diffusion
  Decision on the final resistivity of resistor – today
  Re-polishing can be done in the coming 2-3 weeks
sensor
wafer
handle wafer
1. implant backside
on sensor wafer
2. bond sensor wafer
to handle wafer
3. thin sensor side
to desired thickness
4. process SiMPl arrays
on top side
sensor
wafer
handle wafer
1. implant backside
on sensor wafer
2. bond sensor wafer
to handle wafer
3. thin sensor side
to desired thickness
on top side
Industrial partners
MPI Sem. Lab

## Slide 3: Processing optimization
Test project to optimize the dark rate of SiMPl processing
  Different annealing scenarios tested
  Two best results have been used for further simulations (Wafer 4 and Wafer 11)

## Slide 4: Sensor production status
Start production in ~4 weeks from now
Takes about 3(4) months (August - holidays)  finished by end 2014
  No removal of the handle wafer is planned in this iteration
Layout status:
  Basic cell done (50mm pitch, 16x16 array to match ASICs) - some questions left open
  Variations in gaps with fixed pitch - partially done (depends on the thickness)
  Some additional test structures of conventional SiMPl - done
  Quality test structures – done
  Question for today: do we want to use surrounding substrate for rerouting and interconnection?

## Slide 5: Testing on sensor wafer
Planned testing:
  Processing test structures
  Quality test structures
  Bulk homogeneity
  Diodes
  Arrays without ASICs are just single APDs - do we want to measure all cells before FC?