## Slide 1: SMD placement @ NTC
Quite some struggling with Cu oxide and most likely BCB remainders on some of the samples we got from Laci
  Very bad wetting of the solder balls
  Some investigation needed since, apparently, this did not happen with samples sent to IZM.
NTC got last week 2 new samples with an additional plasma step
  Perfect wetting on these new samples
  Latest news: The two modules have solder balls in every pad. They started yesterday with passive placement.

## Slide 2: Samples

## Slide 3: Samples

## Slide 4: Samples
Bigger pads might need 2 balls. Have to see after passive placement