## Slide 1: Tests of EMCM
Felix Müller on behalf of the MPP / HLL TestCrew
(H.-G. Moser, C. Koffmane, M. Valentan)
Belle II PXD – ASIC Review
October 26 - 27, 2014
Munich
MPP, Germany

## Slide 2: Electrical Multi-Chip Module (EMCM)
Goal
Design and build a fully functional Belle II half-ladder (module) without DEPFET
Reasons
Technological feasibility of the 3-metal (Al1, Al2, Cu) system
Practice flip-chipping (soldering ASICs on pads) and off-module interconnection (Kapton flex cable)
Layout - check if there is enough space for full circuit design, including passive components (decoupling capacitors & termination resistors for LVDS signals)
Power Distribution & Cross-Talk - Testpads to probe the signals and voltages of the ASICs directly
(voltage drops, parasitic capacitances, resistances, check of signal integrity)
Low Noise of all 1000/1024 DCD channels at 320MHz
JTAG programming of all ASICs (including Boundary Scan of all the digital IOs)
Timing and Synchronization (Switcher sequence, DCD data transfer)
Stable operation of all 4 high speed links from DHPT to DHH
Stable Switcher outputs on fully assembled EMCM
PXD6 operation assembled on EMCM
Features
Similar metal system (3 layers) as final modules
Circuitry at periphery (end-of-stave) 4DHPs, 4DCDs, 6 Switchers (additionally 1 DEPFET matrix)
Power Supply, Slow control (JTAG) and High Speed Signals via Kapton flex cable
Sensitive region for test structures (small DEPFET matrix; 32x64 pixels)

## Slide 3
EMCM – Geometrical Overview
Bump bonded steering and r/o ASICs
3 metal layers on periphery
4 layer kapton cable attached
and wire bonded to Si-Module
for I/O and power
Screw through Si
mounting to cooling structure
Space for PXD6
DEPFET Matrix
Load capacitor bank
for switcher test
Long “drain” lines connected to DCD input,
More passives to emulate load of DEPFET cell
Wire bond connections to small matrix
bias connections of matrix via Kapton
Basically it is an electrically active prototype of a half-ladder
Even beam tests are possible with small piggy-back matrix
Test vehicle for metal system and electrical performance of periphery

## Slide 4
EMCM – Electrical Overview
3 metal layers on silicon substrate
2149 different electrical nets
4055 test pads (size down to 70μm x 70μm and 50μm x 100μm)
~15k vias connecting the metal system in 3D (10k aul1 to Al2, 5k Al2 to Cu)
Open and short test necessary before assembly of the ASICs
Short test contains ~110k measurements per EMCM
DCD
DHP
Switcher
Kapton
Flex

## Slide 5: Matrix assembly
Switcher
DCD
DHP
DEPFET
Passives (R,C)
Kapton
Optionally, a matrix can be glued on the EMCM
The DEPFET matrix is electrically connected via wire-bonds
Operate device and compare measurements to PCB-assembled test setups
(performance, noise, Signal-to-noise, stability …)
Drain lines are comparable with final modules ~45mm
PCB
latest generation of ASICs:
- SwitcherB18v2.0
- DCDpp
- DHPT1.0

## Slide 6: Tests – Switcher @ W17-3, 305MHz
DCD
DHP
Switcher
Switcher
Switcher
Clear and Gate
Kapton

## Slide 7: Tests – Switcher @ W17-3, 305MHz
DHH
DHP
Switcher
write switcher sequence
into the DHP memory
Switcher
Switcher
Switcher
Switcher
Switcher
control sequence
EMCM
Bondwires
Bondwires
Bondwires
Bondwires
Bondwires
Bondwires
Switcher 2
Switcher 3
Switcher 0
Switcher 1
5
4
3
2
1
0

## Slide 8: Tests – Switcher @ W17-3
Switchers worked in the beginning
Stop working after movements of the EMCM
TDO of Sw4 does not show any signal
TDI of Sw4 looks fine
(measured at pads, triggered on CLK)

## Slide 9: Tests – Switcher 5 @ W17-3, 250MHz
Switcher 5
CLK
Gate
Clear
Clear
Gate
CLK

## Slide 10: Switcher Summary
All 6 Switchers work properly in normal operation at 305MHz
Switchers can be configured via JTAG (set termination resistors for LVDS)
should not be in a random state when switching them on
Configure termination resistors for each LVDS individually (CLK, StrG, StrC, SerIn)
  (parallel: CLK, StrG, StrC; in series: SerIn)
Module W18-3: All switchers are working fine (need micromanipulator), Matrix attached
Gated-Mode Operation
Operation Mode can be changed in GUI => tested & works (no information about timing, how fast does the mode switch from normal mode to GatedMode operation)

## Slide 11: DHPT 1.0 – Aurora Links – Signal integrity
Known problems:
- Design / Layout error with
- Problems during manufacturing of Kapton (impedance not controlled)
Solutions:
More capacitors at PowerPatchPanel (PCB, connected to Kapton)
Replace Kapton by PCB
DHH firmware allows „half data rate“ (800Mbit/s instead of 1.6Gbit/s) of DHPT to be transmitted

## Slide 12: Aurora Settings – DHPT1.0
A - IDAC CML TX BIAS
B - IDAC CML TX BIASD
C - pll cml dly sel
Source: DHPT 1.0 Manual, Version 0.1, October 13, 2014, University of Bonn

## Slide 13: Aurora Scans – DHPT1.0
Procedure:
Long RST => get link
Check link status (blue dot)
Trigger (transmit data)
Check link status (red dot)

## Slide 14: Aurora Links – Signals Integrity
DHPT
Hybrid 5 - PCB
Wirebond Adapter
DHH / DHHemulator
Infiniband connectors
15m Infiniband cable
EMCM
Kapton
Data Patch Panel
DHH
EMCM Setup

## Slide 15: Aurora Links – Signals Integrity (1)
Module: | DHPT Testboard
Frequency: | 305MHz
Cable length: | 3m
Core Voltage: | 1.2V
Bias | 15
BiasD | 75
Module: | EMCM – DHPT0
Frequency: | 305MHz
Cable length: | 3m
Core Voltage: | 1.6V
Bias | 48
BiasD | 127

## Slide 16: Aurora Links – Signals Integrity (2)
Module: | DHPT Testboard
Frequency: | 305MHz
Cable length: | 15m
Core Voltage: | 1.62V
Bias | 15
BiasD | 150
Module: | EMCM – DHPT0
Frequency: | 305MHz
Cable length: | 15m
Core Voltage: | 1.64V
Bias | 7
BiasD | 150

## Slide 17: Aurora Links – Signals Integrity (3)
Module: | EMCM – DHPT0
Frequency: | 305MHz
Cable length: | 15m
Core Voltage: | 1.6V
Bias | 15
BiasD | 180
Module: | EMCM – DHPT0
Frequency: | 250MHz
Cable length: | 15m
Core Voltage: | 1.6V
Bias | 15
BiasD | 150

## Slide 18: DCD Pipeline (DCDpp) – Noise Measurements
IFBPBias=90
IPSource=90
RefIn = 0.9V
AmpLow = 1.2V
305MHz

## Slide 19: DCD Pipeline (DCDpp) – Noise Measurements
IFBPBias=90
IPSource=90
RefIn = 0.9V
AmpLow = 1.2V
Restart of System, i.e. power cycle
other noisy
channels
305MHz

## Slide 20: DCD Pipeline (DCDpp) – Noise Measurements
IFBPBias=80
IPSource=80
RefIn = 0.9V
AmpLow = 1.2V
305MHz

## Slide 21: DCD Pipeline (DCDpp) – Internal Current Source
DCD
internal current source
Source Measurement Unit (SMU)
EMCM
Kapton
Power Patch Panel
Breakout Board
(Connectors board)
Source Measurement Unit (SMU)
schematic
reality

## Slide 22: DCD Pipeline (DCDpp) – Internal Current Source

## Slide 23: DCD Pipeline (DCDpp) – Internal Current Source
Sig_Mirror

## Slide 24: DCD Pipeline (DCDpp) – Internal Current Source
W17-3
DCDpp0

## Slide 25: DCD Pipeline (DCDpp) – Internal Current Source
W17-3
DCDpp0

## Slide 26: DCD Pipeline (DCDpp) – 2bit Offset DACs
pixel
ADU
Pedestals
2
3
4
5
6
7
8
1
DAC=3
DAC=3
DAC=1
DAC=3
DAC=1
ADC=2
DAC=0
DAC=0

## Slide 27: DCD Pipeline (DCDpp) – 2bit Offset DACs
DHH
DHP
write offset memory
into the DHP memory
DCD
global parameter
individual
parameter
IPDAC
write which pixel has which offset {0,1,2,3}

## Slide 28: DCD Pipeline (DCDpp) – 2bit Offset DACs
Write Test Pattern into DCDpp
Still some problems with timing issues

## Slide 29: DCD Pipeline (DCDpp) – 2bit Offset DACs
Offset=0
Offset=1
Offset=2
Offset=3
IPDAC Current source can compensate 4x the dynamic range

## Slide 30: DHPT1.0 – Pedestal Upload
DHH
DHP
write pedestal values
into the DHP memory
Write Pedestals into Memory of DHPT for all pixels
ReadOut Pedestals, consisting of:
- Current values which are transferred from DCDpp to DHPT
- Memory of DHPT

## Slide 31: DHPT1.0 – Pedestal Upload
current
pedestals
pedestals
in memory

## Slide 32: Summary & Outlook
    Switcher (SwitcherB18v2.0):
    Switchers: work properly in normal operation at 305MHz
    Readout of settings is possible (JTAG)
    DCD (DCD-Pipeline):
    Internal current source is noisy
    IPDAC (offset DACs) is too strong (after irradiation?)
    Noisy ADC channels (need more statistics)
    Works at 305MHz
    Readout of settings is NOT possible (JTAG)
    DHP (DHPT1.0):
    problem with high-speed links
    upload of pedestals, switcher sequence, offset-dacs
    Readout of settings is possible (JTAG)

## Slide 33: Outlook
    Boundary Scan, System scanning using dedicated hardware and software is not done yet (Philipp Leitl, Master Student @ MPP, started to work on that)
    PXD6 operation on EMCM at full speed with DCDpp, DHPT1.0, SwitcherB18v2.0 (Pedestal distribution (spread), noise, laser scan, source tests, GatedMode)
    Studying DCDpp performance (ADC transfer curves, Pedestal Spreads, Noise Distribution, all ASICs, Common Mode Suppression)
    Increase readout speed
    Decrease in performance when operating multiple ASICs simultaneously (cross-talks, voltage drops …)?
Mapping in principle okay, need fine tuning of delay settings
Offset DACs okay, need fine tuning of delay settings
Replacement of Kapton (impedance controlled traces, less connectors, better connection, large loop for DCD Monitor pin)

## Slide 34
Thank
you

## Slide 35: DCD Configuration Problem
Source: Dmytro Levit, TUM
https://indico.mpp.mpg.de/getFile.py/access?contribId=59&sessionId=1&resId=0&materialId=slides&confId=2933
last DCDB requires one bit less during configuration
same situation on the module with only one DHP-DCD pair
work around implemented in software to mitigate the problem

## Slide 36: Setup
Micro
Manipulator
Pico Probe
Data cables
Power cable
LMU Power Cable
Water
cooling
Power Patch
Panel
PCB, Switcher
Output Control
EMCM
Data Patch Panel

## Slide 37: Fully Assembled EMCM
DHP
DHP
DHP
DHP
DCD
DCD
DCD
DCD
SWB
SWB
SWB
SWB
SWB
SWB
DHH
4 x High Speed Link
JTAG and Control Signals
Switcher Control Signals: Clk, StrG, StrC
SerIn
SerOut
New configuration:
JTAG chain with 14 ASICs
6 Switchers in serial
Multiple ASICs connected to the same power supply

## Slide 38: Overview of EMCMs
Three samples fully populated with latest ASICs (DCDPipeline, DHPT, SwitcherB18v2)