## Slide 1
PXD Module Assembly
- Overview and SWB bumping -

## Slide 2: Sensor production phases and where we are
metal_2
oxide
metal_1
polySi_1
polySi_2
n bulk
deep p
deep n
p+
n+
Phase I – before metal
  Implantations
  Polysilicon
  Dielectric depositions
Phase II - Alu
  Metal 1
  isolation
  Metal 2
  & ILD deposition, BCB
metal_2
oxide
metal_1
polySi_1
polySi_2
n bulk
deep p
deep n
p+
n+
Phase III – thinning and Cu
  Handle wafer removal
  Metal 3 (Copper)
  Passivation/solder stop

All batches finished

Phase II:EMCM production(s) for Alu/Cu
:- technology confirmed with EMCM4

thinning and Cu tested on PXD6
:- final verification with PXD9 metal dummies

## Slide 3: PXD9 thinned metal dummies
8 SOI Wafers, 2 with Copper
  450/0.32/75 µm
  Alu-2 + co3n on top
  Final PXD9 back side
  Practice Cu after thinning  done, no problem
  and all subsequent process steps

## Slide 4: Cutting edge – V-grooves
Practice Ladder Assembly procedure
  5 wafers with alu on top, laser-cut
  Material for 5 inner ladders, and 10 outer
  Additional std. silicon samples for gluing tests

## Slide 5: Module Assembly – procedure and status
Flip Chip of ASICs (~240°C):
  Bumped ASICs have the same solder balls (SAC305)
    DHP bumping at TSMC
    DCD bumping ???, availability?
    SWB bumping on chip level at PacTech
    At IZM Berlin for EMCMs and also for final procedure
  Meeting at IZM Dec. 2014: ready to go for pilot run in summer
SMD placement (~200°C):
  Passive components (termination resistors, decoupling caps)
  Dispense solder paste/jetting of solder balls, pick, place and reflow
    PbSn 37/63 solder balls
  For EMCMs at Finetech, Berlin
    Solder jetting, SMD placement at IFIC/NTC Valencia
Kapton attachment (~160°C), wire bonding:
  Solder paste printing on kapton,
    SnBi solder
  Wire-bond, wedge-wedge, 25 µm Al bond wires between kapton and substrate
  EMCM and final at MPP Munich, no issues expected
01005 term. res
Ladder assembly: later in this session

## Slide 6: Reminder: PacTech bumping (‘balling’) on chip level
ENIG  UBM
5µm Ni + flash Au
2. SB²  balls
Sn-Ag-Cu “SAC305”

## Slide 7: The result: 96 solder balls per chip, 100µm diameter

## Slide 8: Summary of test results
  20 (+10 for setup) SWB1.8 V1.0 bumped last summer
  “mechanically” and optically (reported during past meetings)
    height homogeneity okay
    Shear tests passed: ball shear, ~50g/bump
    X-ray: Voids/blisters < 15%, passed
  Electrically tested at Mannheim (Probecard)
    19/20 okay after bumping (Christian Kreidel)
  Filp-chip to home made bump bond adapters at HLL
    Basically same procedure as at IZM for EMCMs

## Slide 9: Before Flipping
Reflow of bare chips at ~250 °C
 dip is “ironed” out
 but the balls are changing “somehow” ..
Test flip-chip with and without this dummy reflow

## Slide 10: X-ray of FC Assemblies
No dummy reflow
with dummy reflow
 The dip does not harm, don’t need to do it!

## Slide 11: Taking it apart: shear tests – with dummy reflow
substrate
ASIC
:- imperfect wetting
:- shear at UMB at substrate side
:- low force: ~10 g/bump

## Slide 12: Taking it apart: shear tests – without dummy reflow
substrate
ASIC
:- perfect wetting
:- shear at UMB on substrate side
:- still somewhat low force but acceptable: ~25 g/bump

## Slide 13: Cross section of flip chip assembly

## Slide 14: In Summary
:- preparations for last production phase finished, awaiting the PXD9-pilot to come
:- thinned module samples (two wafers Copper) available
:- practice FC, SMD, Kapton attach, ladder assembly …
:- PacTech bumping of SWBs successful
:- adjust ball size (100  80 µm)
:- reduce Alu pad/passivation opening at ASICs to be the same as on module
:- don’t expect 100% yield …