## Slide 1: Pilot run – matrix measurements after first metal
7th Belle II VXD workshop
and 18th International Workshop on DEPFET Detectors and Applications
Rainer H. Richter and Paola Avella
for the MPP/HLL team

## Slide 2: Outline
IV measurements on matrices after metal 1 (limited results)
- Top side measurements
metal1 lines within the matrix are not yet connected
(needs metal 2)
Neverthess we can already check for some defects
(diode integrity, some metal shorts)
- Backside measurements
Matrix biasing via Punch through structure
makes life much easier but should work)

## Slide 3: Top side measurements
Simple method: Connecting one p + contact and the n Bulk
provides information about the integrity of all diodes within the entire matrix
(experience with other project)
p+ guard vs Bulk
Contacts are foreseen in metal 1

## Slide 4: How does it works?
Vguard (V-)
Matrix (not connected)
Vbulk (0V)
Backside (not directly accessible)
75µm
5cm
Vguard (V-)
Matrix is not depleted from the backside !
Vdrift= Vguard-Vpt
Vdrain
Early punch through
at small Vbulk
Measurement of a lot of small diodes in parallel
Drift, drains and sources are connected via punch through with small voltage differences

## Slide 5
Vguard (V-)
N+/P+ shorts
Vbulk (0V)
Backside (not directly accessible)
75µm
5cm
Vguard (V-)
Vdrift= Vguard-Vpt
Vdrain
Early punch through
at small Vbulk
Also sensitive to crystal defects generating high leakage currents !
We are sensitive to …all what happens in parallel to the diodes

## Slide 6: Like this: p+ drift in contact with n+ clear
Lethal defect – lost chip

## Slide 7: We are sensitive to …
Vguard (V-)
metal 1 shorts between p+ and n+
Vbulk (0V)
Backside (not directly accessible)
75µm
5cm
Vguard (V-)
Vdrift= Vguard-Vpt
Vdrain
Early punch through
at small Vbulk
We dont‘ see problems between P+ regions (Drift, Drain, Source)
since this does not affect the diode characteristics

## Slide 8: After metal 1
N+ clear line
P+ source line

## Slide 9: Bulk vs Guard Characteristics
All the long matrices of all the three project wafers show small values of current (≈ nA)
Indication that the half ladders are in a healthy status
So far 100% yield
(for the testable items)

## Slide 10: Backside IV measurements (Punch through biassing)
Vpunch through (V-)
Matrix (not connected)
Vbulk (0V)
Backside (not directly accessible)
75µm
5cm

## Slide 11: Punch Through Characteristic What do we expect ?

## Slide 12: Punch Through Characteristic [I]
Depletion region expanding
from punchthrough contact into the bulk
(small volume -> small leakage current)
Vpunch through
Vbulk
Phase 1
Depletion expands

## Slide 13: Punch Through Characteristic [II]
2. Depletion region reaches backside
Vpunch through
Vbulk
Phase 2
Backside reached
Interface current
bulk current

## Slide 14: Punch Through Characteristic [III]
3. Depletion region expands from the entire backside implant into the bulk
Interface current
bulk current
Vpunch through
Vbulk
Phase 3: entire bulk gets depleted

## Slide 15: Punch Through Characteristic [IV]
4. generation states are getting activated
generation current
Vpunch through
Vbulk
Phase 4:
Active generation centers
Interface current
bulk current
Interface and surface currents

## Slide 16: Punch Through Characteristic [V]
5. All generation states are activated
generation current saturates
Vpunch through
Vbulk
Phase 5:
Generation current saturates
Interface current
bulk current
Interface and surface currents
Nice IV curve: low leakage level
Operation volt. (PT) : -55V …-65V

## Slide 17: Punch Through Characteristics all modules of wafer 35
uniform characteristics 
The other wafers?
Faster measurement:
-> fluctuations
Not meaningful

## Slide 18: The other wafers …
Currents on W30 and W36 are higher
Uniform ‘wafer wise‘ behavior:
All modules of wafer 35 are fine
All modules of wafer 30 and 36 are worse
Not really crucial: currents are still in a moderate range
But we want to know the reason …

## Slide 19: Zoom in
Current onset starts with Phase 2: depletion regions

## Slide 20: Punch Through Characteristics – Small matrices

## Slide 21: Layouts of PT same design but different sizes

## Slide 22: Global effect concerning all modules to the entire wafer ?
What is ‘global‘ to all modules on a wafer ??
the handle wafer
We directly connected
the handle wafer

## Slide 23: Cutting Edge (Bulk) vs Handle Wafer
The current flowing between the cutting edge contact and the handle wafer for W35 is much higher than the current measured for W30 and W36.

## Slide 24: Punch Through Characteristics [IV]
VS Cutting Edge
VS Handle Wafer

## Slide 25: Handle wafer vs Bulk (zoom in)

## Slide 26: Additional measurements
Not nice and rather noisy due to limited setup flexibilty in the cleanroom
- Changing handle wafer potential
- pos. w.r.t. bulk : no influence (up to 30V) -> no avalache
- neg. w.r.t. bulk: current increase
Long term meas.
high current is dropping with time

## Slide 27: The nature of the increased current?
Handle wafer acts as backside gate
Not an avalanche current (no reaction on pos. Voltages on handle wafer) 
Influence of holes at the backside of the top wafer
  Inversion layer is connecting backside diode and cutting edge
  Unlikely: Handle wafer cannot become more negative than the backside p+ diode
Depletion of the SIO2/Si interface (Buried oxide)
  The interface of the whole wafer is getting generation active

## Slide 28: No significant generation current (SRH) ? in normal operation
+ + + + + + + + + + + +
Vpunch through (V-)
Vbulk (0V)
good connection
- - - - - - - - - - - - - -
Normal operation: handle wafer at 0V
Wafer outside the module in thermal equilibrium
Interface states are occupied by electrons
- > very small leakage current
Electron accumulation layer
150mm

## Slide 29: Large generation current (SRH) ? If handle wafer floats …
+ + + + + + + + + + + +
Vpunch through (V-)
Vbulk (0V)
bad connection
. . . . . . . .. . . . . . . . . . . ... .
handle wafer floats to neg. potential by cap. coupling
A few 100mV are enough
Accumulation layer gets depleted
Interface states are getting genaration active
> large leakage current
Very good recombination lifetime in the bulk
large diffusion lenghts for holes
-> the whole wafer contributes
Electron accumulation layer disappears
150mm
V-
Vpunch through
Vbulk
Phase 3: entire bulk gets depleted
Backside pot. follows directly Vpt
Small arrays are better due to their
smaller backplane (Cap.)

## Slide 30: Summary and Conclusions
Top side:
Test for diode integrities on all modules were successful
no shorts between Source and Clear lines found
Backside:
Badly connected handle wafer may cause parasitic gate effects
leading to an increase of current
We think that problem disappears if the wafers are diced (laser cut)
laser melting will provide a reliable contact between handle wafer and bulk
All modules of W35 (better connected) show nice IV with low leakage currents
More and better measurements (setup) will follow …