## Slide 1
Belle II PXD Overview
(An attempt to describe the)
Interfaces between ASICs and the Experiment and DEPFET sensor

## Slide 2: What is KEKB and SuperKEKB?
KEKB:
:- small, but powerful e+/e- collider (~3km circ.)
:- holds the world record in peak luminosity
:- status: shut down - under upgrade
:-  SuperKEKB with 40x higher Lumi.
SuperKEKB

## Slide 3: KEKB to SuperKEKB
Belle-II
Smaller beam size & more current:
 40x higher luminosity, goal: 8x1035 cm-2s-1
 probe New Physics at “intensity frontier”
 20x-40x higher background
  Radiation damage and occupancy
  Fake hits and pile-up noise
 10x higher event rate
 Detector upgrade
  Replace inner layers of the vertex detector with a pixel detector, upgrade outer layers
  Replace inner part of the central tracker with a silicon strip detector
  …

## Slide 4: From Belle to Belle II
Beam pipe: R=10mm
SVD
Silicon Vertex Detector
4 layer double sided Si strip detector
R=3.8, 8.0, 11.5 and 14 cm
PXD
Pixel Detector
2 layer Si Pixel at R=1.4 and 2.2 cm
DEPFET active pixel sensor technology

## Slide 5: Towards a pixel vertex detector for Belle II
Find best technically feasible compromise:
  :- for central und forward region
  :- signal/noise of the sensors
  :- # of r/o channels
  :- occupancy
  :- single point and impact parameter res.
Physics driven requirements

## Slide 6: DEPFET Active Pixels
Drain
Source
Gate
fully depleted sensitive volume, mip: ~ 80 e-h pairs/µm
internal amplification
Charge collection in "off" state, read out on demand

## Slide 7: DEPFET Active Pixels
fully depleted sensitive volume, mip: ~ 80 e-h pairs/µm
internal amplification
Charge collection in "off" state, read out on demand

## Slide 8: Internal Amplification – the signal
Photon events
~1700 signal electrons
Clear
Clear
step
time
I_Drain
(Ideal transistor theory - neglecting short channel effects)
gq (pA/e-)
Drain current ID (µA)
(L: nominal gate length)
Belle II: ~400pA/e expected
Full mip signal in 75 µm sensor: ~ 2µA

## Slide 9: Belle II DEPFET pixel cell
Drain
Source
  Basic cell is a DEPFET double pixel
    Common source for two gates/drains
    Clear implant between double pixels
    Gate L=5µm, W/L=2
    Scaling of pixel size with drift regions

## Slide 10: Matrix arrangement and read-out sequence

## Slide 11: The Result – Belle II PXD
 | L1 | L2
# modules | 8 | 12
Distance from IP (cm) | 1.4 | 2.2
Thickness (μm) | 75 | 75
#pixels/module | 768x250 | 768x250
#of address and r/o lines | 192x1000 | 192x1000
Total no. of pixels | 3.072x106 | 4.608x106
Pixel size (μm2) | 55x50 60x50 | 70x50 85x50
Frame/row rate | 50kHz/10MHz | 50kHz/10MHz
Sensitive Area (mm2) | 44.8x12.5 | 61.44x12.5
vertex resolution significantly improved
Z. Drasal
Angular coverage 17°<θ < 155°

## Slide 12: DEPFET all-silicon module
DHP (Data Handling Processor)
  First data compression
  IBM CMOS 90 nm (TSMC 65 nm)
  Size 4.0  3.2 mm2
  Stores raw data and pedestals
  CM and pedestal correction
  Data reduction (zero suppression)
  Timing and trigger control
  Drives data link
SwitcherB - Row Control
  AMS/IBM HVCMOS 180 nm
  Size 3.6  1.5 mm2
  Gate and Clear signal
  32x2 channels
  Fast HV ramp for Clear
DCDB (Drain Current Digitizer)
  Analog front-end
Amplification and digitization of DEPFET signals.
256 input channels
8-bit ADC per channel
92 ns sampling time
new version w/ 50ns sampling time under test
UMC 180 nm
Key to low mass vertex detectors
highest integration!
  Thin sensor area
  EOS for r/o ASICs
  Thin (perforated) frame w/ steering ASICs

## Slide 13: DEPFET Prototype Fabrication and “Thinning” – PXD6
50 µm
400 µm
Top side of prototype run
(“PXD6”)

## Slide 14: All-Silicon Module
Belle II mechanical sample
50µm Si, unsupported
50µm Si in Silicon frame
Half-ladders (modules) are laser-cut
Modules are supported by a monolithic silicon frame
Two inner (outer) modules are assembled to inner (outer) ladders

## Slide 15: Micro joint between half-ladders
butt-joint between two half-ladders
reinforced with 3 ceramic inserts
2x300µm dead area per ladder

## Slide 16: Sensor and r/o electronics: Beam tests with the full system
PXD6 Belle II design
Thin (50 µm) sensor 32x64 pixels
Pitch 50x75 µm2
SwitcherB and DCDB at full speed
Belle II prototype power supply
DCDB readout at 320 MHz  100 ns row time
99% Efficiency
S/N for MIPs: 20-40 depending on gate length
gq≈450 pA/e-
Cluster 3x3 signal
MIP Perpendicular incidence
~10 µm resolution
DCD
DHP
50µmthin DEPFETs
SWB

## Slide 17: Towards a real ladder
Transition from test systems to integrated modules
PCB for the various matrices ….. “hybrids”
first bump bonded chip on PXD6 prototype matrices
  2 metal layers, not the final geometry, simple 3rd metal
  need still support PCB for I/O
  not perforated balcony
Belle-II PXD Module (two modules form a ladder)
  three metal layers, Cu as LM only on periphery
  MCM: 4 DCD, 4 DHP, 6 Switchers  ~3000 bonds/module
  Cu as UBM, bumps partly on thinned perforated frame
  passive components soldered to substrate
  I/O and power over Kapton cable
01005 term. res

## Slide 18: Test vehicle E-MCM
Extensive test program
Interconnect technology
Powering, control, DAQ
Signal integrity, timing …
…
Lessons learned are being applied to
final module layout
100ns/div
5ns/div

## Slide 19: Capacitive load for the ASICs

## Slide 20: The System

## Slide 21: Background - occupancy
Extensive study by MPP group: main contribution QED background (4 fermion final state), e+/e- ~ few MeV range
Andreas Moll, Seeon 2012
Add ~0.14% synchrotron radiation
(Moll/Ritter/Soloviev)

## Slide 22: Background – rad. damage - TiD
Total ionizing dose:
L1 ~2 Mrad/smy
L2 ~0.6 Mrad/smy
Fairly uniform over Z
Effect on DEPFET:
Vth after 10Mrad ~5V
  uniformity of response to radiation?
ASICs to allow for additional pedestal variation
PXD Layer 1

## Slide 23: Background – rad. damage - NIEL
Direct neutrons from all background processes: ~1e11 neq/cm²/smy
NIEL from leptons from QED background: ~1e13 neq/cm²/smy
Effect on DEPFET: Ileak increase, not expected to be critical with moderate cooling

## Slide 24: Injection noise
20 µs frame
10 µs rev. packet
~ 4ms noisy /~ 400 packets
10µs packets with 2503 bunches , 200 ns gap in-between
continuous injection  ~ 400 revolutions with two noisy bunches (100ns apart) every 20 ms
DEPFET integrates two trains, these noisy bunches would blank the frames  20% loss of data
the best solution: gate the DEPFET during the passage of the noisy bunches
100ns gate, with some rise and fall times, twice per frame … is this possible?
the answers is: as far as the DEPFET is concerned, yes!
see Christian Koffmane’s talk
~ 16 ms “clean”

## Slide 25: summary
Top level specs for the supporting ASICs of a DEPFET based Belle II PXD
Expected occupancy: ~1.5%
Rad. Tolerance for 5 years: 10Mrad TiD, 5e13 neq/cm²
Read-out speed: row rate 10MHz
Capacitive load: DCD input 50pF, SWB Gate and Clear 125pF(tbc)
DEPFET bias: Gate_off 3..5 V
Gate_on -3..-10V
Clear_off 2..3V
Clear_on 15..20V
Max. input signal: ~3 mips ~6µA
Signal/noise: >20 (mip MPV)
Pedestal: 100µA
Pedestal variation within matrix: technol. 10%
after irrad. tbd
General: analogue ped. correction for each pixel
support of the “gated mode”