## Slide 1: ASICs: DCD and Switcher

## Slide 2: DCD

## Slide 3: DCD
Changes in design (present status):
Change sampling of TDI for global and pixel register to positive edge (mandatory)
Add fast parallel sampling mode for easier needle card tests (nice to have)
Improve test DAC resolution by adding additional DAC (nice to have)
Stronger digital output driver current (or improved scheme), radiation hard NMOS (mandatory)
Protection diodes for digital signals should be on VDDD for digital (mandatory)
Add transmission switch to monitor (now only PMOS) (nice to have)
Check the voltage drop on power rail – connect gate of the NMOS sources only in one point (nice to have)
Reduce RefIn current (mandatory)
Try to connect DAC Dump and SF VDDA to RefIn (nice to have)
Separated bias DACs for up and down bias/notice larger drop 0-7 then 8-15, try different grouping (mandatory)
Spare ADCs (nice to have)
Redo protection diode, current drain/split nwell (mandatory)
Ipdac 60uA full range (mandatory)
SubIn 4 times or additional DAC (still not clear)
Introduce 15k Feedback resistor setting – low gain mode (mandatory)
More complex digital test patterns (mandatory)
Improve matching and Rout – wider LV PMOS, same orientation, same NMOS, enlarge Diff PMOS (mandatory)

## Slide 4: JTAG and slow controll - Change sampling of TDI
4
Global Register
G_Shift, G_Rb, G_Ld
Address
Pixel Register
P_Shift, P_Rb, P_Ld
Data Register
ShiftDR, CaptureDR, UpdateDR
Instruction Register
ShiftIR, CaptureIR, UpdateIR
ID Register
ShiftDR&IDSel
In
i
CaptureIn
LatchOut
PreLoad
Out
ExtTest
CaptureIn
LatchOut
o
Digital Block
ShiftDR, CaptureDR, UpdateDR
GlobalSel
TDI
FF
FF
FF
FF
ShiftDR, CaptureDR, UpdateDR
PixelSel
PixelSel
GlobalSel
ExtTest OR PreLoad
ShiftIR
The other if not ShiftIR
IDSel
Bypass
TDO
Pads
Commands
State M.
Cont. Signals
TMS
DO0(7:0),DI0(1:0),…,DI3(1:0),SYNC_RES,CLK,RetCLK,TestInjEn,DO4(7:0),…,DI7(1:0)
Readout Reg
CaptureIn
Full custom latches
Ld
TCK
o
Readout
CaptureIn
i
TestMode
Bitck
Res
Res!
TestMode
TestPads

## Slide 5: Digital output driver
The ADC signals are compressed and serialized on DCD. The output drivers of DCD sent the data via non-standard single ended current mode links. The structure of these links is shown in figure. Currently the amplitude of the signal is limited to 220 mV and cannot be changed.
DCD digital block
VDD
Bias block
DCD

## Slide 6: Digital output driver
Stronger digital output driver current (or improved scheme), radiation hard NMOS
In
In
InB
InB
3pF

## Slide 7: Digital output driver
Stronger digital output driver current (or improved scheme), radiation hard NMOS
In
In
InB
InB
1.4m
6pF

## Slide 8: Digital output driver
Stronger digital output driver current (or improved scheme), radiation hard NMOS
In
In
InB
InB
3pF
vdda
vddd
gndd

## Slide 9: Digital output driver
Stronger digital output driver current (or improved scheme), radiation hard NMOS
In
InB
In
In
InB
InB
1.4m
1.4m
6pF
6pF

## Slide 10: Digital output driver
Stronger digital output driver current (or improved scheme), radiation hard NMOS
In
InB
In
In
InB
InB
1.4m
350u
350u
6pF
6pF

## Slide 11: RefIn current
…
RefIn
Source
Source
240uA max
~300uA
~60uA
GNDA
VDDA
SF
AmpOut
VDDA
AmpIn
AmpInCM
RefIn
VDDA
Gate
This makes NMOS scs independent on GNDA noise
This makes current GNDA constant always
RefIn Current isn‘t constant
RefIn
RefIn

## Slide 12: Separated bias DACs
…
DAC
Mirror
d
d
Some measueremnts do not show the effect!

## Slide 13: Separated bias DACs
…
DAC
DAC
Or here

## Slide 14: Connect gate of the NMOS sources only in one point
…

## Slide 15: Connect gate of the NMOS sources only in one point
….

## Slide 16: Long Codes - Simulations

## Slide 17: Monte-Carlo Simulation
We have done Monte Carlo simulations – according to first simulations mismatch (6 sigma) is up to ~2.5uA – which is still smaller than 4uA which produces missing codes
(Simulation without thresholds source)
2.5u

## Slide 18: ADC unit-cell
The ADC-unit has two current-memory cells based on two U-I converters A and B
Depending on the input current amplitude (too low or too high), a reference current (4 μA per cell) will be added or subtracted
The comparison is done in the following way:
Two copies of the current stored in A are made – this is done with the two, layout-identical, UI converters CL and CH that are connected to the same voltage as A
The goal of this preprocessing is “to compress” the input signal so that it occupies 2x smaller range.
14u
A
CH
12u+/-4u
TooLow
TooHi
10u
12u+/-4u
CL
B

## Slide 19: Unit-cell characteristics
The purpose of the comparators is to assure that the reference currents are subtracted/added in the way so that the result current occupies two times smaller range
Only so, the error in algorithm is small
IIn
IOut
-2u
-4u
-8u
8u

## Slide 20: Unit-cell characteristics with offset
Imagine now that the ThHi threshold is shifted by Ref/4 (2uA) +Delta.
Imagine also that the signal is about Ref/2 (=64) In this case the result of the first comparison is zero. The result of all other comparisons is TooHigh. This leads to the binary code 64.
Imagine now that signals are within range Ref/2 and Ref/2+Delta. Obviously the binary code are always 64. This leads to the long code 64.
IIn
IOut
-2u
-4u
-8u
8u

## Slide 21: Bad characteristics causes missing codes
Missing codes around 64
IIn
IOut
-2u
-4u
-8u
8u

## Slide 22: Origin of offset
Why does the current offset happen?
Possibility: transistor mismatch – fix in the next chip: make the layout in a better way e.g. the transistors bigger
Additionally, there may be a systematic offset in comparator that adds to the mismatch
Notice also: two output nodes are not on perfectly same potential
Original UI converter connected to amplifier input, copy UI converter to RefIn – this explains RefIn dependence
PFB
RefFB
Sc2
RefIn
Sc2
Sc2
RefIn
Sc2
RefFB
PFB
TooLow
24u
24u
24u
24u
26u
24u
Low

## Slide 23: Monte-Carlo Simulation
We have done Monte Carlo simulations – according to first simulations mismatch (6 sigma) is up to ~2.5uA – which is still smaller than 4uA which produces missing codes
(Simulation without thresholds source)
2.5u

## Slide 24: Monte-Carlo Simulation
We have done Monte Carlo simulations – according to first simulations mismatch (6 sigma) is up to ~2.5uA – which is still smaller than 4uA which produces missing codes
(Simulation with thresholds source)
Comparator input current for current memory cell current of 4uA (code 64)
If less than 0 we have a long code
2.3u

## Slide 25: Monte-Carlo Simulation
(Simulation with clocked comparator)
Input current = 1 uA/us
14u
A
CH
12u+/-4u
TooLow
TooHi
10u
CL
2uA

## Slide 26: Monte-Carlo Simulation
Systematic offset due to Ref In variations from 600mV to 1.2V
2uA
RefIn
Sc2
Sc2
RefFB
PFB
TooLow
24u
26u
24u

## Slide 27: Monte-Carlo Simulation
Small systematic offset due to PMOS Bias variations from 2u to 8uA
0.3uA
RefIn
Sc2
Sc2
RefFB
PFB
TooLow
24u
26u
24u

## Slide 28: Layout
The NMOS current source has a complicated structure
It is based on enclosed NMOS and a PMOS that should compensate for voltage drops (the simple version with only NMOS behaved worse on DCD1)
The layout is dense
Original cell
TooLow
TooHigh

## Slide 29: Layout
Simulations done but not shown:
Mixed mode simulation of the channel with different RedIn and PMOS bias voltages – OK
ADC works well in RefIn range 0.8V – 1.1 V
Comparator simulation with different corners – OK
Comparator simulation with added 5fC coupling capacitance – the coupling capacitance can contribute to systematic offset (5fC – 2uA) – however in reality we expect less capacitance
Simulations to be done:
Mixed mode simulation of the channel combined with mismatch simulation
Mixed mode simulation of the ADC on netlist extracted from layout
Mixed mode simulation of the channel with lower local VDDA level

## Slide 30: Mismatch - Measurements

## Slide 31: …
14u
A
CH
TooLow
TooHi
10u
CL
A
14u
A
CH
TooLow
TooHi
10u
CL
A
14u
A
CH
TooLow
TooHi
10u
CL
A
ADC0
ADC1
ADC15

## Slide 32: …
14u
A
CH
TooLow
TooHi
10u
CL
A
14u
A
CH
TooLow
TooHi
10u
CL
A
14u
A
CH
TooLow
TooHi
10u
CL
A
ADC0
ADC1
ADC15

## Slide 33: DCD Measurements
A
+

## Slide 34: DCD Measurements
A
+
~1.5u
PMOS current varies by 2.8uA (from expected 24uA+48uA)

## Slide 35: EMCM Tests
ADC characterization
Sw1
Sw2
Sw4
A
TC
DAC
24 μA
SF
Sub
Add
WrB*
WrB
NotRd
AmpLow
24 μA
12 μA
Logic
Cmp1
Cmp2
ThHi
ThLo
Rd=0
3
1
Iin
RefFB
RefIn
Cf
2
En
RefIn
4
Wr*
VFBPBias
VFBNBias (VPSource2)
VFBNCasc
VPSource
VAmpPBias
VPSourceCasc
Sw3
NotWr
NotRd AND Not Wr
Sw5
RefIn
RefNWELL
To Next Cell

## Slide 36: EMCM Tests
ADC characterization
Sw1
Sw2
Sw4
A
TC
DAC
2*24 μA
SF
Sub
Add
WrB*
WrB
NotRd
AmpLow=1
2*24 μA
12 μA
Logic
Cmp1
Cmp2
ThHi
ThLo
Rd=0
3
1
Iin
RefFB
RefIn
Cf
2
En
RefIn
4
Wr*
VFBPBias
VFBNBias (VPSource2)
VFBNCasc
VPSource
VAmpPBias
VPSourceCasc
Sw3
NotWr
NotRd AND Not Wr
Sw5
RefIn
To Next Cell
2*12 μA
2*24μA - 2*24μA - 2*12μA

## Slide 37: DCD Measurements
A
+
1.5u

## Slide 38: …
14u
A
CH
TooLow
TooHi
10u
CL
A
ADC15
14u
A
CH
TooLow
TooHi
10u
CL
A
ADC15
1.5u
1.5u

## Slide 39: …
14u
A
CH
TooLow
TooHi
10u
CL
ADC15
1.5u/sqrt(2)
A
1.5u/sqrt(2)
1.5u/sqrt(2)

## Slide 40: …
14u
A
CH
TooLow
TooHi
10u
CL
ADC15
A
Sqrt(2)*1.5u/sqrt(2)

## Slide 41: …
14u
A
CH
TooLow
TooHi
10u
ADC15
6sigma = 1.5u
A
I-d
I+d
I-d
I+d
IIn
IOut
-2u
-4u
-8u
8u

## Slide 42: Summary
Measurements to be done:
VDDA measurement using test multiplexer
Analog CMC measurements on EMCM
Influence of offset DACs on noise
Matching after irradiation (DC measurement)
Noise without TIA (after irradiation)
Noise without input current source (after irradiation)
Measurements of large matrix (pilot run)
Analog EMCM, influence of offset DACs on noise, gated mode

## Slide 43: DCD 3 irradiation up to 7 MRad
No significant changes after 7 Mrad and 6 days of annealing
ADC characteristic
Analog characteristic of CSC
Noise – channel 1
Noise – channel 2

## Slide 44: Summary
We are planning to submit the final DCD design end of August.
Several improvements:
Digital transmission
Larger output buffer current, adapted scheme, improved radiation tolerance of the output buffer
ADC long code problem
Better layout for better matching
Same orientation in cells
Larger transistors
Reduced voltage drops by distributed bias scheme and reduced RefIn current
Many important measurement results are missing, impossible to have them before the next submission

## Slide 45: SWITCHER

## Slide 46: SWITCHER
SWITCHER
Irradiation of latest SWITCHER has been done at KIT (dose 21 MRad)
The chip works after the irradiation
Bumping: bumping so far done in HD-lab, this works well for prototyping but is slow for production
Bumping with the required pitch (150 μm) is not offered by the vendor (AMS/IBM)
Solution: Company Pactec can place underbump metallization (ENIG) and solder bumps on single dies
SWITCHER submission planned for end of August 2015
Improvements: faster clear driver, needs larger decoupling capacitors for voltage regulators
Separated control of the termination resistance for serial input (should be always on) and for the other fast inputs
Pad geometry should be adapted

## Slide 47: Rise Time Measurements – irradiated chip
Irradiation to 21MRad – 150pF load
We need to increase size of the power transistors
Can be done, but the chip size will increase by 100um

## Slide 48: Simulation
Simulation of clear pulse with 150pF load
Output transistors 3 time wider
20ns

## Slide 49: DCD – Measurements (2)

## Slide 50: DCD tests on single chip PCB

## Slide 51: Chip #1 Test all ADCs

## Slide 52: Chip #1 Test all ADCs
…
ADC characteristics
Noise of the first ADC
Deviation from mean for every input
INL of the first ADC
Deviation from linear fit for every input
DNL: code difference for two consecutive inputs
(first ADC)
All ADCs:
Gain (nA/LSB)
Average noise (LSB)
INL (peak to peak for all inputs)
DNL (peak to peak for all inputs)
Gain vs. ADC position
Noise vs. ADC position
INL vs. ADC position
DNL vs. ADC position

## Slide 53: Chip #1 Test all ADCs
Several ADCs show higher noise (out of 128 tested)
Bad ADCs

## Slide 54: Chip #1 Test all ADCs
…
ADC gain 73nA/LSB
Noise floor: ~0.58LSB (92e @ gq 450pA/e)
3LSB
3LSBs
Noise of the ADC: ~1.3LSB (210e @ gq 450pA/e)
INL the „bad“ ADC: ~5.3LSB

## Slide 55: Chip #2 test all ADCs – fit (-100 to 125)
…

## Slide 56: Chip #2 Test all ADCs
Another chip: no bad ADCs – probably due to more careful optimization of bias parameters
ADC gain 72nA/LSB
Noise: ~0.55LSB
2.5LSB

## Slide 57: Irradiations

## Slide 58: …
Example the measurement of all ADCs on the EMCM performed on the chip irradiated to 3MRad.
All ADC lines for gain 2 setting (output resistance 15kOhm) appear nice.
In the case of gain 1 setting there are several ADC lines which are not good. This is a surprising (“under investigation”), since the only difference between two measurements is the value of the resistor. One explanation can be that first ADC cell works better with an input resistance of 15kOhm. For this setting the bandwidth is lower and the noise is better filtered. In the final design we will use 15kOhm.

## Slide 59: …
…

## Slide 60: …
…

## Slide 61: …
When we look to the lines with gain 2, we can notice that some number of ADCs have a bump (a long code 63)
We have tried to investigate this problem. Our simulations show that if the comparator threshold ThHigh of the first cell is by 2uA (25% of the range) higher than the nominal one, such a problem can occur. The input current is not recognized as too high in the first cell and the current overflows in all subsequent cells.
The resulting code is 63 until the comparator “fires”.

## Slide 62: …
It is a statistical problem. It occurs only in small number of cells.
One explanation: mismatch between the mirror and the original cell. The effect of mismatch is probably enhanced by voltage drops.
The current source IPSource2 may be too strong or PMOS currents too weak, making the threshold too high.
PFB
RefFB
Sc2
RefIn
Sc2
Sc2
RefIn
Sc2
RefFB
PFB
TooLow
24u
24u
24u
24u
26u
24u
Low

## Slide 63: …
Notice also, that the threshold depends to some extent on RefIn voltage.
We know: Mostly all affected pixels are far away from the power contacts. In this regions IPSource2 is stronger with respect to IPSource and IPFB (a voltage drop effect). (=> ADC range is smaller) Also, Ref is smaller due to voltage drops. We can mitigate the problem by reducing RefIn – however this may cause problems in ADCs where IPSource2 has mismatch in other direction or RefIn is higher.
Solution would be to improve the matching of the mirror- and the original cell by several measures
Larger transistors, equal orientation of the transistors, less local voltage drop (within one ADC), separated bias lines or reduced Refin current for less global voltage drop.
PFB
RefFB
Sc2
RefIn
Sc2
Sc2
RefIn
Sc2
RefFB
PFB
TooLow
24u
24u
24u
24u
26u
24u
Low

## Slide 64: …
It is good to increase slightly VPSource (and thus the ADC range) and keep the other bias settings unchanged.
The allowed offset is 25% of the range, so it increases when we increase VSource. If we keep the other settings constant, the mismatch and voltage drop caused offset stays the same.

## Slide 65: …
Irradiation results:
The irradiation has been done on EMCM. One DCD/DHP pair has been irradiated.
Before irradiation the chip settings were optimized. We see that it is optimal when IPSource setting is a bit higher than IPSource2/IFB.
In the following measurement, the IPSource2 has been varied. Only a subset of critical ADCs have been measured. The noise plots look fine. The noise is 2 – 2.5 LSBs for gain 2. It is probably caused by the long line between the calibration current source and the ADCs.

## Slide 66: …
Irradiations: Optimization before irradiation

## Slide 67: …
Irradiations: Optimization before irradiation

## Slide 68: …
Irradiation results:
Every NMOS transistor in the analog part is done with enclosed geometry. We know that enclosed NMOS transistors are radiation tolerant. Transistors are separated by guard rings.
In digital part – NMOSes are not enclosed!
Important results: The digital communication between DCD and DHP is affected by irradiation. This can be seen from the following measurement.
DCD sends a digital test pattern. DHP delay setting is varied until the correct data pattern is received. There are two delay settings - a global one that is of duration of one clock period - 3ns. A local one, that should, ideally, be much finer.
Even before irradiation, there is not much space where a correct data pattern is received.

## Slide 69: …
Irradiations: digital communication

## Slide 70: …
There are many imperfect details.
The digital amplitude produced by DCD is not large – 220mV. The amplitude was chosen such to save the power in output drivers. They operate with 220Ohm termination resistance and 1mA current.
After irradiation (particularly in the dose range ~ 1 MRad) the data links behave worse than initially.
Possible explanation: in this dose range the digital amplitude gets smaller.

## Slide 71: …
Irradiations: digital communication

## Slide 72: …
After 20MRad and annealing, the DCD works well as before the irradiation.
However, the most critical dose is not the highest one. The effects to NMOS transistors usually show a turnaround. There is a threshold voltage decrease from 0 – several MRad (due to trapped holes) and then again increase. The increase can be addressed to activation of the interface traps (which are usually filled by H atoms who get removed). These traps compensate for the trapped holes. Additionally it may be an effect of annealing.

## Slide 73: …
Irradiations: after 20MRad and 5 days annealing

## Slide 74: …
Irradiations: after 20MRad and 5 days annealing

## Slide 75: …
ADC curves at 1MRad. Equal setting as for 20 MRad. For low VPSource2 there is a problem in one ADC. It seems that one bit is stuck.
This is still under investigation. Notice that the problem didn’t occur when the same ADC was measured for low gain setting. Most probably it is a problem in digital communication.
With optimized setting the problem vanished.

## Slide 76: …
Irradiations: after 1MRad

## Slide 77: …
Irradiations: after 1MRad

## Slide 78: …
Irradiations: after 1MRad

## Slide 79: …
The results for 2 and 5 MRad. At 5 MRad the stuck bit problem occurs only at low gain setting. It is difficult to say whether it is caused by wrong data transfer or by ADC itself

## Slide 80: …
Irradiations: after 2MRad

## Slide 81: …
Irradiations: after 2MRad

## Slide 82: …
Irradiations: after 5MRad

## Slide 83: …
Irradiations: after 5MRad

## Slide 84: …
Conclusion: for every step in irradiation, we can find a setting for which the ADCs work fine either in low- or in high gain mode.
Digital communication should be made more robust by increasing of the amplitude in DCD’s transmitter and improving the digital receiver/delay cells in DHP. (Better granularity and symmetry.)
Concerning ADC noise, it was 2 LSBs at 0 and 20 MRad as well as 2 and 5 MRad but had a peak at 3.5 LSBs at 1 MRad.
This effect is under investigation
Bias V.
ADC
RC

## Slide 85: Backup Slides

## Slide 86: DCD tests on EMCM

## Slide 87: DCD
EMCM
All ASICs can be configured and read out, Switcher outputs ok
Small PXD6 matrix connected to DCDPipeline

## Slide 88: EMCM Tests
Digital test pattern has been used to tests the digital blocks and the communication DCD - DHP
bit | 29 | 30 | 31 | 0 | 1 | 2 | 3
7 | 0 | 0 | 0 | 1 | 0 | 0 | 0
6 | 1 | 1 | 0 | 0 | 0 | 1 | 1
5 | 1 | 1 | 0 | 0 | 0 | 1 | 1
4 | 1 | 1 | 0 | 0 | 0 | 1 | 1
3 | 1 | 1 | 0 | 0 | 0 | 1 | 1
2 | 1 | 1 | 0 | 0 | 0 | 1 | 1
1 | 1 | 1 | 0 | 0 | 0 | 1 | 1
0 | 1 | 1 | 0 | 1 | 0 | 1 | 1
DCD digital block
Test pattern
ADCs
mux
DHP

## Slide 89: EMCM Tests
Digital test pattern has been used to tests the digital blocks and the communication DCD - DHP
~/TIMING/15_12_22_DCDpp0_1/test_pattern_of_dhpdcd0_bit61_SLDY_0.pdf
~/TIMING/15_12_22_DCDpp0_3/test_pattern_of_dhpdcd0_bit15_SLDY_0.pdf
305MHz, DCD1, VDDD=1.8V
250MHz, DCD1, VDDD=1.8V
column 223
(128ADU 160ADU)

## Slide 90: EMCM Tests
Digital test pattern has been used to tests the digital blocks and the communication DCD - DHP
~/TIMING/15_01_07_DCDpp0_1/test_pattern_of_dhpdcd0_bit0_SLDY_0.pdf
~/TIMING/15_01_08_DCDpp3_2/test_pattern_of_dhpdcd3_dcd_cmos_clk_dly_0_pll_ser_clk_dly_1.pdf
305MHz, DCD1, VDDD=1.9V
305MHz, DCD4, VDDD=1.9V
PLL_SER_
CLK_DLY=1
column 191
(128ADU 132ADU)
✔

## Slide 91: DCD Measurements
Test pattern
bit | 29 | 30 | 31 | 0 | 1 | 2 | 3
7 | 0 | 0 | 0 | 1 | 0 | 0 | 0
6 | 1 | 1 | 0 | 0 | 0 | 1 | 1
5 | 1 | 1 | 0 | 0 | 0 | 1 | 1
4 | 1 | 1 | 0 | 0 | 0 | 1 | 1
3 | 1 | 1 | 0 | 0 | 0 | 1 | 1
2 | 1 | 1 | 0 | 0 | 0 | 1 | 1
1 | 1 | 1 | 0 | 0 | 0 | 1 | 1
0 | 1 | 1 | 0 | 1 | 0 | 1 | 1
Channel 191

## Slide 92: DCD Measurements
Test pattern
DCD ck
DCD data
Seen by DHP
Delayed data DHP
Synchronized by DHP
Channel 191
DCD ck
DCD digital block
VDD
Bias block
DCD
DHP
Duty cycle

## Slide 93: DCD Measurements
Digital communication works for ~ 99.5% channels
Can be improved (next submissions) by slight resizing of bias currents, delay elements in DHP and DCD
RLC models of DEPFET needed
bit | 29 | 30 | 31 | 0 | 1 | 2 | 3
7 | 0 | 0 | 0 | 1 | 0 | 0 | 0
6 | 1 | 1 | 0 | 0 | 0 | 1 | 1
5 | 1 | 1 | 0 | 0 | 0 | 1 | 1
4 | 1 | 1 | 0 | 0 | 0 | 1 | 1
3 | 1 | 1 | 0 | 0 | 0 | 1 | 1
2 | 1 | 1 | 0 | 0 | 0 | 1 | 1
1 | 1 | 1 | 0 | 0 | 0 | 1 | 1
0 | 1 | 1 | 0 | 1 | 0 | 1 | 1
127
0
-127
127
0
-127
0
127
0
127
Channel 191
Ideal
Realistic
In DHP - CMOS
Reduced sampling window

## Slide 94: EMCM Tests
ADC readout – only one channel has unstable bit 6 (64) (digital problem?)
305MHz, DCD1, VDDD=1.9V
Column 209
ADU: 30, 31, 32, 33 & 63

## Slide 95: EMCM Tests
ADC characterization
ADCs have been measured using internal- and DHE current source
Only 3 ADCs with slightly higher noise – unstable bit (e.g. bit 5)
Column 52
ADU: 94, 95, 96, 126, 127

## Slide 96: EMCM Tests
ADC characterization
Noise measurement with LMU power supply on EMCN
Noise 0.5LSB < 100e
Only one ADC with noise ~ 1.5 LSB
4 DCDs on
daciampbias = 66
dacifbpbias = 80
dacipsource = 88
dacipsource2 = 77

## Slide 97: EMCM Tests
ADC characterization
Sw1
Sw2
Sw4
A
TC
DAC
24 μA
SF
Sub
Add
WrB*
WrB
NotRd
AmpLow
24 μA
12 μA
Logic
Cmp1
Cmp2
ThHi
ThLo
Rd
3
1
Iin
RefFB
RefIn
Cf
2
En
RefIn
4
Wr*
VFBPBias
VFBNBias (VPSource2)
VFBNCasc
VPSource
VAmpPBias
VPSourceCasc
Sw3
NotWr
NotRd AND Not Wr
Sw5
RefIn
RefNWELL
To Next Cell

## Slide 98: EMCM Tests
Different gain settings

## Slide 99: EMCM Tests
Missing code
„missing code“

## Slide 100: SWITCHER
SWITCEHR chips generate fast high-voltage pulses of up to 20 V amplitude to activate gate rows and to clear the internal DEPFET gates.
SWITCHER is implemented in HV AMS 180nm technology.
32 channels with a clear- and a gate-driver each.
SWITCHER in 180nm AMS

## Slide 101: DCD Measurements
Noise vs. Code
Bias V.
ADC
RC

## Slide 102: Problem of low ADC end
Problem of low ADC end
M1 current too weak
Resistance Sw too high
Out too low (Amplifier A saturates)
Low VT of PMOS not produced or bad corner – do corner simulation
Try
Increase Sc2
Decrease NMWELL voltage
Increase RefFB voltage
Decrease AmpLow (better Out_low), but increase IPAmp for higher in
In next chip – increase W/L of differential PMOS
PFB
RefFB
Sc2
Sc2
RefIn
24u
24u
24u
M1
Sw
Out

## Slide 103: …
DCD is a multi channel ADC chip
The ADCs are of the pipeline type.
This means, for 8-bit resolution we need ~8 cells.
The cell contain or two current mode memory cells, two mirror cells, two comparators.
Algorithm: The input current is stored into both cells. Mirror cells make two copies of the current stored in cell 1. The two copies are compared with the high and low threshold. If the current is higher than the high threshold a reference current (ISource) will be subtracted from the output. If the current is lower than the low threshold, the reference current is added to the output.
14u
A
CH
12u+/-4u
TooLow
TooHi
10u
12u+/-4u
CL
B

## Slide 104: …
Why do we need two current memory cells? => the output signal must be the duplicated. We implement the duplication by adding up two stored currents.
The current memory cells are biased by, internally generated, voltages VPSource2 and VPFB. The currents IPSource2 and IPFB should be equal.
The thresholds of the comparators and the reference current are controlled by the bias voltage VPSource.
The reference current and VPSource determine the size of LSB and the ADC range.
For the standard setting (64) the ADC range is 16uA.
IPSource2/IPFB determine the dynamic range of the current memory cell – for standard setting (64) the dynamic range is 24uA.

## Slide 105: Missing codes
The problem can be solved by changing of layout, which can be done within one-two weeks.
Question: Is the long code problem worth of this effort
It reduces dynamic range by ¾
Dynamic range is still 20u which should be ok
„missing code“
20uA