## Slide 1: Laser Measurements (as comparison to test beam data)
Florian Lütticke
University of Bonn
9th VXD Belle 2 Workshop Valencia, 14.01.2016

## Slide 2: Outline
Measurement Setup
Drift/HV Measurements
CCG/Clear Measurements
Large area scan
Large area scan at low HV
Transistor characteristics of PXD 9
… and sorry for using so much color!

## Slide 3: Setup
Hybrid 6
optics
Laser
Reflection of me, taking a picture of the lasersystem
Motor table

## Slide 4: Measurement Setup
Measurement:
Move laser over the matrix
At each point take 800 frames
Step width: 5 um in both directions
8*10 pixels from 2 gates
Analysis:
Create mapping between laser position and firing pixel
Using the mapping filter out noise hits
Calculate seed signal, cluster signal, cluster size, etc.. for each position
Caveat:
“high” noise when running at 128ns per gate.
Solution: Read each gate twice, throw away first reading
Probably dust

## Slide 5
Drift -1V
Drift -2V
Drift -4V
Drift -5V
Drift -6V
Drift -7V
HV -22V
HV -20V
HV -24V
HV -19V
HV -18V
HV -17V
HV -16V

## Slide 17
HV too negative:
  Charge travels close below drift contact and gets into CCG, (like Rainer said) .
  Near the internal gate, this is not a big effect.
  If HV very negative, charge seems to be lost between the pixels (below source and below clear contact)

## Slide 18: CCG vs Clear voltage Scan
First scan: Pedestals
  Find a good range to scan
What can go wrong?
Clear too negative:
  Back Emission
  Electrons overcome the barrier between clear and internal gate. Electrons from clear contact flood the internal gate.
  Can be mitigated by more negative Clear gate.
Clear too positive
  Clear is attractive for electrons during charge collection
  Charge loss

## Slide 19: CCG vs Clear voltage Scan
CCG too negative:
  Charge is not able to overcome the CCG Barrier between drift region and internal gate. Stays there long and diffuses -> bigger Clusters in Drift region.
  Can be mitigated by high clear
  Also: CCG can form a channel between source and drain – high drain currents!
  Later effect can be mitigated by positive Clear
CCG too positive
  Separation between internal gate and clear does not work anymore
  Charge loss

## Slide 20
Clear Gate -1V
Clear Gate -2V
Clear Gate -3V
Clearlow
5V
Clearlow
4V
Clearlow
3V
Cluster Signal

## Slide 21
Clear Gate -1V
Clear Gate -2V
Clear Gate -3V
Clearlow
5V
Clearlow
4V
Clearlow
3V
Seed Pixel position

## Slide 22
Clear Gate -1V
Clear Gate -2V
Clear Gate -3V
Clearlow
5V
Clearlow
4V
Clearlow
3V
Cluster size

## Slide 23: Large Laserscan
Scan most of the matrix with the laser
On each step: move module, trigger system, check data integrity
  Roughly I get 2000 laser points per hour (1.6 sec per point)
  5 um step size not doable on 153.000.000 um^2 (6 Million points, 4-5 months)
Each ~6000 steps take pedestals
Step size 11um and 22um (Pixel size is 50um x 100 um)
  4-5 steps per pixel
  Step size does not divide pixel size – can be used to project scans of multiple pixels onto a standard pixel and get better resoultion
  Small enough to guarantee to have a laser spot in the center of pixel (gain determination)
  Still takes rather long (around two weeks, perfect for )

## Slide 24: Uncorrected pedestals
Very low pedestal currents
(way outside of dynamic range)
Col
Row

## Slide 25: Corrected pedestals
Very low pedestal currents
(way outside of dynamic range)
Area scanned by laser
Col
Row

## Slide 26: Large Laserscan
Col
Row

## Slide 27: Large Laserscan

## Slide 28: Large Laserscan

## Slide 29: Large Laserscan

## Slide 30: Large Laserscan @ HV=-14V
Col
Row

## Slide 31: Large Laserscan @ HV=-14V
Col
Row

## Slide 32: PXD 9 Transistor characteristics

## Slide 33: PXD9: Measurement of DEPFET IV curves
Task: Change VGS, measure IDS
Use ADC in DCDBp for current measurement
ADC has limited range:
  Measure IDS vs VGS
  Increase ISub_In
  Repeat
Assume same VGS, same IDS
  Reconstruct ISub_In
  Add ISub_In to reduce all parts to one curve

## Slide 34: Summary
Optimal voltages of large PXD6 Matrix were determined using Laser scans.
  Obvious non ideal operation points were also studied.
  Module working very nice (though with lower speed)
  Comparison to test beam results will be done soon
Large Area scan revealed gain gradient following the pedestal distribution
  Expected, due to extreme pedestal distribution
  Offset compensation works very nice
At low voltages, stripes (rings?) are observed, similar to PXD9
  HV between -15V and -20V work