## Slide 1
pilot module assembly
- lessons learned -

## Slide 2: Module Assembly – overview
Flip Chip of ASICs (~240°C):
  Bumped ASICs have the same solder balls (SAC305)
    DHP bumping at TSMC, DCD bumping via Europractice
    So far SWB bumping on chip level at PacTech
  @ IZM Berlin
SMD placement (~200°C):
  Passive components (termination resistors, decoupling caps)
  Dispense solder paste/jetting of solder balls, pick, place and reflow
    PbSn 37/63 solder
  @ HLL, backup at IFIC
Kapton attachment (~170°C), wire bonding:
  Solder paste printing on kapton,
    SnBi solder
  Wire-bond, wedge-wedge, 32 µm Al bond wires
  @ MPP Munich
  Link to Google sheet: List of observed issues to be followed up

## Slide 3: Flip Chip at IZM
IZM experience
  First flip chip on EMCMs 2013
    10 EMCMs, two modules showed problems after FC, cause not completely clear
    4 PXD9 modules: 3 perfect, one had issues with SWB FC
  W30-OF2 somehow “cursed”
    IZM used manual equipment instead of automatic  bad soldering!
    Trials to repair, shipment  module broke

## Slide 4: W30-OF2

## Slide 5: SMD: Status as of today
Tooling and process installed at HLL
Two EMCMs successfully assembled
With special adapter plates assembly of pilot modules done
EMCM Qualification

## Slide 6: SMD: Qualification of the process
Shear tests of SMDs  okay (350g to 470g for 0201 cap)
Cross sections  okay
Thermal cycling  okay (-50°/+50°, no effect on shear strength)

## Slide 7: SMD: Qualification of the process
Optimization, fine tuning, reliability …  need higher quality SMDs
Crack in SMD cap. ceramics

## Slide 8: SMD: Qualification of the process
Optimization, fine tuning, reliability …  reduce solder paste volume
“Side balls”

## Slide 9: SMD Profile
10µF 0401 SMD on EOS are too high!

## Slide 10: SMD Profile
DCD, SWB@Balcony okay?

## Slide 11: Kapton attachment
  Screen printing of solder: Bi58/Sn42
Solder stop on kapton too wide
Possible contact to cutting edge
 short to bulk

## Slide 12: W30-OB2

## Slide 13: W30-OB2

## Slide 14: Wire bonding to kapton
Non-standard parameters, difficult wire bonding to kapton pads
dummy

## Slide 15: Wire bond pads on kapton

## Slide 16: Metal system on kapton

## Slide 17: Metal system on kapton

## Slide 18: Summary
:- pilot run was also the first hot assembly!
:- many lessons learned
:- flip-chip basically okay, need more care for shipment
:- a bit of optimization in SMD, find smaller caps (!), quality of caps …
:- isolate kapton/module edge to avoid shorts
:- improve metal system on Taiyo kapton
:- more complete list:
:- on google docs: link