## Slide 1: Silicon Detectors
The big success of silicon radiation detectors is based mainly on:
Large signal:
106 electrons/cm (gas: 20-50 electrons/cm)
Fine pattering (photolithography):
=> excellent spatial resolution O(10 µm)
Good detection properties for light and soft x-rays
Well established production methods
(semiconductor industry)
- Good interfacing to electronics (integration)

## Slide 2: Silicon Detectors
First Lecture (1.7.16)
Semiconductor:
basic properties
pn junction,
leakage current
signal generation
charge transport
Interaction with radiation
Semiconductors: Si, GaAs, others
Second Lecture (4.7.16)
Fabrication of silicon detector
Silicon Detectors: Detector Types
Diodes
Strip Detectors,
Double Sided Strip Detectors
Pixel Detectors
Drift Detectors
CCDs
Silicon Photomultipliers
Radiation Damage
Silicon Detector Systems:
Front End Electronics
Noise
Integration
Active Pixel Sensors
CMOS Sensors
DEPFETs
Detector Systems

## Slide 3: Literature

## Slide 4: Band Model
Eg
Conduction Band
Valence Band
Fermi Level
k: Boltzmann constant
Ef: Fermi Level
Ec
Ev
Conduction Band
Valence Band
Fermi Level
Eg
Conduction Band
Valence Band
Fermi Level
Discrete energy levels of atoms develop into allowed energy bands and forbidden zones if ‘squeezed ‘ together in a solid state body
insulator
semiconductor
concuctor

## Slide 5: Fermi-Statistics
Chart: 
E/eV
F(E)
Ef

## Slide 6: For E>Ev
Chart: 
| 1.0000000000000007 | 1.0100000000000007 | 1.0200000000000007 | 1.0300000000000007 | 1.0400000000000007 | 1.0500000000000007 | 1.0600000000000007 | 1.0700000000000007 | 1.0800000000000007 | 1.0900000000000007 | 1.1000000000000008
 | 3.9815e-09 | 2.7042e-09 | 1.8367e-09 | 1.2475e-09 | 8.4732e-10 | 5.7551e-10 | 3.9089e-10 | 2.6549e-10 | 1.8032e-10 | 1.2248e-10 | 8.3187e-11
 | 4.6421e-10 | 3.0203e-10 | 1.9651e-10 | 1.2786e-10 | 8.3187e-11 | 5.4124e-11 | 3.5215e-11 | 2.2912e-11 | 1.4907e-11 | 9.699e-12 | 6.3104e-12
E/eV
F(E)
T=300K
T=270K

## Slide 7: Intrinsic Semiconductors
Intrinsic Semiconductors: Si, Ge, D (Diamond), InSb, GaAs, InAs, CdS, CdTe…..
At T = 0°K: Half of the states occupied by electrons:
empty conduction band
full valence band
=> no conductivity
Silicon: band gap ~ 1 eV: thermal excitation at finite temperature
Eg
Conduction Band
Valence Band
Fermi Level
Intrinsic
Ev
Ec
n
p

## Slide 8: Carrier Densities
Density of states (conduction band):
Electron density (conduction band)
Similar for holes (valence band)
Nc and Nv are the effective density of states at the conduction and valence band
Charge conservation and Eg = Ec-Ev:

## Slide 9: Carrier Density
Law of mass action
(holds even if )
Charge conservation:

## Slide 10: Doped Semiconductors
Pure Silicon: all bonds saturated: intrinsic semiconductor
Free carriers only by thermal generation: high resistivity, large temperature dependence
Eg
Conduction Band
Valence Band
Fermi Level
Intrinsic
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si

## Slide 11: Doped Semiconductors
N-doped: an unbound electron of phosphorous atom can easily be ionised and act as free carrier. In the band model this is an donor ~45 meV below the conduction band.
At room temperature these states are ionized and the electrons move freely in the conduction band
Si
P
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Conduction Band
Valence Band
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
n-doped
-

## Slide 12: Doped Semiconductors
p-doped (e.g. Boron): missing bond acts effectively as positive charge (‘hole’)
In the band model this corresponds to an acceptor level ~45meV above the valence band
At room temperature these states are occupied and the corresponding holes in the valence band act as free carriers
Conduction Band
Valence Band
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
p-doped
Si
B
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
+

## Slide 13: Doping
Eg
Conduction Band
Valence Band
Fermi Level
Intrinsic
Conduction Band
Valence Band
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
n-doped
Conduction Band
Valence Band
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
p-doped
Si, Ge, GaAs, InSb..
Doped with
P, As, Sb
‘Donor’ ND
Doped with B
‘Acceptor’ NA
DE~0.045eV

## Slide 14: Basics: the pn-junction
At the junction: creation of a depleted region (space charge)
Conduction Band
Valence Band
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
Conduction Band
Valence Band
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
Vbi
d
n-doped
p-doped

## Slide 15: pn-junction forward biased
Forward bias (positive voltage at p-region)
Depleted zone reduced => current increase
Conduction Band
Valence Band
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
Conduction Band
Valence Band
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
Vbi
d
+
Vext
n-doped
p-doped
D: diffusion coefficient
t: recombination lifetime

## Slide 16: pn-junction: reverse biased
Conduction Band
Valence Band
-
-
-
-
-
-
+
+
+
+
+v
v+
Conduction Band
Valence Band
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
Vbi
n-doped
p-doped
v+
v+
-
-
Vext
Reverse bias (positive at n region): increase of depleted zone
Current dominated by thermal generation current (leakage current)
+v
-

## Slide 17: pn-junction under bias
Applying a (reverse) voltage increases the
depleted region
Electric field:
Potential:
Thickness of depleted region
Voltage to deplete a thickness D
2x1011 cm-3
1013 cm-3
e = e0 esi ~ 1 pF/cm
dep
p
n

## Slide 18: Depleted Diode: Current and Capacitance
No free charge carriers in depleted region
except:
Thermally generated current
Small leakage current
Capacitor (parallel plate):
Difference to a chamber: space charge!
=> can be used to shape field

## Slide 19: Leakage Current
Shockely Read Hall
Eg > kT (T = 300K)
No generation or recombination at room temperature
However, generation and recombination possible due to mid-gap traps = recombination centres
Eg
Conduction Band
Valence Band
x
Fermi Level
x x x x x x
Leakage current level depends on impurity level
Rule of thumb: leakage current doubles each 6°C temperature rise

## Slide 20: IV and CV characteristics
 | U < Udep | U>Udep
1/C² | ~U | const. (measures Udep)
I |  | ~const (+ surface contributions)

## Slide 21: Examples
Doping concentration is related to the resistivity r and the carrier mobility m
For silicon
1
2
3
4
5
1: extremely pure n-type silicon (hard to get)
2 fairly pure n-type material
3: note: for p-type material: mh = me/3
4: irradiated material (LHC level: 1014 neutrons(1MeV)/cm2)
5 extremely irradiated (sLHC): 1016 neutrons(1MeV)/cm2)

## Slide 22: Solid State Ionisation Chamber
Electrons & holes generated by ionising particles or photon conversions drift to the electrodes and induce a signal

## Slide 23: Charge Transport
In the electric field the charge carries drift to the electrodes with a velocity
For not too large fields! At high fields (Esat) the drift velocity saturates and becomes independent of the field (here Silicon):
Electrons drift three times faster than holes (in Si)
Saturation can happen in Si-sensors (thick, low resistivity)

## Slide 24: Charge Collection time
For low fields (no saturation) the transition time to traverse a sensor of
thickness d is:
Udep: Voltage to deplete the device with thickness d
DU: overvoltage (for DU = 0 the transition time becomes infinite)
(in practice: collection by diffusion)
e.g. 20kOcm n-type, Udep=15V, DU=5V, d=300 mm:
ttrans(e)=40ns trans(h)=120ns
Can be improved going to higher fields (low resisitivty material)
e.g. 2kOcm n-type, Udep=150V, DU=10V, d=300 mm
ttrans(e)=2ns trans(h)=6ns

## Slide 25: Charge Spread
a) Diffusion:
D=kT/m
For detectors of d=300 mm: s ~ 5-20 mm
b) Lorentz angle:
-> spreads charge over larger area
-> larger Lorentz angle for electrons (4.5 x)
~ 10° at 1T
mh: Hall mobility differs from drift mobility
e: mh = 1670 cm2/Vs m=1450 cm2/Vs
h: mh = 370 cm2/Vs m=505 cm2/Vs
B
E

## Slide 26: Charge Collection
Does one need to collect the charges physically on the electrodes to detect a signal?
No!
Moving charges induce a current (S. Ramo, 1937)
Ewi is the weighting field, parameterizing the coupling of a charge to the electrode I
It depends only on the geometry of the electrodes, not on space charge, Ubias etc.
Set Uwi = 1 for the collecting electrode
Uwi = 0 for all other electrodes

## Slide 27: Charge Collection
The induced charge of a carrier drifting from r(t0) to r(t) is:
For an electron drifting from r0 to the anode at r=d:
And the hole drifting to r=0 (“backplane”)
The sum of the two contributions is q, independent of r
      Q = Qe + Qh = q
Both electrons and holes contribute, but with different magnitude
0
)]
Qe =
Qh =

## Slide 28: Planar Diode
A planar diode has a simple, linear weighing potential
(and a constant weighting field)
The contribution of electron and holes is proportional to their respective drift path,
That is, on average, equal.
This is fo for a n in p device, the collecting electrode collects electrones!
backplane
n/p junction
n bulk

## Slide 29: Segmented Device (Strip, Pixel)
The weighting potential gets strongly peaked at the collecting electrode
=> Signal contribution dominated by the region close to the electrode
This is fo for a n in p device, the collecting electrode collects electrones!
n bulk
backplane
n/p junction

## Slide 30: Consequences
Signal shape: fast component by electrodes followed by a slow component of the holes (slower drift)
Relative contribution of (slow) hole and (fast) electron signal depends on the distance to the electrode
Neighbour electrodes: U(r=0) = U(r=d) = 0
should not see a signal!
induced current is bipolar and integrates to 0
However: if the charge collection is incomplete (trapping, partial depletion)
Signal visible on neighbour electrodes
even with opposite polarity

## Slide 31: Impact Ionisation
In high electric fields electrons and holes acquire enough energy to create e-h pairs by impact ionisation
Electrons >~ 300 kV/cm
Holes >~ 400 kV/cm
300 kV/cm < E < 400 kV/cm
Only electrons ionize
Linear mode
Gain < 10
N(l) = exp(al)
E ~ 400 kV/cm
Both electrons and (rarely) holes ionize
Still linear mode
Gain: 50 – 300
Excess noise: s(N) = k N1/2
d
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
t
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
t
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
t
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
t
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
h
e
e
e
e
h
h
h
e
h
e
h
E > 400 kV/cm
Both electrons and holes ionize
Geiger mode
Gain: infinite (breakdown)
e: ~ 1 pair/µm
h: ~ 0.1 pair/µm
e: ~ 4 pair/µm
h: ~ 0.8 pair/µm
e: ~ 8 pair/µm
h: ~ 2 pair/µm

## Slide 32: Impact Ionisation
High electric fields must be avoided not to risk breakdown
On the other hand: a smart implementation of high field regions lead to sensors with intrinsic amplification
= > APD (avalanche photo diode)

## Slide 33: Interaction of Radiation with Matter
Ionizing Radiation:
detection and tracking of charged particles
=> Bethe Bloch Formula
Non Ionizing Radiation
  Photons
  visible: Inter-band transitions: discussed later
  X-ray and gamma:
  Photo Effect
  Compton Effect
  Pair creation
  In the energy range useful for silicon detectors the photo effect dominates

## Slide 34: Ionisation
The average energy loss due to ionisation is given by the Bethe-Bloch formula:
(see PDG report p. 258 for the symbols…..)
MIP =
minimum
Ionizing
particle

## Slide 35: Ionisation
Wide, asymmetric distribution (Landau)
High loss tail: contribution from d-rays: energy not deposited near the track
(lost in thin or highly segmented devices)
More relevant: most probable energy loss
Rule of thumb:
~ 270 eV/mm for MIPs in Silicon
3.6 eV are needed to create an e/h pair:
75 e/h pairs/mm
However:
Most probable energy loss decreases
for thinner layers!

## Slide 36: Energy Loss in Thin Detectors

## Slide 37: Thin Detectors
Energy lost in many collisions => statistical fluctuations
Thinner layers => less colllisons => larger fluctuations
Energy loss due to delta-rays which can escape
=> Energy loss spectrum shifted and wider than expected by Landau theory
From H. Bichsel, Rev. Mod. Phys 60 (1988)
Data
Landau

## Slide 38: Signal Generation: Optical
Photo effect: possible if Eg > Eg (=1.1 eV in Si)
Fine for visible light
Near infrared: Si becomes transparent for l> 1100 nm
UV: light is absorbed in thin (un-depleted) surface layer for l < 400nm

## Slide 39: Light Absorption in Silicon
Si Band Structure

## Slide 40: Photon Conversion Efficiency
Photon must be absorbed in the sensitive volume of the device
Problems:
Loss in insensitive surface layer (highly doped p or n implant to create junction)
depth typically O(100 nm)
Problem for short wavelengths
UV sensitive diodes need
extremely thin entrance windows
(special technology)
Photons of long wavelength traverse the sensitive volume
2 mm sensitive volume
10% conversion efficiency for l=800 nm

## Slide 41: X-ray absorption in Si
Energetic x-rays generate several e/h pairs
Useful range: 100eV – 20 keV (for Si of 500 mm thickness)

## Slide 42: X-Ray Detection
300µm
Si drift chamber
On average: 3.6 eV needed to generate an e/h pair in Si
This is more then the band gap of 1.1 eV
some of the energy heats up the lattice (creates phonons)
Consequence: improved resolution:
Fano factor F=0.1 in Si (U. Fano, Phys Rev 72 (1947))

## Slide 43: Which Semiconductor?
 | Si | Ge | GaAs | Diamond
Eg (eV) | 1.12 | 0.67 | 1.35 | 5.5
m(e) (cm2/Vs) | 1450 | 3900 | 8800 | 1800
m(h) (cm2/Vs) | 450 | 1900 | 320 | 1600
e (pF/cm) | 11.9 | 16.2 | 12.9 | 5.7
DE(e/h) | 3.6 | 3.0 | 4.35 | 13
dE/dx (MeV/cm) | 3.2 | 7.1 | 5.6 | 6.1
r (g/cm3) | 2.33 | 5.3 | 5.32 | 3.5
X0 (cm) | 9.4 | 2.3 |  | 12.15
Low Band gap => large signals
=> large leakage currents (cooling needed)
High mobility => fast signals
Low e => low capacitance => low noise
Large X0 => small multiple scattering
For a specific purpose there may be other important parameters:
Thermal conductivity, displacement energy,……

## Slide 44: Why Silicon?
Except for: large volume detectors (spectrometers): Ge
Infrared sensors (InSb, HgCdTd..)
X-ray sensors (InAs)
Silicon is dominating the market for photo and tracking detectors
Why? In many respects other semiconductors are superior?
Sophisticated and readily available processing possibilities
Electronics industry uses silicon (CMOS)
Reason: “perfect” interface of SiO2 and Si
basis for patterning, CMOS structures etc
Huge amount of knowledge how to process silicon
Processes and machinery readily available
Device and process simulation helps to design devices

## Slide 45
End of Lecture I

## Slide 46: Silicon Detectors
First Lecture
Semiconductor:
Basic properties
pn junction,
leakage current
signal generation
charge transport
Interaction with radiation
Semiconductors: Si, GaAs, others
Second Lecture
Fabrication
Silicon Detectors: Detector Types
Diodes
Strip Detectors,
Double Sided Strip Detectors
Pixel Detectors
Drift Detectors
CCDs
DEPFETs
Silicon Photomultipliers
Radiation Damage
Silicon Detector Systems:
Front End Electronics
Noise
Integration
Active Pixel Detectors
CMOS Sensors
DEPFETs
Full Detector Systems

## Slide 47: Fabrication
Fabrication of Silicon Detectors
Engineering!
Detailed knowledge of technology needed
Chemical etching
Energy/depth relation for implantations
Diffusion during thermal treatment
Optics
Technology widely used in semiconductor industry (much more advanced)
However: some details not disclosed
Cleanroom of the semiconductor laboratory of the Max-Planck Society (Munich)

## Slide 48: Fabrication
Photolithography
Start with oxidised wafer
Si-bulk
SiO2 (~100nm))

## Slide 49: Fabrication
Photolithography
Add a layer of photoresist
Si-bulk
SiO2 (~100nm))
Si-bulk
SiO2 (~100nm))
Photoresisist (~ µm)

## Slide 50: Fabrication
Photolithography
Expose to light through a patterned glass mask (chromium)
Si-bulk
SiO2 (~100nm))
Si-bulk
SiO2 (~100nm))
Photoresist (~ µm)

## Slide 51: Fabrication
Photolithography
Develop photoresist
Exposed regions are removed
Si-bulk
SiO2 (~100nm))
Si-bulk
SiO2 (~100nm))

## Slide 52: Fabrication
Photolithography
Etch away SiO2 (using HF)
Opening which can be used as a contact to the bulk
Si-bulk
SiO2 (~100nm))
Si-bulk
SiO2 (~100nm))
Si-bulk
SiO2 (~100nm))

## Slide 53: Fabrication
Implant with an ion beam to dope the silicon
Phosphor: n doped
Boron: p doped
Energy of beam and thickness of resist has to be chosen that ions are 100% absorbed in photoresist
Si-bulk
SiO2 (~100nm))
Si-bulk
SiO2 (~100nm))

## Slide 54: Fabrication
Result: diode (if p implanted in n-bulk) which can later be contacted by
metal to create a charge collecting sensor
Si-bulk
SiO2 (~100nm))
Si-bulk
SiO2 (~100nm))

## Slide 55: Layout
Si detectors are made of several structured layers
Silicon bulk with implantations
Oxide layers as insulation
Metal or polysilicon as contacts
Passivation layer
All these layers have to be designed and converted into photolithographic masks
55

## Slide 56: Device Simulation

## Slide 57: Cleanroom
particle removal by a continuous filtered air stream (from ceiling to bottom).
clean processing by handling, clothing and separation from outside world.
clean process gases and chemicals.
supply of ultra-clean water.

## Slide 58
metal_2
oxide
metal_1
polySi_1
polySi_2
n bulk
deep p
deep n
p+
n+
Animation by P. Lechner
Process steps (DEPFET)

## Slide 59: Basic Silicon Detector Types
Silicon sensors are made form Si-wafers:
Diameter thickness
4” (~10 cm) ~300 mm
6” (15 cm) ~500 mm
8” (20 cm) no high resistivity material available yet
thin, large area detectors
Photon detection (visible & near infrared)
Soft x-ray detection (spectroscopy & imaging)
Tracking of ionising particles (position sensitive)

## Slide 60: Planar Diode
Mainly used as photodiode
Area ~ 1cm2
Rather large capacitance: 80 pF => 500 electrons noise (ENC)
Readout of scintillator crystals with high light yield (CsI(Tl), BGO)
Nuclear counter effect!

## Slide 61: Strip Detectors
Position resolution (projective)
Typical pitch: p ~ (25 – 100) mm
Capacitance ~ 1pF/cm

## Slide 62: Resolution
Binary readout: fixed threshold, yes/no information
charge contained in one cell (strip)
Analogue readout with charge division & weighting:
diffusion
Lorentz angle
Inclined tracks
Capacitive division
Attention: Landau fluctuations
Effective S/N > 14%
Typical: ~10 mm, but values around 1 mm have been achieved

## Slide 63: Coupling/Bias
a) DC coupling: Bias mechanism can be part of external electronics
Bias resistor
Current sink
b) AC coupling: integrated bias mechanism
Integrated resistors: polysilicon
Punch through
Simple, but amplifier has to absorb the leakage current
No leakage current flowing into amplifier
But many resistors needed (impossible for high density pixel sensors)
Quality problem
Elegant solution: allows AC coupling without individual bias contacts

## Slide 64: Double sided strip detector
2-dimensional resolution (projective => ambiguities)
Any stereo angle possible (trade resolution versus ambiguities)
Floating electronics or breakdown of decoupling capacitors
Routing of readout lines
Interstrip insulation at n-side

## Slide 65: Interstrip Insulation
positive oxide charges attract electrons -> short between n-strips
a problem for n-strips in n-bulk (n-in-n)
and n-strips in p-bulk (n-in-p)
b) field plates (MOS structure in depletion mode)
c) p-stops
d) p-spray
Oxide charge density increases with radiation
Insulation structure impacts capacitance and breakdown behaviour

## Slide 66: Pixel/pad detectors
real 2-dim resolution
works at highest track densities
small pixels sizes (50 x 50 mm2)
Low capacitance (~400 fF)
Challenge:
Connection to amplifier
Number of channels
Data rate

## Slide 67: Sideward Depletion
Symmetric bias
Asymmetric bias
Change shape of
potential
Deplete large area detector from one small contact
=> Small capacitance

## Slide 68: Silicon Drift Detector
True 2-dim information (segmented anode & drift time)
Needs high voltage across voltage divider
Good time resolution needed for resolution of drift (~7 mm/ns)
External t0 needed: beam clock, scintillator trigger
Typical resolution: 20 mm (anode) 25 mm (drift) [STAR]
Low capacitance, low noise => measure dE/dx

## Slide 69: Silicon Drift Detector
Simpler layout and production
Unstructured backside (optimal entrance window for x-rays)
Low capacitance (~ fF) for large area detector area (~ cm2)
Extremely low noise (3-6 e- RMS)
Soft x-ray spectrometers (100eV–20keV)

## Slide 70: CCD
Shift charge in potential pockets
Extremely low noise (~2 e- rms)
X-ray imaging spectrometer
Large area possible (6x6 cm2)
Needs low temperature operation (100K)

## Slide 71: Silicon Photomultiplier
The device is operated above the breakdown voltage
Photons are absorbed in depleted silicon, create e/h pairs
The electron (or hole) drifts into high field region.
Avalanche amplification (Geiger breakdown) occurs.
The signal size (“amplification”) is given by the overvoltage and the cell capacity Q = C x DU (~ 106).
Passive quenching by integrated resistor (limits current)
Single SiPM cell: binary signal of fixed size!
Basic building block: avalanche photodiode operating in Geiger mode

## Slide 72: Silicon Photomultiplier
Array of cells all connected to a single output:
Signal = S of cells fired
If probability to hit a single cell < 1 => Signal proportional to # photons
Pixel size: ~25 x 25 mm2
- ~100 x 100 mm2

## Slide 73: Silicon Photomultiplier
Single & multiphoton peaks
“self calibrating” photon counter”
Dynamic range ~ number of pixel
Saturation for large signal: N = Npix [1-exp(- eNph/Npix)]

## Slide 74: Advantages
Simple, robust device
Photon counting capability
Insensitive to magnetic fields
Fast response (< 1 ns)
Large signal (only simple amplifier needed)
Good quantum efficiency (~ 40% @ 500 nm)
No damage by accidental light
Low operation voltage (40 – 70 V)

## Slide 75: Cross talk
Hot carrier luminescence in avalanche:
~ 1 photon/105 carries
(A. Lacaita, IEEE (1994))
Photons may trigger neighbour cells => > 1 pixel/photon
Typical values: 10% - 30%
Dark counts: Non-poisson distribution
Emission microscope picture
n+
n-substrate
p- epi
p+
p+
Trenches & Double junction

## Slide 76: Dark Rate
Thermally generated currents: Dark Rate
- Increases with overvoltage/gain (larger depleted area; tunneling)
- problem for large area devices (~50 MHz for 5x5 mm2 at room temp.)
- cooling helps (but beware of afterpulsing due to trapping)
20.7 0C
-50 0C

## Slide 77: Geiger efficiency of electrons and holes
Electrons have a higher probability to trigger an avalanche breakdown than holes
Efficiency depends on depth of photon conversion and hence on the wavelength
Solutions:
Increase overvoltage
Or:
- Ensure that only electrons trigger an avalanche
holes
p-substrate
p- epi
p+
n+
el.
n-substrate
n- epi
n+
p+
el.
holes
“standart”
inverted

## Slide 78: Sensitivity at different wavelengths
Thin entrance window needed
holes
electrons
Holes trigger
Avalanche
(p-substrate)
Electrons trigger
Avalanche (p-subs.)
p-substrate: photons < 450 nm: only holes contribute
photons > 700 nm: lost in insensitive bulk
n-substrate: ok for short wavelengths,
hole efficiency dominates for l > 500 nm
Example:
p-substrate

## Slide 79: Spectral Response
p-substrate
Measurement: IRST
peak at ~ 550 nm
Inverted structure
(n-substrate):
better blue response
peak at 400 nm
However, sensitivity becomes poor above 500 nm
(only 2 mm drift region + hole sensitivity!)
IRST
Hamamatsu

## Slide 80: Radiation Damage
Semiconductor sensors should detect radiation
Unfortunately radiation damages semiconductors
Two important damage types
Surface damage due to ionizing radiation
in Si: oxide charge up (positive), interface traps
main damage mechanism in CMOS electronics
Bulk damage: particle may displace nuclei from their lattice position
NIEL: non ionising energy loss
increase of leakage current
change of bulk properties (“type inversion”)
introduction of traps for charge carriers

## Slide 81: Increase of leakage currents
G. Lindstroem et al, NIMA 466 (2001)
Annealing!

## Slide 82: Type Inversion
- donor removal
- acceptor creation
=> type inversion (n -> p)
=> increase of depletion voltage
G. Lindstroem et al, NIMA 466 (2001)
Parameters depend on material
Complex annealing!

## Slide 83: Detector Type
n
p+
n+
E
p
p+
n+
E
n
n+
p+
E
p
n+
p+
E
p
n+
p+
E
p
n+
p+
E
irradiation
p-in-n (“classic”)
Low cost
After type inversion:
Low CCE
Cannot operate partially depleted
n-in-n
Expensive (double sided processing)
After type inversion:
high CCE
Can operate partially depleted
n-in-p
Low cost
No type inversion
High CCE
Can operate partially depleted

## Slide 84: Strip insulation
SiO2: positive oxide charges
+ + + + + + + + + + + + + + + + + + + + + + +
n+
- - - - - - - - - -
- - - - - - - - - -
n+
n+
Electron accumulation layer
N-strips shorted by accumulation layer
+ + + + + + + + + + + + + + + + + + + + + + +
n+
- - - - - - - - - -
- - - - - - - - - -
n+
n+
Electron accumulation layer
p+
p+
Accumulation layer interrupted by p-stop
(or p-spray)
Problem: capacitance
high field
n-in-n and n-in-p detectors need insulation structures (p-stop or p-spray)
Otherwise readout strips are shorted.
Fine tuning needed to adjust to changing conditions before and after irradiation.

## Slide 85: Trapping in highly irradiated detectors
If ldrift = t vdrift < d
Inefficient charge collection
Make vdrift high (saturation!)
Make d small
Electrons better than holes

## Slide 86: Electric field and drift velocity
Is there an advantage of thin detectors compared to thick detectors operated partially depleted?
At the same voltage thin
(=over depleted) detectors have a higher electric field than thick (= partially depleted) detectors
Higher drift velocity
Better CCE
(however vdrift ~ vsat)
In addition the depleted volume of thick detectors is larger
Larger leakage currents
(shot noise, heat)
Additional volume does not give a signal (ldrift<zdep)
f = 5x1015 n/cm2
Uop = 200V
Simplified!

## Slide 87: “3D” Detectors
Thin detector: high CCE but small signal
Idea (S. Parker):
collect charge horizontally to with narrowly space colums
- small drift distance: high CCE
- total detector thickness active

## Slide 88: “3D” Detectors
Processing: using RIE etching holes with ~ 1/20 aspect ratio can be etched into silicon (“Bosch process”)
Filled with doped polysilicon these holes act as charge collecting electrodes.
Complex and expensive technology -> several variants

## Slide 89: Signal Amplification
Charge Sensitive Amplifier followed by shaper (RCCR)
CSA: output proportional integrated charge Q: U = Cf x Q
Shaper: Band-path to filter out high and low frequency noise
Silicon sensors generate small signals (~ 24000 e- /MIP in 300 µm => 3.8 fC)
Need amplifiers to generate a detectable signal

## Slide 90: Signal Amplifiction
Is: Signal (current source)
Cd: detector capacitance
Cf: feedback capacitor of CSA (U = C * Qs)
Reset: = clears signal after t = R Cf
Shaper: high and low pass RC filter

## Slide 91: Noise Soures
Noise of input FET of amplifier
First term: Channel noise which depends on Transconductance qm of the FET:
µ: mobility of carriers
Cox: oxide sheet resistance of FET
W: gate width
L: gate length
ID: drain current
Serial noise: voltage fluctuations
Parallel noise: current fluctuations

## Slide 92: Noise Sources
Noise of input FET of amplifier
Second term is 1/f noise:
Due to trapping and de-trapping of charges
Approx. Proportional to 1/f
Depends on transistor parameter W and L and Cox
and a process dependent factor Kf
(~10-31C²/cm²)

## Slide 93: Noise Sources
Shot noise to leakage current Ileak
Thermal noise from bias resistor R:
Serial noise: voltage fluctuations (channel noise and 1/f noise)
Parallel noise: current fluctuations (shot noise and bias resistor thermal noise)

## Slide 94: Filtering
The power spectrum has to be convoluted by the response function of the shaper
With the response function of the RCCR shaper:
For serial noise : with Ct the total capacitance of the shaper
For parallel noise:

## Slide 95: Evaluation
Channel noise
1/f noise
Shot noise
Bias noise

## Slide 96: Noise Sources
Thermal noise input FET: ~ C/t1/2
1/f noise: ~ FET parameters, independent of t
Shot noise: ~ (Ileak t)1/2
Summing up all noise sources in quadrature and normalizing to units of elementary charge (q):
Bias noise: ~ (1/R t)1/2

## Slide 97: Typical behaviour

## Slide 98: Notes
Noise depends crucially on C, t, Ileak, R and FET technology
Noise can be minimized by an appropriate choice of t
Good practice:
reduce C (small pixels, narrow strips)
choose large bias resistor
best FET technology (good gm, low 1/f)
keep leakage current under control (cooling)
fast detectors (small t) need high gm:
=> large ID, high power!
More sophisticated filtering techniques are possible. 1/f noise can be reduced by
‘correlated double sampling’

## Slide 99: Examples
 | Area | Capaci tance | gm | current | Shaping | Channel noise | Shot noise | Bias resistor | total
Diode | 1 x 1 cm² | 33pF | 800 µS | 40 nA | 1 µs | 760 e | 250 e | 800 e | 1125 e
Strip | 12 cm x 25 µm | 15 pF | 800 µS | 2.0 µA | 25 ns | 2160 e | 280 e | 125 e | 2190 e
Pixel | 50µm x 400µm | 400fF | 800µS | 2.5 nA | 25 ns | 58 e | 10 e | - | 60 e
The leakage currents for strip and pixel assume irradiation damaged sensors (LHC)
Typical signal of a 300µm thick sensors for a MIP : 24000 e

## Slide 100: ASICs
Application Specific Integrated Circuit
Became available in the mid 80s
=> Integrate many (~100) amplifier channels in a cm2 chip
1984: Microplex (NMOS)
1988: CAMEX64 (CMOS)
Noise low enough to get S/N > 10 for 12 cm long strips
=> (small) vertex detectors in colliding beam experiments
~1cm

## Slide 101: Interconnection
Connection of sensors to ASIC using wirebonds
ASICs (hopefully) outside acceptance
Thin wire (17 mm diameter)
Simple pitch: 50 mm ok
Staggering and multiple loops:
` 12.5 mm possible (4x)

## Slide 102: Pixel Detector Electronics
Face to face interconnection: ASIC - Sensor
Pitch: 50 mm

## Slide 103: 3D Interconnection
Basic Problem:
How to integrate good sensors and good electronic circuits?
3D Interconnection:
Two or more layers (=“tiers”) of thinned semiconductor devices interconnected to form a “monolithic” circuit.
Different layers can be made in different technology
(BiCMOS, deep sub-m CMOS, SiGe,…..).
3D is driven by industry:
  Reduces R,L and C.
  Improves speed.
  Reduces interconnect power, x-talk.
  Reduces chip size.
  Each layer can be optimized individually.
Si pixel sensor
BiCMOS analogue
CMOS digital
Better: slides from vertex2012

## Slide 104: Advantages for Module Design
Contact pixels through vias:
-> 4-side buttable.
-> No “cantilever” needed.
Larger module with minimal dead space.
Less support structures & services.
Substantial material savings.
Large pitch of I/O connections allows use of large diameter/low aspect ration vias
=> Rather mature technology, several vendors

## Slide 105: New Concepts
Integration of sensor (Si) and electronics (Si)

## Slide 106: CMOS Sensors
CMOS Sensors are used as optical sensors e.g. in digital cameras
Replacing CCDs
Advantage:
Combine sensor, amplifier and processing on one chip
Cheap (CMOS)

## Slide 107: CMOS Sensors: MAPS
Modification to use as particle tracker
R. Turchetta (2000)
n-well used for signal collection
only p-well possible for FET (NMOS)
no PMOS transistors (only in periphery)
Charge collection by diffusion in thin epi-layer (slow, small signal)
Successful prototypes
(MIMOSA series, Strasbourg)
S/N: >20/1, Resolution < 2 mm
Only small (cm2) chips possible (stepping)
Evolution: triple well technologies
Many activities: France, UK, US, Italy
(MAPS, CAPS, FAPS…..)

## Slide 108: Multiple Well Technologies
p
n
n
n
p
p
N-well imbedding PMOS transistor acts as parasitic charge collection node
=> Reduced charge collection efficiency
p
n
n
n
p
p
Another p-well surrounding the n-well suppresses this parasitic charge loss.
=> Full efficiency and full CMOS

## Slide 109: Summary: Integration

## Slide 110: The DEPFET active pixel sensor
Depleted Field EffectTransistor
p+
p+
n+
drain
bulk
source
p
n+
n
internal gate
top gate
clear
n
-
n+
p+
-
-
+
+
+
+
-
-
-
-
-
-
-
Each pixel is a p-channel FET on a completely depleted bulk
A deep n-implant creates a potential minimum for electrons under the gate (“internal gate”)
Signal electrons accumulate in the internal gate and modulate the transistor current (gq ~ 400 pA/e-)
Accumulated charge can be removed by a clear contact (“reset”)
Fully depleted:
large signal, fast signal collection
Low capacitance,
internal amplification: => low noise
High S/N even for thin sensors
Rolling shutter mode (column parallel) for matrix operation
100 ns readout/pixel 20
=> Low power (only few lines powered)

## Slide 111: Matrix operation
Charge collection in "OFF" state of the transistor
Select one row via external gates and measure pedestal + signal current
Reset that row and measure pedestal currents …..
Only one single row active at a time and dissipating power
However, sensor is sensitive even if DEPFET is OFF!

## Slide 112: How does it work?
Source
Drain
P-channel
Gate
Gate-oxide; C=Cox W L
L
W
d
FET in saturation:
Id: source-drain current
Cox: sheet capacitance of gate oxide
µ: mobility (p-channel: holes)
Vg: gate voltage
Vth: threshold voltage
Transconductance:
Internal
gate
A charge q in the internal gate influences a mirror charge aq in the channel
(a <1, for stray capacitance)
This mirror charge is compensated by a change of the gate voltage:
DV = a q / C = a q / (Cox W L)
Conversion factor:
112

## Slide 113: Gain and Noise
Measurements in good agreement
Typical values:
gq ~ 400 pA/e (for L = 6 µm)
Could be pushed up to 1 nA/e
1.6 e ENC at t=10 ms
40 e ENC at t=20ns (50MHz)

## Slide 114: Detector Systems

## Slide 115: Tracking Detectors
Several (N) layers of segmented sensors within a B-field
Measure by ionisation (of gas or silicon)
Curvature k = 1/R measures the momentum
pT in GeV/c
B in T
R in m
Resolution:
L
s
For N equally spaced layers with equal position resolution s
Good resolution
Large B
Large L and N (expensive)
Good position resolution

## Slide 116: Impact Parameter
At very high energies (LHC) the decay tracks from the B become very collimated and the decay vertex becomes difficult to reconstruct.
A better parameter is the impact parameter
By how much misses track (i) the primary vertex
(lab frame)
(rest frame)
On average (spherical decay) = <d> = ct ~ 450 µm (independent of the boost)
Again: a good detector has to measure a fraction of this: s = O(10µm)

## Slide 117: What has/will be achieved
How to improve impact parameter resolution?
Small pixels
Close to the beam
Low material budget
Layer layout (lever arm)
Good S/N
Resolution
Distance to IP
Material (scattering)

## Slide 118: Some History
~1980: NA11/NA32
First silicon strip detector operating in a particle physics experiment!

## Slide 119: History
ALEPH Experiment
LEP/CERN, 1989 – 1995
First double sided silicon strip detector operation in a colliding beam experiment
Major contributions to B-physics
Evidence for Bs, Lb
Individual lifetimes of all B0, B+, Bs, Lb
Time dependence of B0 oscillations

## Slide 120: ATLAS and ATLAS Inner Detector
ID length: 7 m
ID diameter: 2m

## Slide 121: The ATLAS Inner Detector
Sub-
Detector r(cm) element size resolution hits/track channels
Pixel 5-12.5 50mm x400mm 12mm x 60mm 3 93x106
(Silicon) (3D)
SCT 30-52 80mm x 12cm 16mm x 580mm 4 6x106
(Silicon Strip) (stereo)
TRT 56-107 4 mm x 74cm 170mm 36 0.4x106
(Straw Tubes) (projective)
Three subdetectors using different technologies to match the requirements of granularity and radiation tolerance

## Slide 122: Pixel Detector Module
Sensor:
  250 μm thick n-on-n sensor
  47232 (328 x 144) pixels
  Typical pixel size 50 x 400 μm2 (50 x 600 μm2 pixels in gaps between FE chips)
  Bias voltage 150 – 600 V
Readout:
  16 FE chips, 2880 pixels each
  Zero suppression in the FE chip, MCC builds module event
  Pulse height measured by means of Time over Threshold
  Data transfer 40 – 160 MHz depending on layer

## Slide 123: Semiconductor Tracker (SCT)
4 barrel layers, 9 disks per end-cap
4088 modules, 6.3M channels (61 m2)
Intrinsic Resolution = 17 μm / 580 μm (Rϕ/z)
Operational T = -8ºC to ~5ºC
C3F8 Evaporative Cooling, in common with Pixel detector

## Slide 124: SCT Modules
strip direction
strip direction
Basic Concept (Endcap)
4 Si-strip detectors in 2 planes (40 mrad stereo)
-Mechanical carrier made from Thermal Pyrolytic Graphite (Ck>1700 W/m/°K) and AlN
-Flex Hybrid (Kapton) on carbon substrate with ASIC readout electronics
-Glas pitch adaptors for mechanical/electrical connection detector-electronics (heat barrier)

## Slide 125: SCT Silicon Detectors
Radiation tolerant up to 3x1014 p/cm2
p-on-n single sided detectors
285 micron 2-8 kOhm
4“ substrate
Barrel: 64x64 mm2
Forward: wedge shaped (5 shapes)
768 readout strips with ca 80 mm pitch
No intermediate strips
AC coupled strips
Polysilicon or implanted bias resistors
Multi guardring structure to ensure stability up to 500 V
Ca. 20000 needed
Produced by Hamamatsu and CIS

## Slide 126: Belle II
Time-of-Flight, Aerogel
Cherenkov Counter →
Time-of-Propagation counter
(barrel),
prox. focusing Aerogel RICH
(forward)
7.4 m
RPC µ & KL counter:
scintillator + Si-PM
for end-caps
5.0 m
CsI(Tl) EM calorimeter:
waveform sampling
electronics, pure CsI
for end-caps
4 layers DS Si Vertex
Detector →
2 layers PXD (DEPFET),
4 layers DSSD
Central Drift Chamber:
smaller cell size,
long lever arm

## Slide 127: Requirements for the Belle II detector
- gb reduced by a factor of 2: compensated by improved vertexing
radiation damage and occupancy
fake hits and pile-up noise in the EM Calorimeter
- higher rate trigger, DAQ and computing
Critical issues at L= 8 x 1035/cm2/sec
4 Higher background ( 10-20)
4 Higher event rate ( 10)
4 Special features required
Result: significant upgrade

## Slide 128
Significant improvement in z-vertex resolution
PXD: 2 layer Si pixel detector (DEPFET technology) (R = 1.4, 2.2 cm)
monolithic sensor
thickness 75 µm (!),
pixel size 50 x 55 µm² to 50 x 85µm² (depending on layer and z)
SVD: 4 layer Si strip detector (DSSD) (R = 3.8, 8.0, 11.5, 14.0 cm)
15mm
30mm
Belle
Belle II
pbsin(q) [GeV/c]
0.4
2.0
0
0.8
1.2
1.6
100
20
50
σ [µm]
PXD
PXD+SVD
Silicon Tracking System @ Belle II

## Slide 129: How does this compare?
Resolution
Distance to IP
Material (scattering)
Belle II
Belle II almost reaches
ILC performance
(note p < 2 GeV/c² at Belle)

## Slide 130: Sensor Module/Ladder

## Slide 131: ASICs for control and readout
Switcher
Control of gate and clear
32 x 2 channels
Switches up to 30V
AMS 0.18 µm HV technology
Tested up to 36 Mrad
DCDB
Amplification and digitization of DEPFET signals
256 input channels
8-bit ADC per channel
92 ns sampling time
UMC 180nm
Rad hard design
DHP
Signal processor
Common mode correction
Pedestal subtraction
0-supression
Timing and trigger control
TSMC 65nm
Rad hard design

## Slide 132: Sensor Thinning
?
Process backside
e.g. structured implant
Wafer bonding
SOI process
Thinning of top wafer (CMP)
Processing
etching of handle wafer (structured)
diodes and large mechanical samples
Belle II module
Need thin (50µm-75µm) self supporting all silicon module
450mm
50mm
Cut through the matrix

## Slide 133: Prototype at a beam test
Strip detector
2nd layer PXD
1st layer PXD
Cooling block

## Slide 134: All-silicon module – material budget (single layer)
 | Belle II
Frame thickness | 525 µm
Sensitive layer | 75 µm
Switcher thickness | 500µm
Cu layer | only on periphery
Total | 0.21 %X0

## Slide 135: Injection Noise & Gating
Sensor filled with hits from freshly injected bunches => ~ 20% dead time
Gating : Sensor is made blind for a short time during high background (noisy bunch)
Signals detected in the clean period before are preserved
Simulations, lab tests with lasers and particle beams demonstrate feasibility of gating

## Slide 136: Gated Operation
In normal clear operation
the gate is pulsed negatively
(repells electrons)
The clear is pulsed positively
(attracts electrons from internal gate and bulk underneath)
In gated mode the gate is
not pulsed,
Remains attractive for electrons
The clear is pulsed positively,
Attracte electrons fro, bulk underneath

## Slide 137: Electron drift directions
Normal operation:
Signal charge drifts into internal gate
Gated Mode
Charges from background drift directly to clear gate
Signal already stored in internal gate is protected

## Slide 138: Tests with laser
No clear
clear
Protection of signal
Rejection of background
E. Prinker

## Slide 139: More DEPFETs
Like gating other interesting detectors can be constructed based on DEPFETs

## Slide 140: Repetitive Readout
repetitive
non destructive
readout
Multiple measurement of signal charge reduces 1/f noise
rms noise < 0.25 e
counts individual signal electrons!

## Slide 141: End of 2nd Lecture

## Slide 142: Punch through biassing
Vpunch through (V-)
Matrix (not connected)
Vbulk (0V)
Backside (not directly accessible)
75µm
Illustrations by Rainer Richter, MPG HLL
n bulk
p contact
n+ ohmic contact

## Slide 143: Punch Through Characteristic I-V curve

## Slide 144: Punch Through Characteristic [I]
Depletion region expanding from punchthrough contact into the bulk
(small volume -> small leakage current)
Vpunch through
Vbulk
Phase 1
Depletion expands

## Slide 145: Punch Through Characteristic [II]
Depletion region reaches backside
(sudden increase of leakage current due surface generation at backside)
Vpunch through
Vbulk
Backside reached
Interface current
bulk current

## Slide 146: Punch Through Characteristic [III]
Depletion region expands from the entire backside implant into the bulk
(small increase of current due to volume increase)
Interface current
bulk current
Vpunch through
Vbulk
entire bulk gets depleted

## Slide 147: Punch Through Characteristic [IV]
generation states are getting activated generation current at upper surface
Vpunch through
Vbulk
Active generation centers
Interface current
bulk current
Interface and surface currents

## Slide 148: Punch Through Characteristic [V]
All generation states are activated generation current saturates
Vpunch through
Vbulk
Generation current saturates
Interface current
bulk current
Interface and surface currents