## Slide 1: Ladder Assembly Improved Procedure
22st International Workshop on DEPFET Detectors and Applications
8th April 2018
Hans-Guenther Moser, Felix Mueller, Enrico Toeppner

## Slide 2: Accidents L2_022
L2_022: BWD module mechanically broken due to height offset
~90 um
W06_OB1
W11_OF2
⇩
L2_023: dummy modules glued → procedure “okay”
W11_OF2: power up without any problem

## Slide 3: Accidents – L2_024
L2_024: particles on surface caused shorts in some pixels
  gate-off and gate-on in current limit during power up
  source current (20 mA) although gates are off
  shorts over matrix → current flows directly to drains
~9 um
W44_OB1
W12_OF1

## Slide 4: L2_024 – repair and effect
W44_OB1
W12_OF1
HV current too high if HV is lower than -35 V
=> Ladder is broken

## Slide 5: Discussions and Conclusions about accidents
Ladder gluing procedure needs to be revised!
  Clean all modules before the assembly – send to HLL
    Remove particles by air
    Remove particles by special Q-tips
  Clean the module jigs just before they are used
    Use the microscope for optical inspection
    Use Flashlight, Q-tips and needles to see and remove particles
    Document with pictures (see next slides)
  Check vacuum!
    Used manometer to measure the vacuum strength
    0.4 bar at vacuum pump (tubes and jig need to be considered)
    negligible (0.06 bar) vacuum at jig, which is exposed to modules (see next slides)
    Inspect jigs for burrs (Grate): optical and with straightedge (Haarlineal)

## Slide 6: Vacuum strength
Pump on
=> difference: -60 mbar
Pump off

## Slide 7: Pictures of the jig before gluing
Remove it by tweezers
L1 set 1, FWD

## Slide 8: Dummy Module W01_IF before gluing
Use LUJ-SMcs to protect. After removing it again:
Use filtered air in order to remove the particles from the surface
Initial condition
LUJ-SMcs =
ladder universal jig – sensor module clamping set

## Slide 9: Transfer on vacuum jig
Vacuum jig for turning and ladder gluing
fits on top side (cut outs for switcher)
Mode from microporous plate (gentle vacuum on sensor top side)
Modules arrive with kapton attached (tested)
Vacuum jig on sensor
Screw kapton jig to vacuum jig
Unscrew kapton jig from base jig

## Slide 10: Remove base jig
Turn around and take off base jig (LUJ-Sbj)

## Slide 11: Prepare for glue dispensing
Add clamping set (LUJ-SMcs)
to be sure: module is securely held by
vacuum…

## Slide 12: Mount on glue dispenser
2nd module is prepared the same way
Glue is automatically dispensed on both modules in one step

## Slide 13: Glue Dispenser

## Slide 14: Place modules on alignment jig
bwd module 1st
fwd module 2nd

## Slide 15: Align and glue together
Precision achieved:
10 µm over full length of ladder
Modules are pushed together to 30 µm to ensure good contact and distribution of the glue.
Then they are driven apart to the nominal gap of 80 µm

## Slide 16: Add ceramic stiffeners
Stiffeners are handled with a vacuum tool
Glue is applied with a needle (works better than with a dispenser)

## Slide 17: 48h later….
After curing ladder base jig is added
For curing the ladder is covered and put apart

## Slide 18: Remove vacuum jigs
Fix kapton jigs to ladder base jig
Unscrew vacuum jig
Remove ladder and turn over

## Slide 19: Protect and store
Add cover for sensors
Put in transport/storage box

## Slide 20: Pictures after gluing L1_025 – before gluing L1_026
L1 set 1, FWD
Using Q-tip, needle and air

## Slide 21: Pictures after gluing

## Slide 22: Protocol
Glue gap
Delta z
Delta x
Delta h

## Slide 23
Summary – Dummies / Prototypes
Dummy ladders assembled
  plain thinned silicon, plastic ‘kapton’
  thinned silicon with copper, real kapton
  Including ASIC dummies
  L1_025 (W08_IB & W01_IF)
  L1_026 (W10_IB & W38_IF)
  L1_027 (W33_IB & W33_IF) – currently done
2 Prototype ladders produced
  L1_012 (W37_IB & W31_IF)
  L2_010 (W31_OB1 & W30_OF1)
  L2_023

## Slide 24
Summary – L1 Modules & L1 Ladders
Production ladders produced
  L1_012 - Switchers removed
  L1_013 - overheated & separated
  ✔ L1_014 – IB: many broken pixels (G94.4)
  ✔L1_015
  L1_016 – short (10 drains affected, rest working)
  ✔L1_017
  ✔L1_018
  ✔L1_019 - Switcher power off problem
  ✔L1_020
  ✔L1_021
Future ladders
  W03_IB, W42_IB fully tested (grade A)
  W09_IB, W43_IF (kapton rework / reattachment)
  P3-6: W04_IB, W13_IB, W09_IF, W13_IF (wait for Kapton attachment)
  W04_IF need some rework (strange pedestal picture, HLL)

## Slide 25
Summary L2 Modules & Ladders
Production ladders produced
  L2_022 – mechanically broking during gluing process
  L2_024 – surface mechanically damaged during gluing
Future ladders
  W09_OF1, W09_OB1, W43_OF1 (kapton rework / reattachment or Switcher rework)
  W32_OB2, W33_OB1, W42_OB1, W42_OB2, W45_OB2, W46_OB1, W08_OB1, W08_OB2, W09_OB2 (grade A)
  W12_OB1, W12_OB2 (grade B)
  W46_OB2, W05_OB1 (unknown grade)
  W44_OB2, W03_OB1 (under test)
  W09_OB1, W04_OB1, W10_OB1 (P3-7, waiting for kapton attachment)
  W32_OF1, W32_OF2, W33_OF2, W41_OF1, W45_OF1, W08_OF2, W11_OF1, W33_OF1 (grade A)
  W46_OF1, W46_OF2 (under test)
  W45_OF2 (DHP short, reworked)
  W02_OF1, W03_OF2, W04_OF1, W05_OF1 (waiting for Kapton attachment)

## Slide 26: Backup

## Slide 27
Pull Tests
Strip pattern: breaks at > 3 kg
Dot pattern weaker (~2 kg)
3 kg is considered sufficient (silicon breaks at ~3 kg)
Confirmed by pull test of dummy ladder
=> 3.9 kg =>