## Slide 1: DEPFETs for the GREST project
A. Bähr, A. Feller, D. Mießner, J. Ninkovic, M. Polovykh, R. Richter, F. Schopper, J. Treis
22nd International Workshop on DEPFET Detectors and Applications

## Slide 2: GREST - Getting Ready for the European Solar Telescope
Notes: A venture for the development of new technologies for the application at EST

## Slide 3: GREST
Notes: Through Modulator and Analyzer, the polarisation at a given point in time is encoded as intensity variation. By detecting the intensity variation for 4 different polarization states, the complete polarization information can be retrieved.
For standard sensors Modulation and Frame rate are coupled.

## Slide 4: GREST
Modulation ~ 10 kHz
Frame-Rate ~ 400 Hz
Notes: We intend to built a sensor that is capable to decouple modulation frequency and frame rate.
How are we going to do that?

## Slide 5: DEPFET
intrinsic amplification
low noise
backside illumination
100% fill-factor
intrinsic amplification
low noise
backside illumination
100% fill-factor

## Slide 6: DEPFET
intrinsic amplification
low noise
backside illumination
100% fill-factor

## Slide 7: DEPFET
intrinsic amplification
low noise
backside illumination
100% fill-factor

## Slide 8: Quadropix
four storage areas
fast modulation

## Slide 9: Quadropix
four storage areas
fast modulation

## Slide 10: Quadropix
four storage areas
fast modulation

## Slide 11: Quadropix
four storage areas
fast modulation

## Slide 12: Quadropix
four storage areas
fast modulation
gate A/B
gate C/D
source A/D
source B/C
drain A
drain B
drain D
drain C
clear A/D
cleargate A/D
clear B/C
cleargate B/C

## Slide 13: Prototype Sensor
production of first batch finished
Test Sensor: 64 x 32 Quadropixel
60 x 60 µm² pixel size
450 µm bulk
Notes: Devices were fabricated based on 2D simulations
prototypes are produced and were already pre-characterized

## Slide 14: Measurement Setup
B

## Slide 15: Test Sequence

## Slide 16: Target Measurement
injection while A collects

## Slide 17: Target Measurement
injection while B collects

## Slide 18: Target Measurement
injection while C collects

## Slide 19: Target Measurement
injection while D collects

## Slide 20: Standard Buffer

## Slide 21: Debugging Buffer

## Slide 22: Debugging Buffer / ?Cross – Talk?

## Slide 23: Debugging Buffer / ?Cross – Talk?

## Slide 24: Backside Sweep
-79 V

## Slide 25: Backside Sweep
-80 V

## Slide 26: Backside Sweep
-81 V

## Slide 27: Backside Sweep
-82 V

## Slide 28: Backside Sweep
-83 V

## Slide 29: Backside Sweep
-84 V

## Slide 30: Backside Sweep
-85 V

## Slide 31: Backside Sweep
-86 V

## Slide 32: Backside Sweep
-87 V

## Slide 33: Backside Sweep
-88 V

## Slide 34: Measurement Setup
B
Notes: Optical desing provided by Alexander Feller from MPS

## Slide 35: Pinhole Measurement

## Slide 36: Pinhole Measurement / left-right

## Slide 37: Pinhole Measurement / top-bottom

## Slide 38: 55Fe Spectrum
median noise of:
2.9 e- (first readout)
2.4 e- (second readout)
FWHM ~ 150 eV
T=-30C

## Slide 39: Intermediate Conclusion
B
Quadropix concept is functional
limited operation window for backside voltage
large and asymmetric spreading of charge over multiple pixels

## Slide 40: Intermediate Conclusion
B
Quadropix concept is functional
limited operation window for backside voltage
large and asymmetric spreading of charge over multiple pixels

## Slide 41: TCAD simulations
for details see: Bähr et al „Advanded DePFET concepts: Quadropix“
https://doi.org/10.1016/j.nima.2017.10.048
small operation window for standard geometry
optimization incrases operation window up to about 10 V

## Slide 42: TCAD simulations
standard device, close approximation of testes sensor

## Slide 43: TCAD simulations
standard device, thin (50 µm) substrate

## Slide 44: TCAD simulations
standard device, thin (50 µm) substrate, focussing implant on the backside

## Slide 45: Polarimetric Crosstalk (based on TCAD simulations)
standard device, close approximation of testes sensor
center
lower left

## Slide 46: Polarimetric Crosstalk (based on TCAD simulations)
standard device, thin (50 µm) substrate, focussing implant on the backside
center
lower left

## Slide 47: Conclusion
B
Quadropix concept functional
optimization of geometry already investigated by simulations -> possible

## Slide 48
B
Thanks for your attention