## Slide 1: S/N for thin DEPFETs in the Belle II environment – simple calculus –

## Slide 2: Assumptions …
DEPFET: 50x50 mm2
gQ = 400 pA/e gQ ~ (dOX/Lgate3 )1/2
Electronic noise
Single sampling no pedestal correction with 20ms read out time
47nA  ENC = 117e
Single sampling with pedestal correction with 20ms read out time
30nA  ENC = 88e
Double correlated sampling with 20ms read out time
102nA  ENC = 300e
Device noise
DEPFET noise 40e

## Slide 3: Assumptions …
Bulk contribution
1% occupancy  F = 1·1013 n/cm2
I0= 100pA/cm2 (bulk leakage current from produced thin PIN diodes)
Surface generated current (10Mrad)
I (depfet area) = 12 pA

## Slide 4: S/N for the thin DEPFETs in the Belle II environment …
Noise [e]
Single sampling w/o pedestal subtraction

## Slide 5: S/N for the thin DEPFETs in the Belle II environment …

## Slide 6: S/N for the thin DEPFETs in the Belle II environment …

## Slide 7: S/N for the thin DEPFETs in the Belle II environment …
Thickness Elect. noise T[°C] | 50mm S-S w Ped | 75mm S-S w Ped | 50mm S-S w/o Ped | 75mm S-S w/o Ped | 50mm D-S | 75mm D-S
20 | 28 | 39 | 21 | 30 | 10.9 | 16.2
30 | 23 | 32 | 19 | 26 | 10.6 | 15.5
40 | 18.3 | 24.2 | 15.8 | 21.5 | 10.0 | 14.3

## Slide 8: DEPFET – Transconductance
gm is 25% lower after 7.5MRad

## Slide 9: S/N for the thin DEPFETs in the Belle II environment …

## Slide 10: S/N for the thin DEPFETs in the Belle II environment …
Thickness Elect. noise T[°C] | 50mm S-S w Ped | 75mm S-S w Ped | 50mm S-S w/o Ped | 75mm S-S w/o Ped | 50mm D-S | 75mm D-S
20 | 28 | 39 | 21 | 30 | 10.9 | 16.2
30 | 23 | 32 | 19 | 26 | 10.6 | 15.5
40 | 18.3 | 24.2 | 15.8 | 21.5 | 10.0 | 14.3
Thickness Elect. noise T[°C] | 50mm S-S w/o Ped | 75mm S-S w/o Ped
20 | 18.4 | 26.7
30 | 16.8 | 23.9
40 | 14.6 | 20.2
7.5 MRad

## Slide 11: gQ variations

## Slide 12: gQ variations