## Slide 1: A Reliable Approach to Charge-Pumping Measurements in MOS-Transistors
Paper Presentation for the Students Seminar
Andreas Ritter – 7.4.2010

## Slide 2
What is this Paper about?
It’s about Traps…
…and how they can be filled

## Slide 3
Interface Traps depend on: Density
[111]
[100]
…and Location

## Slide 4
Interface Traps depend on: Speed

## Slide 5
Interface Traps depend on: Speed

## Slide 6: Interface Traps – Origin and Generation

## Slide 7
At the Interface between Si and SiO2…
Lattice constants of Si and SiO2 do not match
open bindings
highly electrically active

## Slide 8
At the Interface between Si and SiO2…
H2 diff zum Interface
passivation
Nicht alle getroffen
Paar übrig, liegen 0.2 eV
Von der andkante
Use Hydrogen (Forming Gas) to get rid of Interface Traps
Passivation

## Slide 9
At the Interface between Si and SiO2…
Ionizing radiation creates/frees protons somewhere in the device.
Via diffusion and drift Hydrogen nuclei get to the interface.
H+ + Si-H  Si+ + H2

## Slide 10
At the Interface between Si and SiO2…
The most common interface trap is called Pb.
Hot-electron induced passivation of silicon dangling bonds
at the Si(111)/SiO2 interface
E. Cartier and J. H. Stathis from
Appl. Phys. Lett., Vol. 69, No. 1, 1 July 1996
Interface trap is amphoteric = act as Donor or as Acceptor.
In lower Half Band Gap mostly acceptor type, in the upper half donor-type.

## Slide 11: Charge Pumping – Basic Working Principle

## Slide 12
Measurement Setup
Pulse Generator drives Layer beneath the Gate into Inversion and Accumulation
Current Meter measures the net current ICP
Vrev is set at a certain reverse Voltage – no influence on the charge pumping current ICP

## Slide 13
Working Principle – Strong Inversion
Transistor is in Strong Inversion
Most of Interface Traps occupied with holes

## Slide 14
Working Principle
Transistor is in Strong Inversion
Most of Interface Traps occupied with holes

## Slide 15
Working Principle
Transistor is going from Inversion to Accumulation
Emission of holes from Interface Traps too slowly – Traps remain occupied

## Slide 16
Working Principle
Transistor in Accumulation
Occupied traps (with holes) are reloaded with electrons

## Slide 17
Working Principle
Transistor in Accumulation
Traps are now occupied with electrons
Emission of electrons is too slowly – Circle starts again…

## Slide 18
Working Principle
Transistor in Accumulation
Traps are now occupied with electrons
Emission of electrons is too slowly – Circle starts again…

## Slide 19
Measurement Data - Current
Charge in Interface Traps is
and applying a frequency
Assuming a mean surface trap density

## Slide 20
Four Currents
During One Cycle there exist four currents:
  ICP due to hole emission
  ICP from electron neutralizing hole occupied traps
  ICP from electron emission
  ICP due to holes neutralizing electrons occupied traps
Net current flowing out to the bulk:
and through Source and Drain:

## Slide 22
Four currents…One device