## Slide 1: DePFET for the ATHENA Wide Field Imager DePFET Workshop München, 18.05.22
Alexander Bähr
MPG HLL
on behalf of the ATHENA WFI sensor teams

## Slide 2: Contributors
Alexander Bähr
Peter Lechner
Raik Lehmann
Danilo Mießner
Jelena Ninković
Rainer Richter
Gerhard Schaller
Florian Schopper
Johannes Treis
Christian Zirr
WFI PI-ship
Annika Behrens
Michael Bonholzer
Valentin Emberger
Norbert Meidinger
Johannes Müller-Seidlitz
Kirpal Nandra (PI)
Wolfgang Treberspurg
Semiconductor Lab
of Max-Planck-Society
Munich, Germany
Max-Planck-Institute for Extraterrstrial Physics
Garching, Germany
concept & layout
fabrication
device test
readout & control electronics
data acquisition
focal plane architecture
wafer & die level test
assembly

## Slide 3: ATHENA Mission
ESA's 2nd 'Cosmic Vision' L-class mission
  next large X-ray observatory
  launch ~ 2030, Ariane 6.4, life time > 4 y
  halo orbit around Lagrange point L2
  science theme: 'The Hot & Energetic Universe'
    formation of large scale structures
    evolution of black holes
instrumentation
  movable mirror array
    Si pore optics
    effective area > 1.4 m² @ 1 keV
    angular resolution 5 arcsec HEW
    focal length 12 m
  X-ray Integral Field Unit (X-IFU)
    cryogenic transition edge sensor
    highest resolution 2.5 eV @ 6 keV
    field of view 5 arcmin
    pixels 3840 (x 250 µm )
    temperature 50 mK
  Wide Field Imager (WFI)
movable mirror array
(Advanced Telescope for High ENergy Astrophysics)
cosine/ESA
science instrument module
Si pore optics
modules
X-IFU
WFI

## Slide 4: ATHENA Wide Field Imager
large-area detector, 'the' Wide Field Imager
4 identical tiles 512 x 512
gap compensation by dithering
X-ray imaging spectrometer with spectral, position and time resolution
science drivers
specifications
  point source
  sensitivity
  angular resolution
  ≤ 5 arcsec
  < 0.3 mm
  survey power
  field of view
  ≥ 40 arcmin
  ≥ 14 cm Ø
  pile-up limit
  line spectroscopy
  energy resolution
  < 80 eV @ 1 keV
  < 170 eV @ 7 keV
  quantum efficiency
  energy range
  0.1 … 15 keV
  light-curve of bright point sources
  transients
  rate capability (1 Crab*)
  throughput > 90 %
  pile-up < 1 %
  time resolution
* 1 Crab ≈ 105 cps
WFI parameters
  pixel size
  130 µm 
  > 2x oversampling
  format
  1024 x 1024 pixels
  14 x 14 cm²
  row / frame time
  ≤ 10 µsec / 5 msec
  low electronic noise
  ≤ 10 el. ENC
  thin entrance window
  thickness 450 µm
  position out of focus
  ~ 35 mm
  4 mm PSF
  frame time
  ≤ 80 µsec
high-rate detector
64 x 64 version of WFI
identical layout & technology
identical readout & control
out of focal plane, no imaging
ATHENA WFI focal plane arrangement
  Mo structure
  thermal connection by heat pipes / thermal straps
structure: 0 °C, front-end: -20 °C, sensor: -60 … -80 °C

## Slide 5: DePFET
(DEpleted P-channel Field Effect Transistor)
principle
  p-FET on depleted n-bulk
  signal charge collection in potential well below FET channel ('internal gate')
  drain current modulation, Ơ(100 pA/el.)
combined sensor & amplifier
  low capacitance (20 fF) and noise
   excellent spectroscopic performance
  complete clearing of signal charge
   no reset noise
  charge storage capability
   readout on demand
  non-destructive readout
   potential of repetitive readout
  backside illuminated, fully depleted
   quantum efficiency
readout sequence
equivalent circuit
readout sequence
  1st measurement: signal + baseline
  clear: removal of signal charges
  2nd measurement: baseline
  difference = signal
  settling times after switch-on & clear

## Slide 6: Production Overview
prototype production (PXD11)
  may15 – nov16
  many small devices
  layout & technology variations
  selection of best variant
pre-flight production (PXD12)
  2 batches
  oct17 – jun19, jan18 -
  consolidated layout & technology
  final device formats
    quadrant 512 x 512
    fast timing 64 x 64 split frame
flight production
  mid2020 –
  unchanged layout & technology
  wafer number

## Slide 7: Prototype Production PXD11 - DePFET Layout
performance (64 x 64 prototypes)
  gain
  noise
  timing
ATHENA WFI layout: linear gate
previous generations: circular gate
  e.g. BepiColombo MIXS
  analytical DePFET model
W/L = 25 µm / 3.5 µm
W/L = 45 µm / 5 µm

## Slide 8: Prototype Production PXD11 - Readout Electronics
source follower
  stable configuration
  easy to operate
  speed limitation by parasitic line capacitance
drain current readout
  motivation: the need 4 speed
  DePFET terminals at fixed potentials
  requires homogeneity of DePFET characteristics
  VERITAS redesign with reduced I2V gain to widen the input range
Sven Herrmann / SLAC, BNL
comparison
  VERITAS 2.1 offers both input stages
  drain current configuration can double the readout speed for large matrices, e.g. circular gate devices:
readout mode | source follower |  | drain current |  | 
time / row [µsec] | 9.8 | 13.8 | 2.5 | 5.0 | 8.7
FWHM [eV] @ 5.9 keV | 156 | 138 | 174 | 145 | 135
ENC [el. r.m.s.] | 4.98 | 2.85 | 7.70 | 4.95 | 3.93

## Slide 9: Prototype Production PXD11
P-format 64 x 64
  ~ ATHENA WFI fast detector
spectroscopy performance
  55Fe source, Mn-Ka line 5.9 keV
  processing time per row 2.5 µsec
  energy resolution FWHM 128 eV
  mean pixel noise 2.3 el. ENC

## Slide 10: Prototype Production PXD11
quarter format 256 x 256
  ~ ATHENA WFI large area detector
spectroscopy performance
  55Fe source, Mn-Ka line 5.9 keV
  processing time per row 9.8 µsec
  energy resolution FWHM 128 eV
  mean pixel noise 1.8 el. ENC

## Slide 11: Prototype Production PXD11
quarter format 256 x 256
  ~ ATHENA WFI large area detector
spectroscopy performance
  multi-target X-ray tube
  processing time per row 9.8 µsec
  energy resolution FWHM 50 eV @ 183 eV B
  57 eV @ 525 eV O
  69 eV @ 1.5 keV Al
  128 eV @ 5.9 keV Mg
  174 eV @ 11 keV Ge

## Slide 12: Prototype Production PXD11 – lessons learned
pxd11 - quarter devices
pass
fail
handling
inline yield test
  using global contacts
    gate (polySi2)
    cleargate (polySi1)
    clear (n-implant)
    ring2 (p-implant)
  detectable
    vertical shorts between layers
    lateral shorts within layers
    diode integrity
  not detectable
    defect number, nature & location
    missing contacts

## Slide 13: Prototype Production PXD11 – lessons learned
lesson 1 learned from PXD11
  random polySi etching imperfections
  single, isolated defects polySi 1 & 2
  not detected by µTEC inspection system
  detected and identified by PHEMOS emission microscope
  uneven edges of polySi structures, "nose"
   short by touching neighbouring via
tiled image of 256 x 256 quarter device by PHEMOS light-emission microscope
short cleargate - clear
short gate - drain

## Slide 14: Prototype Production PXD11 – lessons learned
automatic inspection system
  optics update: magnification x10  x50
  reliable detection of defects ≥ 500 nm
  smaller defects irrelevant
  virtual die-die comparison within a large format device
  computation time ~ 5 h per wafer
polySi process optimisation
  test project, ~ 50 wafers
  ATHENA WFI representative layouts
  optimisation of polySi lithography & etching
    new development recipe
    polySi patterning with photoresist, no LTO hardmask
    smooth & straight edges
    ideal climbing over polySi1 steps
x10
x50
artificial defect

## Slide 15: Prototype Production PXD11 – lessons learned
lesson 2 learned from PXD11
  suspicion of metal shorts
  related to device type
  rework of pixel layout
  PXD11 prototype
    compact DePFET dimensions
    gate extension for via placement
    vertical polySi1 & 2 stack
    frequent changes between metal layers 1 & 2
    narrow gaps in metal layers
  PXD12 pre-flight
    relaxed DePFET layout
    extended S & D regions, W & L unchanged
    cleaned-up metal system
    min. number of vias
    full testability after metal 1
    confirmed by 3D device simulation

## Slide 16: Pre-Flight Production PXD12
final layout & technology
large area imager quadrant
  format 512 x 512
  sensitive area 66.56 x 66.56 mm²
  chip size 78.00 x 76.15 mm²
  inner edges 2 mm
  rolling shutter mode
  displaced bond pads
high rate detector
  format 64 x 64
  chip size 16.00 x 16.00 mm²
  split frame readout
  one row per hemisphere  2 r/o ASICs
  two rows per hemisphere  4 r/o ASICs
first devices available beginning 2019
ATHENA WFI quadrant
ATHENA WFI
fast detector
2 rows readout
ATHENA WFI
fast detector
4 rows readout
PXD12 wafer map

## Slide 17: Pre-Flight Production PXD12 - Fast Detector (FD)
Excellent spectroscopic performance of the first fast detector was confirmed with the measurement of further emission lines (see below).
A second FD was mounted and investigated. FD#2 verified the performance of FD#1.
Spectral performance of the first Fast Detector for different emission lines. All measurements were done at the required readout speed of 80 µs per frame.
Fast Detector mounted in a vacuum chamber. An 55Fe source is located in the holdfast on the left.

## Slide 18: Pre-Flight Production PXD12
quadrant device
  mounted at HLL
  operated by MPE detector group
  non-functioning
  identified defect: short source – ring1
short in all large devices from PXD12-2

## Slide 19: Pre-Flight Production PXD12
failure mechanism
  intra-layer short within metal1
   ruled out by layout
  inter-layer short by insufficient insulation
   triple stack polySi/metal1/metal2
  not known from previous productions
  no repair option for diced chips (PXD12.2)
PXD12 pixel layout
conductive layers
 metal1
 metal2
 polySi
PXD12 pixel micro-photograph
source
source
ring1

## Slide 20: Pre-Flight Production PXD12
repair approach for wafers of PXD12.3
  etching of metal2 lines
    isolated metal2 islands
      at critical triple stacks
      at contact holes
  only inside pixel, periphery unchanged
  short circuit source/ring1 disappeared
  new metal3 layer required
after metal2 etching
PXD12 pixel layout
conductive layers
metal 2 etching mask
source
ring1

## Slide 21: Pre-Flight Production PXD12
metal3 layer
  replacement of metal2 lines
  modified layout, avoidance of triple stacks
  source/ring1 insulation still ok
  other tests nominal, working device
after metal3 patterning
PXD12 pixel layout
conductive layers
metal3 layer

## Slide 22: Pre-Flight Production PXD12 - Large Detector (LD)
Spectrum taken with a Large Detector and an 55Fe source at a frame time of 2 ms. Due to the large fraction of readout to exposure time of a Large Detector, the detector-induced background is low and various fluorescence lines of elements used in the vacuum chamber are visible.
Spectroscopic performance of a Large Detector measured for different frame times. For all measurements with a frame time of > 1.5 ms the signal shaping time of the Veritas ASIC was kept constant. The increase of settling times does not improve the overall spectral performance.
Large Detector Module connected to its cooling interface used in the laboratory test setups.

## Slide 23: Pre-Flight Production PXD12 - Large Detector (LD)
unexpected noise pattern
some pixels show factor 2-3 higher noise
can be reduced by data analysis
could limit low energy resolution
not observer for any device before
origin is still unknown

## Slide 24: Flight Production (PXD14)
wafer layout
  updated pixel layout
  flight devices
    1 x quadrant 512 x 512
    4 x fast detector 64 x 64
  others
    18 x WFI-like 64 x 64
    29 x diodes 10 mm², 64 mm² for qeff measurements
production
  start Sep 20
  volume: 36 wafers
  sub-batches 3 x 12 wafers
  1 batch before aluminum deposition
  2 batches in poly process
PXD14 wafer layout

## Slide 25: Summary
ATHENA
  one of the biggest European science projects of the coming decades
DePFET-based Wide Field Imager
  superior performance demonstrated by PXD11 prototypes
  challenge of a large number of large format devices
  positive results of pre-flight production PXD12
  still open questions

## Slide 26: Full Frame Readout
parallel readout
  increasing probability of photon events during readout sequence
  false energy information-energy
internal storage DePFET
  two DePFETs per pixel
  alternating function
    ON readout
    OFF collection & storage
prototype demonstration
  repetition rate 1/10 µsec
  false event contribution to low-energy background reduced
full frame readout device
  127 hexagonal pixels, Ø = 800 µm
  X-ray spectroscopy (& imaging) at frame rate > 100 kHz
  not baseline for ATHENA WFI

## Slide 27: DePFET Active Pixel Sensor
matrix organisation
  horizontal supply lines
    clocked voltages connected to SWITCHER ASIC
    global contacts connected to bond pads
  vertical signal lines
    connected to VERITAS readout ASIC
  individually addressable pixels
  optional windowing mode
rolling shutter mode operation
  one active row
    DePFETs on
    read-clear-read sequence
    column-parallel readout
  other rows integrating signals
    DePFETs off
ATHENA WFI prototype 64 x 64
front-end electronics
  SWITCHER-A control ASIC
    supply of clocked voltages
    row selection & reset
    64 channels, 3 ports each
    daisy-chainable
    row switching rate 10 MHz
    rise time < 10 nsec @ 20 V
  VERITAS 2.1 readout ASIC
    64 channels
    fully differential
    selectable input stages
      source follower
      current readout
    pre-amplifier
    trapezoidal filter
    64:1 multiplexer
ATHENA WFI pixel
  130 µm x 130 µm
  surrounding drift ring
  scalable format

## Slide 28: BepiColombo MIXS Heritage
BepiColombo mission
  magnetospheric & planetary orbiters
  launch oct18, arrival in orbit dec25
MIXS instrument
  Mercury surface elemental mapping
  MIXS-C (collimator), MIXS-T (telescope)
  DePFET Active Pixel Sensor
    active area 1.92 x 1.92 cm²
    format 64 x 64
    pixel size 300 x 300 µm²
    split frame readout 165 µsec
    energy resolution 138 eV FWHM @6 keV
Kourou, 19.10.2018
(Mercury Imaging X-ray Spectrometer)
figure: ESA
MPO
MMO
MIXS lab prototype detector

## Slide 29: Prototype Production PXD11
full width
512 x 64
full height
128 x 512
quarter
256 x 256
64 x 64
prototype production
  prototype 64 x 64 device flavour selection
  quarter 256 x 256 large area
  full width 512 x 64
  full height 128 x 512
purpose
  selection of technology variant
    thin gate oxide
    blanket deep n implanation
    wet etching of polySi structures
  selection of layout variant
    linear gate
    large clear
    halo implantation
status
  finished 2017
  fully analised
long connection lines

## Slide 30: Pre-Flight Production PXD12
inline yield test
  using global contacts
    gate (polySi2)
    cleargate (polySi1)
    clear (n-implant)
    ring2 (p-implant)
  detectable
    vertical shorts between layers
    lateral shorts within layers
    diode integrity
  not detectable
    defect number, nature & location
    missing contacts
pixel count
x4
pxd11 - quarter devices
pxd12, 1st sub-batch - quadrant devices
pass
fail
handling

## Slide 31: Pre-Flight Production PXD12
entrance window diode
  large area 44 cm²
  reverse current @ depletion 2.83 nA
  leakage current level 64 pA/cm²
  best PXD value so far

## Slide 32: Contents
ATHENA mission
Wide Field Imager
  requirements & specifications
  DePFET device
  DePFET Active Pixel Sensor
prototype production PXD11
  DePFET layout
  readout electronics
pre-flight production PXD12
flight production PXD14

## Slide 33: Pre-Flight Production PXD12
metal2 etching & metal3 deposition
  applied to metal1/metal2 contact chains
  contact between metal2 & metal3 
  climbing of metal3 
after metal2 etching
after metal3 deposition & patterning
metal2 etching
metal3 deposition & patterning

## Slide 34: Prototype Production PXD11
summary
  linear gate layout DePFET
  drain current readout
  excellent noise < 3 el. ENC
  fast readout 2.5 µsec / row
  fully in ATHENA WFI specs