## Slide 1: Irradiation of DEPFET transistors with 60CO up to 10 Mrad in Santiago
5th International Workshop on DEPFET Detectors and Applications 29 Sep -1 Oct Valencia (Spain)
Pablo Vázquez, Eliseo Pérez, Pablo Rodríguez (IGFAE-USC)

## Slide 2: Irradiation procedure
We have used the USC Radiation Physics Laboratory
  http://www.usc.es/en/investigacion/riaidt/radiofisica/index.html
It houses a cobalt 60 radioactive source of 2080 Ci of activity (as for May 2009) emitting gamma photons of 1.17 and 1.33 MeV of energy
Dose: 11.5 Krad/h (June 2010) -> 11.3 Krad/h (August 2010)
  T1/2(60CO) = 2.57 years
Irradiation was made in 11 steps up to 10 Mrad + annealing @ room T
  0.1 -> 0.2 -> 0.43 -> 0.7 -> 0.97 -> 1.95 -> 2.95 -> 4 -> 5.55 –> 7.45 -> 10 -> annealing (28 days)
  IV curves was measured for each transistor after each step
To measure the variations on
  Vth
  Gain
  Subthreshold zone
To study dependence on
  Vgs biasing
  Dopping
  Width/Length ratio

## Slide 3: Schedule (summer 2010)
2 power cuts on:
step 7 (2->3 Mrad)
step 12 (annealing)
Annealing of
8h (1 night) for step 0
60h (1 weedend) for step 1

## Slide 4: Setup (outside the bunker)
IV Test
Irradiation Biasing

## Slide 5: Setup (inside the bunker)
60Co source
2mm Pb
1mm Al
Ionizing chamber (PTW 30013) for dose measurement

## Slide 6: 4-Quadrant 2-Transistor structures
Instrumentation limited to 30 transistors over 172
QI -> 7
QII -> 11
QIV - > 12

## Slide 7: Transistor biasing during irradiation
Different biasing voltages were chosen to be applied during irradiation
Voltage | Value | Transistors
IG,bulk | 10 | all
Vs | 0 | all
Vd | -5 | 37
 | 0 | 23
Vgs | -5 | 6
 | -3 | 6
 | -2 | 6
 | -1 | 4
 | 0 | 24
 | 2 | 8
 | 5 | 6

## Slide 8: Status of transistors during irradiation
OK =>
  IV curve fine, can connect InternalGate
notOK =>
  cannot connect IG (Gate-IG short), I=cte for just one irradiation step, double slope in IV curve, Igs = Overflow for certain Vgs values…
KO =>
  I=cte or Overflow (>2mA) for several steps, sinusoidal shape
Status before irradiation
  OK = 55%; notOK = 40%; KO = 5%
Status after irradiation + annealing
  OK = 37%; notOK = 27%; KO = 25%
status | chip |  | column |  |  |  |  |  | Vgs |  |  |  |  |  |  | Shorts | 
 | 1 | 3 | 3 | 7 | 8 | 9 | 10 | 11 | -5 | -3 | -2 | -1 | 0 | 2 | 5 | Rgs | Rgig
OK | 11 | 11 | 6 | 4 | 6 | 2 | 5 | 1 | 3 | 3 | 2 | 3 | 6 | 2 | 3 | 50 | 27
notOK | 12 | 11 | 4 | 3 | 3 | 1 | 5 | 5 | 2 | 3 | 2 | 0 | 10 | 3 | 3 | 10 | 33
KO | 7 | 8 | 2 | 3 | 1 | 7 | 0 | 2 | 1 | 0 | 2 | 1 | 8 | 3 | 0 |  | 
Total | 30 | 30 | 12 | 10 | 10 | 10 | 10 | 8 | 6 | 6 | 6 | 4 | 24 | 8 | 6 | 60 | 60
Step | Mrad | InternalGate connected? | 
 |  | yes | no
S0 | 0 | 33 | 27
S1 | 0.1 | 28 | 32
S2 | 0.2 | 23 | 37
S3 | 0.43 | 23 | 37
S4 | 0.7 | 23 | 37
S5 | 1 | 23 | 37
S6 | 2 | 22 | 38
S7 | 3 | 21 | 39
S8 | 4 | 0 | 60
S9 | 5.5 | 0 | 60
S10 | 7.5 | 0 | 60
S11 | 10 | 0 | 60
S12 | anneal | 0 | 60

## Slide 9: The analysis (Gm, Vth)
Ids is made positive to be able to calculate the square root
  Ids = Ids - Idsmin in case Idsmin < 0
The linear trend of the curve sqrt(Ids) vs Vgs is searched
  A loop selects groups of 10 points and fit them to a straight line. The fit with the highest slope is selected and it gives:
  Gm: the slope (which is proportional to the transconductance gm)
    Gm = ∂(√Ids)/∂Vgs ; gm = ∂(Ids)/∂Vgs
    gm = 2 Gm (Vgs - Vth)
  Vth: the cross with the X-axis

## Slide 10: Ids vs Vgs, Vth, Gm for a good transistor

## Slide 11: Ids vs Vgs, Vth, Gm for a bad transistor
Behaves as a column 3 (full width) transistor
Behaves as a column 11 transistor

## Slide 12: Ids vs Vgs, Vth, Gm for a bad transistor
Double slope

## Slide 13: Ids vs Vgs, Vth, Gm for a bad transistor
Igs=cte for S4
Igs overflow

## Slide 14: The analysis (Subthreshold zone)
The Subthreshold zone is calcucated as the subtraction of the Vgs of the two points which determine the begining of conduction zone and the end of the cut zone
  Those points are the first ones with a distance to their fit > 10-4
1.3V
Distance to the conduction fit
Distance to the cut fit

## Slide 15: Vth shift vs dose (by quadrants & Vgs)
Points on 12 Mrad mean annealing
Vgs
-5
-2
-1
+5
Vgs
0
2
Vgs
-3
0
QIV has no IG implemented

## Slide 16: Gm vs dose (by quadrants & columns W/L)
W/L
20
6.7
W/L
20
6.7
1.7
1
W/L
13
6.7
3.3
1.7
1
W/L
20
6.7
1.7

## Slide 17: Subthreshold zone vs dose (by quadrants & W/L)
W/L
20
6.7
1.7
1
W/L
13
6.7
3.3
1.7
1
W/L
20
6.7
1.7

## Slide 18: Results
Vth shift after 10 Mrad ~23 V for transistors of QI,II and ~18 V in QIV
Vth shift decreases by 3.5 V after 28 deays of annealing
Vth shift decrease ~3.5 V changing Vgs from -5 V to 5V
Gm is a factor 4 below what spected from W/L ratio
Gm is reduced 40% after 10 Mrad and slightly recovers after the anealling
Subthreshold zone increases up to 4±2 V after 10 Mrad (the method is still not well tuned)
W/L | <Gm> 10Mrad
1 | -9.7E-04
1.7 | -1.2E-03
3.3 | -1.8E-03
6.7 | -2.4E-03
13 | -3.5E-03
20 | -4.3E-03
Chart: Vth_shift vs Vgs (10 Mrad)
| -5.0 | -2.0 | -1.0 | 0.0 | 2.0 | 5.0
Qi&QII | 23.45 | 22.85 | 22.87 | 23.57 | 22.23 | 21.17
QIV | 18.34 | 17.86

## Slide 19: Back up slides

## Slide 20: Distance to the conduction linear fit
Distance = 10-4

## Slide 21: Irradiation Board

## Slide 22: IV test board

## Slide 23: Irradiation housing board scheme
2 mm Pb
1mm Al
Ionizing
chamber
connector
adaptor
depfet
connector
adaptor
depfet
Patch panel pcb
15mm
45mm
45mm